| Appendix II. Comparison of XRF and ICP-MS analyses |
| --- |
| Area | Italy | Thomas Range | Long Valley Caldera | Taylor Creek |
| Units | Lipari | Topaz Mts. | Glass Creek | Obsidian Dome | Punch Bowl | Tt11/SMC |
| Sample # | 98502 | 98701 | 98702 | 98711 | 98712 | 98717 | 98911 |
| Rock Type | rhyolite | rhyolite | rhyolite | rhyolite | obsidian | rhyolite | rhyolite | rhyolite | rhyolite |
| Sample type | whole rock | glass | glass | glass | whole rock | whole rock | glass | whole rock | glass |
| Technique | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS |
| SiO2 | 73.95 | 73.61 | 74.41 |  | 73.96 |  | 73.59 |  | 73.40 | 74.23 | 76.65 | 75.19 | 76.27 |  | 76.59 | 77.39 | 75.49 |  |
| TiO2 | 0.04 | 0.07 | 0.08 |  | 0.06 |  | 0.06 |  | 0.10 | 0.14 | 0.01 | 0.06 | 0.03 |  | 0.08 | 0.12 | 0.09 |  |
| Al2O3 | 13.99 | 12.2 | 13.21 |  | 14.42 |  | 14.01 |  | 14.40 | 13.75 | 13.49 | 12.25 | 12.59 |  | 13.17 | 11.49 | 13.25 |  |
| FeO | 1.39 | 1.56 | 0.59 |  | 0.35 |  | 0.45 |  | 1.26 | 1.80 | 0.66 | 1.19 | 0.52 |  | 0.57 | 1.17 | 0.74 |  |
| MnO | 0.04 | 0.04 | 0.04 |  | 0.03 |  | 0.03 |  | 0.05 | 0.05 | 0.04 | 0.04 | 0.04 |  | 0.05 | 0.05 | 0.03 |  |
| MgO | 0.11 | 0.05 | 0.14 |  | 0.14 |  | 0.10 |  | 0.00 | 0.22 | 0.00 | 0.04 | 0.03 |  | 0.00 | 0.05 | 0.10 |  |
| CaO | 0.74 | 0.71 | 0.69 |  | 1.34 |  | 0.99 |  | 0.62 | 0.78 | 0.45 | 0.56 | 0.62 |  | 0.07 | 0.26 | 0.16 |  |
| Na2O | 3.85 | 3.53 | 3.97 |  | 4.52 |  | 4.25 |  | 4.51 | 4.26 | 4.12 | 3.85 | 4.33 |  | 4.12 | 3.63 | 4.23 |  |
| K2O | 5.17 | 5.09 | 4.65 |  | 4.95 |  | 4.37 |  | 4.86 | 5.37 | 4.40 | 4.77 | 4.19 |  | 4.65 | 4.75 | 4.88 |  |
| P2O5 | 0.01 | 0.02 | 0.00 |  | 0.00 |  | 0.01 |  | 0.05 | 0.20 | 0.04 | 0.34 | 0.01 |  | 0.03 | 0.08 | 0.02 |  |
| Total | 99.29 | 99.42 | 97.79 |  | 99.79 |  | 97.87 |  | 99.25 | 100.80 | 99.86 | 98.29 | 98.64 |  | 99.33 | 98.99 | 98.99 |  |
| Trace elements | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS |
| Rb | 288 | 252 | 345 | 413 | 424 | 464 | 144 | 161 | 164 | 149 | 186 | 161 | 187 | 213 | 352 | 317 | 393 | 454 |
| Sr | 11 | 13.2 | 14 | 15.1 | 15 | 15.8 | 142 | 148 | 44 | 42.7 | 8 | 8.1 | 3 | 3.9 | 6 | 5.5 | 3 | 4.1 |
| Ba | 5 | 6.5 | 21 | 27 | 26 | 19 | 315 | 344 | 353 | 349 | 21 | 25 | 15 | 15.5 | 23 | 22 | 16 | 11 |
| Y | 43 | 39.5 | 41.1 | 38.5 | 44.4 | 41.5 | 17.7 | 14.5 | 28 | 24.5 | 33 | 25 | 28.6 | 27 | 104 | 83.5 | 78.7 | 88.5 |
| Zr | 142 | 142.5 | 110 | 130 | 106 | 118.5 | 122 | 117 | 229 | 216 | 103 | 104.5 | 99 | 99.5 | 143 | 152 | 161 | 165 |
| Nb | 48 | 30 | 104 | 70 | 75 | 63 | 15 | 15 | 32 | 19 | 40 | 19 | 33 | 21 | 103 | 42 | 76 | 45 |
| Th | 44 | 41 | 65 | 55 | 59 | 58 | 15 | 12 | 23 | 23 | 19 | 21 | 22 | 17 | 34 | 37 | 40 | 32 |
| La |  | 42.5 |  |  |  |  |  |  | 83 | 78 | 22 | 26 |  |  | 42 | 41.5 |  |  |
| Ce |  | 83.5 |  |  |  |  |  |  | 150 | 139.5 | 49 | 50.5 |  |  | 106 | 100.5 |  |  |
| Nd |  | 35.5 |  |  |  |  |  |  | 50 | 45.5 | 26 | 22 |  |  | 46 | 38 |  |  |
| XRF analyses performed at Baylor University |
| ICP-MS analyses performed at ALS-Chemex Lab |
| * Calculated from quartz contamination correction |
| Appendix II. Comparison of XRF and ICP-MS analyses (continued) |
| Area | Taylor Creek | Valles Caldera | Valles Caldera | Long Valley |
| Units | Tt12/ | SMR | SMR | SMR | SMR | Punch Bowl |
| Sample # | 98912 | 93908B | 95811B | 98901 | 98901 | 98717 |
| Rock Type | rhyolite | rhyolite | rhyolite | rhyolite | rhyolite | rhyolite | rhyolite |
| Sample type | glass | whole rock | whole rock | whole rock | glass | plagioclase | plagioclase |
| Technique | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | EPMA | ICP-MS* |
| SiO2 | 73.01 |  | 76.29 | 75.88 | 75.93 | 74.17 | 77.20 | 76.19 | 74.20 |  | 64.03 | 65.27 | 64.78 | 63.31 |
| TiO2 | 0.06 |  | 0.09 | 0.14 | 0.08 | 0.12 | 0.08 | 0.12 | 0.02 |  | 0.01 | <0.01 |  | <0.01 |
| Al2O3 | 14.16 |  | 14.02 | 12.64 | 14.08 | 12.37 | 13.51 | 11.63 | 13.16 |  | 21.88 | 20.97 | 22.60 | 22.21 |
| FeO | 0.58 |  | 0.49 | 1.16 | 0.60 | 1.14 | 0.48 | 1.01 | 0.40 |  | 0.18 | 0.33 | 0.13 | 0.23 |
| MnO | 0.06 |  | 0.05 | 0.04 | 0.07 | 0.05 | 0.05 | 0.04 | 0.04 |  | 0.00 | <0.01 |  | <0.01 |
| MgO | 0.12 |  | 0.01 | 0.3 | 0.06 | 0.12 | 0.01 | 0.11 | 0.14 |  | 0.13 | <0.01 |  | <0.01 |
| CaO | 0.17 |  | 0.41 | 0.57 | 0.45 | 0.53 | 0.45 | 0.53 | 0.49 |  | 3.17 | 3.17 | 3.06 | 2.92 |
| Na2O | 4.45 |  | 4.01 | 3.86 | 4.10 | 3.68 | 3.69 | 3.41 | 3.70 |  | 9.07 | 8.60 | 1.38 | 1.59 |
| K2O | 5.21 |  | 4.45 | 4.93 | 4.46 | 4.51 | 4.37 | 4.32 | 4.49 |  | 1.38 | 1.22 | 9.25 | 8.62 |
| P2O5 | 0.01 |  | 0.04 | 0.46 | 0.03 | <0.01 | 0.05 | 0.03 | 0.00 |  | 0.00 | 0.01 |  | <0.01 |
| Total | 97.83 |  | 99.86 | 99.98 | 99.86 | 98.95 | 99.89 | 97.39 | 96.63 |  | 99.86 | 99.57 | 101.20 | 98.88 |
| Trace elements | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | XRF | ICP-MS | Least-square-fitted line regressed equation |
| Rb | 412 | 459 | 201 | 174.5 | 211 | 188.5 | 198 | 182 | 261 | 297 |  | 5.6 | 12 | 12.5 | Rb: y = 1.1696x - 33.077; R2 = 0.9504 |
| Sr | 3 | 2.7 | 28 | 27 | 27 | 26.6 | 28 | 27.1 | 8 | 9.8 | 181 | 186 | 60 | 72.8 | Sr: y = 1.0242x + 0.5204; R2 = 0.997 |
| Ba | 17 | 16.5 | 120 | 108 | 107 | 107 | 126 | 129 | 36 | 48 | 197 | 199 | 34 | 35.2 | Ba: y = 1.0246x + 0.3754; R2 = 0.9943 |
| Y | 29.1 | 21 | 59 | 49 | 63 | 50.5 | 56 | 46 | 61.2 | 68.5 | 0.6 | 0.5 | 4 | 1.6 | Y : y = 0.9212x - 0.8934; R2 = 0.9169 |
| Zr | 156 | 159 | 105 | 102 | 103 | 105 | 100 | 109 | 91 | 93.5 | 5 | 6.5 | 8 | 16.4 | Zr: y = 0.9571x + 7.4642; R2 = 0.9842 |
| Nb | 65 | 51 | 98 | 55 | 101 | 57 | 90 | 56 | 105 | 74 | 4 | <1 | 1 | <1 | Nb: y = 0.5687x + 4.055; R2 = 0.7961 |
| Th | 39 | 33 | 28 | 31 | 31 | 32 | 28 | 29 | 40 | 32 | 1 | <1 | 1 | <1 | Th: y = 0.8549x + 2.6473; R2 = 0.9073 |
| La |  |  | 33 | 37.5 | 33 | 41 | 33 | 36 |  |  |  | 12.5 |  | 9.0 | La: y = 0.8304x + 9.2849; R2 = 0.9801 |
| Ce |  |  | 70 | 76 | 76 | 80.5 | 68 | 73 |  |  |  | 13.5 |  | 9.0 | Ce: y = 0.8416x + 13.832; R2 = 0.99 |
| Nd |  |  | 31 | 28 | 35 | 30 | 31 | 26.5 |  |  |  | 2.5 |  | 2.5 | Nd: y = 0.9013x - 1.2054; R2 = 0.9672 |