Appendix 2. Reflectance values for makarochkinite, sample 400Shch-6

|  (nm) | Rmin (%) | Rmax (%) |
| --- | --- | --- |
| 400 | 9.08 | 9.91 |
| 410 | 9.02 | 9.77 |
| 420 | 8.99 | 9.74 |
| 430 | 8.97 | 9.67 |
| 440 | 8.94 | 9.62 |
| 450 | 8.92 | 9.59 |
| 460 | 8.91 | 9.53 |
| 470 | 8.88 | 9.51 |
| 480 | 8.83 | 9.46 |
| 490 | 8.84 | 9.45 |
| 500 | 8.84 | 9.41 |
| 510 | 8.82 | 9.40 |
| 520 | 8.80 | 9.38 |
| 530 | 8.80 | 9.37 |
| 540 | 8.79 | 9.33 |
| 546 | 8.78 | 9.30 |
| 550 | 8.77 | 9.28 |
| 560 | 8.74 | 9.24 |
| 570 | 8.71 | 9.19 |
| 580 | 8.69 | 9.14 |
| 589 | 8.68 | 9.11 |
| 590 | 8.68 | 9.11 |
| 600 | 8.68 | 9.05 |
| 610 | 8.64 | 9.02 |
| 620 | 8.63 | 8.96 |
| 630 | 8.58 | 8.86 |
| 640 | 8.52 | 8.79 |
| 650 | 8.48 | 8.71 |
| 660 | 8.43 | 8.63 |
| 670 | 8.40 | 8.56 |
| 680 | 8.38 | 8.53 |
| 690 | 8.36 | 8.52 |
| 700 | 8.33 | 8.47 |
| Note: Obtained in plane-polarized light in air at a spectral resolution of 10 nm with a Zeiss MPM800 microspectrophotometer equipped with a Zeiss 10 Ultrafluar objective. A 100 W halogen lamp was used as light source and silicon carbide (SiC) served as standard. Accuracy is 0.2% |  |  |

Appendix 3. Powder X-ray diffraction data for makarochkinite

| Index |  |  | #3319* |  |  |  |  | Polyakov et al. (1986)§ |  |  | #400/12† |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| h | k | l |  | dcalc (Å)§ | dobs (Å) | Iobs |  | dobs (Å) | Iobs |  | dobs (Å) | Iobs |
| 0 | 0 | 1 |  | 8.032 |  |  |  |  |  |  |  |  |
| 0 | 1 | 0 |  | 8.030 |  |  |  |  |  |  |  |  |
| 1 | 0 | 0 |  | 7.992 | 7.997 | 57 |  | 7.97 | 40 |  | 7.99 | 57 |
| 0 | -1 | 1 |  | 7.382 | 7.365 | 6 |  |  |  |  |  |  |
| 1 | -1 | 1 |  | 6.346 | 6.329 | 6 |  |  |  |  |  |  |
| 0 | 1 | 1 |  | 4.785 | 4.779 | 29 |  | 4.76 | 40 |  | 4.78 | 38 |
| 1 | -2 | 2 |  | 3.761 | 3.762 | 4 |  |  |  |  | 3.77 | 9 |
| 0 | -2 | 2 |  | 3.691 | 3.692 | 6 |  |  |  |  | 3.69 | 10 |
| -2 | 1 | 2 |  | 3.436 |  |  |  |  |  |  |  |  |
| -2 | 3 | 0 |  | 3.435 | 3.434 | 14 |  |  |  |  | 3.42 | 26 |
| 0 | 1 | 2 |  | 3.118 | 3.120 | 32 |  | 3.123 | 100 |  | 3.11 | 53 |
| 0 | 2 | 1 |  | 3.118 |  |  |  |  |  |  |  |  |
| 3 | -2 | 1 |  | 3.059 | 3.060 | 5 |  |  |  |  | 3.05 | 9 |
| -1 | -2 | 2 |  | 3.051 |  |  |  |  |  |  |  |  |
| -2 | -1 | 2 |  | 2.983 | 2.984 | 7 |  |  |  |  | 2.986 | 11 |
| 2 | -3 | 2 |  | 2.983 |  |  |  |  |  |  |  |  |
| 1 | 2 | 0 |  | 2.925 |  |  |  |  |  |  |  |  |
| 0 | -1 | 3 |  | 2.923 | 2.924 | 69 |  | 2.918 | 70 |  | 2.925 | 90 |
| 0 | -3 | 1 |  | 2.922 |  |  |  |  |  |  |  |  |
| -3 | 3 | 1 |  | 2.811 | 2.810 | 6 |  |  |  |  | 2.805 | 8 |
| -1 | 2 | 2 |  | 2.769 | 2.770 | 10 |  |  |  |  |  |  |
| 3 | -1 | 1 |  | 2.755 | 2.756 | 18 |  |  |  |  | 2.753 | 36 |
| -3 | 2 | 2 |  | 2.714 | 2.714 | 10 |  |  |  |  | 2.711 | 12 |
| 0 | 0 | 3 |  | 2.677 |  |  |  |  |  |  |  |  |
| 0 | 3 | 0 |  | 2.677 |  |  |  |  |  |  |  |  |
| -1 | 3 | 1 |  | 2.677 |  |  |  |  |  |  |  |  |
| -2 | 0 | 3 |  | 2.675 | 2.676 | 77 |  | 2.675 | 80 |  | 2.673 | 100 |
| 2 | -4 | 1 |  | 2.674 |  |  |  |  |  |  |  |  |
| -3 | 0 | 2 |  | 2.668 |  |  |  |  |  |  |  |  |
| 3 | 0 | 0 |  | 2.664 | 2.666 | 18 |  |  |  |  |  |  |
| -2 | 1 | 3 |  | 2.548 | 2.547 | 13 |  |  |  |  |  |  |
| -3 | 4 | 0 |  | 2.547 |  |  |  |  |  |  |  |  |
| -2 | 4 | 0 |  | 2.547 |  |  |  |  |  |  |  |  |
| -4 | 2 | 0 |  | 2.532 |  |  |  |  |  |  |  |  |
| -2 | -1 | 3 |  | 2.528 | 2.530 | 100 |  | 2.529§§ | 60 |  | 2.525 | 95 |
| 2 | -4 | 2 |  | 2.528 |  |  |  |  |  |  |  |  |
| -1 | 1 | 3 |  | 2.517 | 2.517 | 6 |  |  |  |  |  |  |
| 3 | -2 | 2 |  | 2.506 | 2.507 | 6 |  |  |  |  |  |  |
| 2 | 0 | 2 |  | 2.453 | 2.453 | 7 |  |  |  |  | 2.450 | 15 |
| 2 | 1 | 1 |  | 2.452 |  |  |  |  |  |  |  |  |
| 2 | -2 | 3 |  | 2.409 | 2.410 | 28 |  |  |  |  | 2.410 | 33 |
| -2 | -2 | 1 |  | 2.409 |  |  |  |  |  |  |  |  |
| 0 | 2 | 2 |  | 2.393 | 2.393 | 5 |  |  |  |  |  |  |
| -4 | 2 | 2 |  | 2.323 | 2.323 | 5 |  |  |  |  |  |  |
| -4 | 4 | 0 |  | 2.322 |  |  |  |  |  |  |  |  |
| -1 | 4 | 0 |  | 2.322 |  |  |  |  |  |  |  |  |
| 3 | 0 | 1 |  | 2.309 |  |  |  |  |  |  |  |  |
| -4 | 1 | 0 |  | 2.308 | 2.308 | 12 |  |  |  |  | 2.309 | 15 |
| 4 | -2 | 1 |  | 2.308 |  |  |  |  |  |  |  |  |
| -1 | -3 | 3 |  | 2.191 | 2.191 | 6 |  |  |  |  |  |  |
| -4 | 0 | 2 |  | 2.088 |  |  |  |  |  |  |  |  |
| 4 | -4 | 2 |  | 2.088 | 2.088 | 10 |  | 2.096 | 90 |  | 2.098 | 98 |
| 4 | -1 | 1 |  | 2.075 | 2.075 | 39 |  | 2.079 | 60 |  | 2.077 | 67 |
|  |  |  |  |  |  |  |  |  |  |  | 1.982 | 41 |
|  |  |  |  |  |  |  |  |  |  |  | 1.937 | 18 |
|  |  |  |  |  |  |  |  | 1.464 | 70 |  |  |  |
| Note: *The pattern of sample #3319 was recorded with a Guinier-Hägg camera (Si internal standard, CuK1). The observed intensities were obtained by scanning the film. A total of 29 lines were observed up to 2 = 44 (strong fluorescence due to the high Fe content resulted in a high background that masked the weaker lines). The observed reflections give: a = 10.332(4), b = 10.720(5), and c = 8.851(5) Å,  = 105.71(4),  = 96.25(5),  = 124.86(4), V = 730.0(4) Å3. §The indices assigned to some lines by Polyakov et al. (1986) differed from the indices given here. §§This line could also be read as “2.629” in Polyakov et al. (1986, p. 109), but this ambiguity results from the poor printing quality of the original publication. †The pattern of sample #400/12 was obtained with a Dron-2.0 diffractometer using FeK radiation at 2°/min speed. Values of the intensities (Iobs) were calculated from the relative areas of the reflections taking the most intense reflection as 100%. Twenty-one reflections were observed in the interval up to 2 = 67°. |  |  |  |  |  |  |  |  |  |  |  |  |