Table 4. T-O-T angles, in UNIT I e II,  calculated from the instantaneous atomic positions along the MD trajectory for the two extreme cell volumes, corresponding to Pamb and 8.8 GPa. The σ’s reported in this Table are not standard errors, but represent a measure of the finite temperature fluctuations of the T-O-T angles along the trajectory, determined by the thermal motion of the atoms.

|  | TOT, σ (º) |  |  | TOT, σ (º) |  |
| --- | --- | --- | --- | --- | --- |
|  | Pamb | 8.8 GPa |  | Pamb | 8.8 GPa |
| Si1I O4I Si2I | 139.6 (6.1) | 129.5 (5.4) | Si1I O1I Al1I | 131.1 (5.1) | 120.8 (4.2) |
| Si1II O4II Si2II | 140.9 (7.0) | 134.7 (4.9) | Si1II O1II Al1II | 127.2 (4.4) | 120.2 (4.2) |
| Si1I O5I Si3I | 138.9 (6.4) | 129.1 (4.7) | Si2I O2I Al1I | 142.2 (6.0) | 123.9 (4.2) |
| Si1IIO5II Si3II | 137.3 (6.3) | 130.1 (4.2) | Si2II O2II Al1II | 142.0 (5.4) | 125.2 (4.2) |
| Si2II O6I Si3I | 124.8 (4.2) | 117.9 (3.7) | Si3I O3I Al1II | 158.7 (6.9) | 152.9 (5.9) |
| Si2I O6II Si3II | 127.3 (4.8) | 120.2 (4.0) | Si3II O3II Al1I | 152.2 (7.2) | 150.5 (6.4) |
| Si1I O8I Si5I | 164.1 (6.9) | 153.6 (9.1) | Si2I O7I Al1II | 127.6 (5.0) | 121.3 (3.9) |
| Si1II O8II Si5II | 165.0 (6.8) | 133.9 (4.7) | Si2II O7II Al1I | 127.4 (5.2) | 122.2 (3.7) |
| Si4II O10I Si5I | 131.7 (5.1) | 120.8 (4.7) | Si3I O9I Al2I | 158.6 (6.3) | 145.3 (7.9) |
| Si4I O10II Si5II | 126.1 (4.0) | 120.3 (3.9) | Si3II O9II Al2II | 165.6 (6.2) | 132.6 (5.6) |
| Si4I O11I Si6I | 143.2 (5.4) | 121.8 (3.8) | Si4I O12I Al2I | 141.0 (5.4) | 145.0 (4.5) |
| Si4II O11II Si6II | 144.4 (6.1) | 125.6 (3.8) | Si4II O12II Al2II | 135.4 (5.6) | 143.0 (5.5) |
| Si5I O13I Si6II | 134.4 (6.2) | 130.8 (4.9) | Si5I O14I Al2I | 139.3 (7.0) | 140.7 (8.4) |
| Si5II O13II Si6I | 135.8 (4.7) | 133.2 (4.6) | Si5II O14II Al2II | 135.8 (6.1) | 156.6 (7.0) |
| Si4I O16I Si6II | 140.4 (6.1) | 119.1 (3.9) | Si6I O15I Al2I | 131.7 (5.1) | 119.5 (4.6) |
| Si4II O16II Si6I | 139.2 (5.6) | 121.7(4.3) | Si6II O15II Al2II | 134.5 (5.7) | 125.1 (6.8) |
| <Si-O-Si> | 139.6 (12.5) | 127.6 (9.9) | <Si-O-Al> | 140.6 (13.1) | 134.0 (14.0) |