- Appendix A. Densities calculated for each single buoyancy measurements resulting from three separate immersions for each bob (large and small bob). These single density values have been computed in order to determine a mean density and a standard deviation for each melt and each temperature that are reported in Table 2.

| Samples | T (K) | # 1 | # 2 | # 3 | # 4 | # 5 | # 6 | # 7 | # 8 | # 9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NS-5Ce | 1552 | 2.325 | 2.320 | 2.319 | 2.315 | 2.310 | 2.309 | 2.314 | 2.309 | 2.308 |
|  | 1502 | 2.336 | 2.334 | 2.334 | 2.324 | 2.322 | 2.322 | 2.325 | 2.323 | 2.323 |
|  | 1455 | 2.348 | 2.343 | 2.345 | 2.335 | 2.330 | 2.332 | 2.338 | 2.333 | 2.336 |
|  | 1406 | 2.358 | 2.353 | 2.351 | 2.345 | 2.340 | 2.338 | 2.348 | 2.343 | 2.341 |
| NS-10Ce | 1553 | 2.399 | 2.395 | 2.385 | 2.405 | 2.401 | 2.392 | 2.412 | 2.408 | 2.399 |
|  | 1505 | 2.414 | 2.408 | 2.404 | 2.424 | 2.418 | 2.414 | 2.422 | 2.417 | 2.412 |
|  | 1456 | 2.424 | 2.420 | 2.415 | 2.435 | 2.430 | 2.425 | 2.433 | 2.428 | 2.424 |
|  | 1409 | 2.434 | 2.429 | 2.422 | 2.446 | 2.442 | 2.435 | 2.445 | 2.440 | 2.433 |
| NS-5Pr | 1556 | 2.330 | 2.329 | 2.329 | 2.324 | 2.323 | 2.323 | 2.325 | 2.324 | 2.324 |
|  | 1507 | 2.343 | 2.339 | 2.342 | 2.336 | 2.332 | 2.335 | 2.338 | 2.334 | 2.336 |
|  | 1459 | 2.352 | 2.347 | 2.351 | 2.348 | 2.343 | 2.347 | 2.351 | 2.346 | 2.350 |
|  | 1411 | 2.361 | 2.355 | 2.360 | 2.356 | 2.350 | 2.355 | 2.361 | 2.355 | 2.360 |
| NS-25Pr | 1553 | 2.675 | 2.662 | 2.667 | 2.681 | 2.669 | 2.674 | 2.677 | 2.665 | 2.669 |
|  | 1503 | 2.688 | 2.678 | 2.676 | 2.696 | 2.685 | 2.683 | 2.695 | 2.685 | 2.683 |
|  | 1466 | 2.699 | 2.693 | 2.687 | 2.706 | 2.700 | 2.694 | 2.703 | 2.697 | 2.692 |
|  | 1431 | 2.706 | 2.698 | 2.708 | 2.706 | 2.698 | 2.698 | 2.706 | 2.697 | 2.697 |
|  | 1407 | 2.716 | 2.708 | 2.700 | 2.721 | 2.712 | 2.704 | 2.719 | 2.711 | 2.703 |
| NS-5Nd | 1551 | 2.317 | 2.317 | 2.314 | 2.322 | 2.321 | 2.319 | 2.312 | 2.312 | 2.309 |
|  | 1503 | 2.332 | 2.336 | 2.331 | 2.343 | 2.347 | 2.342 | 2.326 | 2.330 | 2.325 |
|  | 1454 | 2.346 | 2.346 | 2.344 | 2.358 | 2.359 | 2.357 | 2.336 | 2.337 | 2.334 |
|  | 1407 | 2.355 | 2.355 | 2.351 | 2.367 | 2.367 | 2.363 | 2.348 | 2.348 | 2.344 |
| NS-25Nd | 1565 | 2.710 | 2.712 | 2.718 | 2.711 | 2.713 | 2.720 | 2.716 | 2.718 | 2.725 |
|  | 1515 | 2.723 | 2.724 | 2.731 | 2.724 | 2.725 | 2.732 | 2.729 | 2.729 | 2.737 |
|  | 1472 | 2.734 | 2.743 | 2.746 | 2.734 | 2.744 | 2.747 | 2.740 | 2.749 | 2.752 |
|  | 1417 | 2.751 | 2.759 | 2.762 | 2.751 | 2.759 | 2.762 | 2.754 | 2.762 | 2.765 |
|  | 1368 | 2.756 | 2.770 | 2.769 | 2.763 | 2.777 | 2.776 | 2.768 | 2.782 | 2.781 |
|  | 1345 | 2.767 | 2.769 | 2.775 | 2.768 | 2.770 | 2.776 | 2.778 | 2.781 | 2.786 |
| NS-5Sm | 1551 | 2.328 | 2.319 | 2.323 | 2.324 | 2.315 | 2.319 | 2.334 | 2.324 | 2.329 |
|  | 1503 | 2.337 | 2.328 | 2.331 | 2.333 | 2.323 | 2.327 | 2.341 | 2.331 | 2.334 |
|  | 1454 | 2.345 | 2.336 | 2.341 | 2.340 | 2.331 | 2.336 | 2.348 | 2.339 | 2.344 |
|  | 1406 | 2.355 | 2.345 | 2.351 | 2.349 | 2.339 | 2.345 | 2.357 | 2.347 | 2.353 |
| NS-25Sm | 1558 | 2.733 | 2.726 | 2.727 | 2.748 | 2.741 | 2.741 | 2.741 | 2.734 | 2.734 |
|  | 1509 | 2.749 | 2.737 | 2.742 | 2.766 | 2.754 | 2.759 | 2.753 | 2.742 | 2.747 |
|  | 1467 | 2.763 | 2.751 | 2.757 | 2.779 | 2.767 | 2.774 | 2.767 | 2.755 | 2.762 |
|  | 1412 | 2.774 | 2.761 | 2.769 | 2.794 | 2.780 | 2.788 | 2.782 | 2.768 | 2.776 |
|  | 1364 | 2.785 | 2.776 | 2.781 | 2.802 | 2.794 | 2.798 | 2.792 | 2.784 | 2.788 |
| NS-5Eu | 1556 | 2.325 | 2.326 | 2.320 | 2.328 | 2.329 | 2.323 | 2.332 | 2.332 | 2.327 |
|  | 1507 | 2.336 | 2.333 | 2.334 | 2.336 | 2.334 | 2.335 | 2.342 | 2.340 | 2.341 |
|  | 1468 | 2.352 | 2.352 | 2.349 | 2.349 | 2.349 | 2.346 | 2.351 | 2.351 | 2.348 |
|  | 1411 | 2.365 | 2.367 | 2.363 | 2.360 | 2.361 | 2.357 | 2.358 | 2.360 | 2.356 |
| NS-25Eu | 1556 | 2.734 | 2.739 | 2.742 | 2.732 | 2.737 | 2.740 | 2.738 | 2.743 | 2.745 |
|  | 1507 | 2.747 | 2.752 | 2.751 | 2.748 | 2.753 | 2.751 | 2.744 | 2.748 | 2.747 |
|  | 1469 | 2.754 | 2.761 | 2.759 | 2.754 | 2.761 | 2.759 | 2.752 | 2.759 | 2.757 |
|  | 1437 | 2.763 | 2.770 | 2.769 | 2.758 | 2.765 | 2.764 | 2.762 | 2.769 | 2.768 |
| NS-5Gd | 1556 | 2.325 | 2.321 | 2.324 | 2.330 | 2.326 | 2.328 | 2.318 | 2.315 | 2.317 |
|  | 1506 | 2.333 | 2.330 | 2.333 | 2.340 | 2.337 | 2.340 | 2.324 | 2.321 | 2.324 |
|  | 1469 | 2.343 | 2.339 | 2.341 | 2.352 | 2.348 | 2.349 | 2.334 | 2.330 | 2.331 |
|  | 1410 | 2.355 | 2.353 | 2.350 | 2.362 | 2.361 | 2.358 | 2.343 | 2.342 | 2.339 |
| NS-25Gd | 1555 | 2.754 | 2.756 | 2.752 | 2.747 | 2.749 | 2.744 | 2.768 | 2.770 | 2.765 |
|  | 1507 | 2.771 | 2.766 | 2.768 | 2.767 | 2.762 | 2.764 | 2.783 | 2.778 | 2.779 |
|  | 1468 | 2.785 | 2.781 | 2.781 | 2.786 | 2.782 | 2.782 | 2.797 | 2.794 | 2.794 |
|  | 1411 | 2.802 | 2.795 | 2.795 | 2.804 | 2.796 | 2.797 | 2.814 | 2.807 | 2.807 |
|  | 1388 | 2.805 | 2.801 | 2.805 | 2.805 | 2.801 | 2.805 | 2.814 | 2.810 | 2.814 |
| NS-5Tb | 1551 | 2.316 | 2.323 | 2.326 | 2.318 | 2.325 | 2.328 | 2.313 | 2.320 | 2.323 |
|  | 1503 | 2.319 | 2.324 | 2.328 | 2.330 | 2.335 | 2.339 | 2.321 | 2.326 | 2.330 |
|  | 1453 | 2.328 | 2.334 | 2.336 | 2.342 | 2.348 | 2.350 | 2.332 | 2.338 | 2.340 |
|  | 1407 | 2.343 | 2.350 | 2.350 | 2.349 | 2.357 | 2.356 | 2.338 | 2.346 | 2.345 |
| NS-25Tb | 1553 | 2.791 | 2.780 | 2.786 | 2.792 | 2.780 | 2.787 | 2.792 | 2.780 | 2.786 |
|  | 1506 | 2.794 | 2.797 | 2.799 | 2.793 | 2.796 | 2.798 | 2.794 | 2.798 | 2.799 |
|  | 1467 | 2.801 | 2.804 | 2.809 | 2.797 | 2.800 | 2.805 | 2.798 | 2.801 | 2.806 |
| NS-5Dy | 1552 | 2.328 | 2.328 | 2.326 | 2.326 | 2.326 | 2.325 | 2.333 | 2.333 | 2.332 |
|  | 1503 | 2.339 | 2.342 | 2.342 | 2.337 | 2.340 | 2.340 | 2.344 | 2.346 | 2.347 |
|  | 1454 | 2.349 | 2.351 | 2.354 | 2.348 | 2.350 | 2.353 | 2.354 | 2.356 | 2.359 |
|  | 1407 | 2.358 | 2.363 | 2.363 | 2.358 | 2.363 | 2.363 | 2.366 | 2.371 | 2.371 |
| NS25Dy | 1555 | 2.764 | 2.757 | 2.764 | 2.766 | 2.759 | 2.766 | 2.780 | 2.773 | 2.780 |
|  | 1507 | 2.781 | 2.777 | 2.784 | 2.783 | 2.779 | 2.786 | 2.789 | 2.785 | 2.792 |
|  | 1467 | 2.795 | 2.789 | 2.796 | 2.794 | 2.788 | 2.795 | 2.804 | 2.799 | 2.805 |
|  | 1410 | 2.803 | 2.801 | 2.804 | 2.803 | 2.801 | 2.804 | 2.815 | 2.812 | 2.816 |
|  | 1386 | 2.804 | 2.802 | 2.806 | 2.805 | 2.803 | 2.806 | 2.818 | 2.815 | 2.819 |
| NS-5Ho | 1551 | 2.347 | 2.337 | 2.337 | 2.336 | 2.327 | 2.326 | 2.342 | 2.333 | 2.332 |
|  | 1502 | 2.352 | 2.349 | 2.347 | 2.343 | 2.340 | 2.338 | 2.348 | 2.345 | 2.343 |
|  | 1454 | 2.362 | 2.358 | 2.357 | 2.353 | 2.348 | 2.348 | 2.359 | 2.354 | 2.353 |
|  | 1406 | 2.371 | 2.368 | 2.367 | 2.364 | 2.360 | 2.359 | 2.369 | 2.365 | 2.364 |
| NS-25Ho | 1552 | 2.776 | 2.785 | 2.780 | 2.781 | 2.790 | 2.786 | 2.785 | 2.794 | 2.789 |
|  | 1502 | 2.802 | 2.796 | 2.794 | 2.809 | 2.803 | 2.801 | 2.810 | 2.804 | 2.802 |
|  | 1456 | 2.801 | 2.807 | 2.806 | 2.813 | 2.818 | 2.817 | 2.813 | 2.818 | 2.817 |
|  | 1438 | 2.808 | 2.814 | 2.814 | 2.815 | 2.821 | 2.820 | 2.817 | 2.823 | 2.822 |
|  | 1416 | 2.811 | 2.814 | 2.817 | 2.819 | 2.822 | 2.826 | 2.820 | 2.823 | 2.826 |
| NS-5Er | 1551 | 2.335 | 2.331 | 2.332 | 2.337 | 2.333 | 2.334 | 2.343 | 2.339 | 2.340 |
|  | 1503 | 2.344 | 2.345 | 2.347 | 2.343 | 2.344 | 2.346 | 2.348 | 2.348 | 2.351 |
|  | 1458 | 2.348 | 2.350 | 2.352 | 2.352 | 2.354 | 2.356 | 2.355 | 2.357 | 2.359 |
|  | 1435 | 2.354 | 2.354 | 2.354 | 2.357 | 2.358 | 2.358 | 2.361 | 2.361 | 2.361 |
|  | 1411 | 2.355 | 2.357 | 2.357 | 2.360 | 2.362 | 2.362 | 2.363 | 2.365 | 2.365 |
| NS-25Er | 1552 | 2.790 | 2.791 | 2.788 | 2.786 | 2.786 | 2.784 | 2.789 | 2.790 | 2.787 |
|  | 1502 | 2.808 | 2.807 | 2.805 | 2.804 | 2.803 | 2.801 | 2.806 | 2.805 | 2.803 |
|  | 1456 | 2.820 | 2.819 | 2.814 | 2.819 | 2.818 | 2.812 | 2.817 | 2.816 | 2.811 |
|  | 1438 | 2.824 | 2.821 | 2.819 | 2.822 | 2.818 | 2.817 | 2.824 | 2.820 | 2.818 |
|  | 1416 | 2.835 | 2.831 | 2.825 | 2.830 | 2.826 | 2.819 | 2.831 | 2.826 | 2.820 |
| NS-5Tm | 1541 | 2.331 | 2.325 | 2.328 | 2.335 | 2.33 | 2.336 | 2.333 | 2.328 | 2.334 |
|  | 1495 | 2.340 | 2.343 | 2.344 | 2.343 | 2.346 | 2.346 | 2.341 | 2.343 | 2.344 |
|  | 1449 | 2.345 | 2.350 | 2.350 | 2.349 | 2.355 | 2.354 | 2.349 | 2.355 | 2.354 |
|  | 1426 | 2.354 | 2.352 | 2.350 | 2.359 | 2.357 | 2.355 | 2.359 | 2.357 | 2.355 |
| NS-25Tm | 1555 | 2.808 | 2.802 | 2.794 | 2.815 | 2.810 | 2.801 | 2.825 | 2.819 | 2.811 |
|  | 1507 | 2.812 | 2.810 | 2.798 | 2.825 | 2.823 | 2.812 | 2.828 | 2.826 | 2.814 |
|  | 1482 | 2.823 | 2.814 | 2.809 | 2.834 | 2.826 | 2.820 | 2.835 | 2.826 | 2.821 |
|  | 1468 | 2.822 | 2.817 | 2.810 | 2.835 | 2.829 | 2.823 | 2.837 | 2.831 | 2.824 |
| NS-5Yb | 1544 | 2.330 | 2.335 | 2.333 | 2.336 | 2.341 | 2.339 | 2.335 | 2.340 | 2.338 |
|  | 1497 | 2.342 | 2.346 | 2.345 | 2.348 | 2.351 | 2.350 | 2.345 | 2.348 | 2.347 |
|  | 1450 | 2.353 | 2.357 | 2.354 | 2.356 | 2.360 | 2.357 | 2.354 | 2.358 | 2.355 |
|  | 1426 | 2.354 | 2.358 | 2.357 | 2.362 | 2.365 | 2.364 | 2.357 | 2.360 | 2.359 |
| NS-25Yb | 1552 | 2.802 | 2.784 | 2.790 | 2.815 | 2.796 | 2.803 | 2.814 | 2.796 | 2.802 |
|  | 1504 | 2.799 | 2.798 | 2.808 | 2.806 | 2.805 | 2.815 | 2.809 | 2.808 | 2.818 |
|  | 1465 | 2.808 | 2.807 | 2.815 | 2.815 | 2.814 | 2.821 | 2.830 | 2.828 | 2.836 |
|  | 1432 | 2.817 | 2.816 | 2.814 | 2.817 | 2.816 | 2.814 | 2.839 | 2.838 | 2.836 |

Appendix B. Data relevant to the present melts used for the separate linear regressions along the various Na-disilicate - lanthanide sesquioxides binary joins that allow to obtain the partial molar volumes of the lanthanide sesquioxides given in Tables 4 and 5.

| Samples | T (K) | V (cm3/mol) | SiO2# | LanthOx#* | Na2O# |
| --- | --- | --- | --- | --- | --- |
| NS2 | 1300 | 26.306 | 0.6843 | 0.0000 | 0.3157 |
| NS2 | 1350 | 26.437 | 0.6843 | 0.0000 | 0.3157 |
| NS2 | 1400 | 26.569 | 0.6843 | 0.0000 | 0.3157 |
| NS2 | 1450 | 26.702 | 0.6843 | 0.0000 | 0.3157 |
| NS2 | 1500 | 26.837 | 0.6843 | 0.0000 | 0.3157 |
| NS2 | 1550 | 26.973 | 0.6843 | 0.0000 | 0.3157 |
| NS2 | 1600 | 27.111 | 0.6843 | 0.0000 | 0.3157 |
| NS-5Ce | 1300 | 26.704 | 0.6624 | 0.0097 | 0.3279 |
| NS-5Ce | 1350 | 26.829 | 0.6624 | 0.0097 | 0.3279 |
| NS-5Ce | 1400 | 26.955 | 0.6624 | 0.0097 | 0.3279 |
| NS-5Ce | 1450 | 27.082 | 0.6624 | 0.0097 | 0.3279 |
| NS-5Ce | 1500 | 27.211 | 0.6624 | 0.0097 | 0.3279 |
| NS-5Ce | 1550 | 27.340 | 0.6624 | 0.0097 | 0.3279 |
| NS-5Ce | 1600 | 27.471 | 0.6624 | 0.0097 | 0.3279 |
| NS-10Ce | 1300 | 26.900 | 0.6539 | 0.0208 | 0.3253 |
| NS-10Ce | 1350 | 27.035 | 0.6539 | 0.0208 | 0.3253 |
| NS-10Ce | 1400 | 27.172 | 0.6539 | 0.0208 | 0.3253 |
| NS-10Ce | 1450 | 27.311 | 0.6539 | 0.0208 | 0.3253 |
| NS-10Ce | 1500 | 27.451 | 0.6539 | 0.0208 | 0.3253 |
| NS-10Ce | 1550 | 27.592 | 0.6539 | 0.0208 | 0.3253 |
| NS-10Ce | 1600 | 27.735 | 0.6539 | 0.0208 | 0.3253 |
| NS-5Pr | 1300 | 26.764 | 0.6646 | 0.0113 | 0.3241 |
| NS-5Pr | 1350 | 26.886 | 0.6646 | 0.0113 | 0.3241 |
| NS-5Pr | 1400 | 27.008 | 0.6646 | 0.0113 | 0.3241 |
| NS-5Pr | 1450 | 27.132 | 0.6646 | 0.0113 | 0.3241 |
| NS-5Pr | 1500 | 27.257 | 0.6646 | 0.0113 | 0.3241 |
| NS-5Pr | 1550 | 27.383 | 0.6646 | 0.0113 | 0.3241 |
| NS-5Pr | 1600 | 27.511 | 0.6646 | 0.0113 | 0.3241 |
| NS-25Pr | 1300 | 28.168 | 0.6245 | 0.0609 | 0.3145 |
| NS-25Pr | 1350 | 28.302 | 0.6245 | 0.0609 | 0.3145 |
| NS-25Pr | 1400 | 28.438 | 0.6245 | 0.0609 | 0.3145 |
| NS-25Pr | 1450 | 28.574 | 0.6245 | 0.0609 | 0.3145 |
| NS-25Pr | 1500 | 28.713 | 0.6245 | 0.0609 | 0.3145 |
| NS-25Pr | 1550 | 28.852 | 0.6245 | 0.0609 | 0.3145 |
| NS-25Pr | 1600 | 28.993 | 0.6245 | 0.0609 | 0.3145 |
| NS-5Nd | 1300 | 26.547 | 0.6599 | 0.0095 | 0.3306 |
| NS-5Nd | 1350 | 26.696 | 0.6599 | 0.0095 | 0.3306 |
| NS-5Nd | 1400 | 26.847 | 0.6599 | 0.0095 | 0.3306 |
| NS-5Nd | 1450 | 26.999 | 0.6599 | 0.0095 | 0.3306 |
| NS-5Nd | 1500 | 27.153 | 0.6599 | 0.0095 | 0.3306 |
| NS-5Nd | 1550 | 27.309 | 0.6599 | 0.0095 | 0.3306 |
| NS-5Nd | 1600 | 27.467 | 0.6599 | 0.0095 | 0.3306 |
| NS-25Nd | 1300 | 27.324 | 0.6344 | 0.0562 | 0.3095 |
| NS-25Nd | 1350 | 27.458 | 0.6344 | 0.0562 | 0.3095 |
| NS-25Nd | 1400 | 27.594 | 0.6344 | 0.0562 | 0.3095 |
| NS-25Nd | 1450 | 27.731 | 0.6344 | 0.0562 | 0.3095 |
| NS-25Nd | 1500 | 27.870 | 0.6344 | 0.0562 | 0.3095 |
| NS-25Nd | 1550 | 28.010 | 0.6344 | 0.0562 | 0.3095 |
| NS-25Nd | 1600 | 28.151 | 0.6344 | 0.0562 | 0.3095 |
| NS-5Sm | 1300 | 26.831 | 0.6659 | 0.0097 | 0.3244 |
| NS-5Sm | 1350 | 26.928 | 0.6659 | 0.0097 | 0.3244 |
| NS-5Sm | 1400 | 27.027 | 0.6659 | 0.0097 | 0.3244 |
| NS-5Sm | 1450 | 27.126 | 0.6659 | 0.0097 | 0.3244 |
| NS-5Sm | 1500 | 27.225 | 0.6659 | 0.0097 | 0.3244 |
| NS-5Sm | 1550 | 27.326 | 0.6659 | 0.0097 | 0.3244 |
| NS-5Sm | 1600 | 27.427 | 0.6659 | 0.0097 | 0.3244 |
| NS-25Sm | 1300 | 27.326 | 0.6343 | 0.0556 | 0.3101 |
| NS-25Sm | 1350 | 27.460 | 0.6343 | 0.0556 | 0.3101 |
| NS-25Sm | 1400 | 27.595 | 0.6343 | 0.0556 | 0.3101 |
| NS-25Sm | 1450 | 27.731 | 0.6343 | 0.0556 | 0.3101 |
| NS-25Sm | 1500 | 27.869 | 0.6343 | 0.0556 | 0.3101 |
| NS-25Sm | 1550 | 28.008 | 0.6343 | 0.0556 | 0.3101 |
| NS-25Sm | 1600 | 28.149 | 0.6343 | 0.0556 | 0.3101 |
| NS-5Eu | 1300 | 26.515 | 0.6647 | 0.0090 | 0.3263 |
| NS-5Eu | 1350 | 26.649 | 0.6647 | 0.0090 | 0.3263 |
| NS-5Eu | 1400 | 26.785 | 0.6647 | 0.0090 | 0.3263 |
| NS-5Eu | 1450 | 26.922 | 0.6647 | 0.0090 | 0.3263 |
| NS-5Eu | 1500 | 27.061 | 0.6647 | 0.0090 | 0.3263 |
| NS-5Eu | 1550 | 27.201 | 0.6647 | 0.0090 | 0.3263 |
| NS-5Eu | 1600 | 27.342 | 0.6647 | 0.0090 | 0.3263 |
| NS-25Eu | 1300 | 27.536 | 0.6189 | 0.0556 | 0.3255 |
| NS-25Eu | 1350 | 27.643 | 0.6189 | 0.0556 | 0.3255 |
| NS-25Eu | 1400 | 27.751 | 0.6189 | 0.0556 | 0.3255 |
| NS-25Eu | 1450 | 27.860 | 0.6189 | 0.0556 | 0.3255 |
| NS-25Eu | 1500 | 27.970 | 0.6189 | 0.0556 | 0.3255 |
| NS-25Eu | 1550 | 28.081 | 0.6189 | 0.0556 | 0.3255 |
| NS-25Eu | 1600 | 28.192 | 0.6189 | 0.0556 | 0.3255 |
| NS-5Gd | 1300 | 26.717 | 0.6645 | 0.0090 | 0.3265 |
| NS-5Gd | 1350 | 26.832 | 0.6645 | 0.0090 | 0.3265 |
| NS-5Gd | 1400 | 26.948 | 0.6645 | 0.0090 | 0.3265 |
| NS-5Gd | 1450 | 27.065 | 0.6645 | 0.0090 | 0.3265 |
| NS-5Gd | 1500 | 27.182 | 0.6645 | 0.0090 | 0.3265 |
| NS-5Gd | 1550 | 27.301 | 0.6645 | 0.0090 | 0.3265 |
| NS-5Gd | 1600 | 27.421 | 0.6645 | 0.0090 | 0.3265 |
| NS-25Gd | 1300 | 27.042 | 0.6311 | 0.0529 | 0.3159 |
| NS-25Gd | 1350 | 27.191 | 0.6311 | 0.0529 | 0.3159 |
| NS-25Gd | 1400 | 27.341 | 0.6311 | 0.0529 | 0.3159 |
| NS-25Gd | 1450 | 27.493 | 0.6311 | 0.0529 | 0.3159 |
| NS-25Gd | 1500 | 27.647 | 0.6311 | 0.0529 | 0.3159 |
| NS-25Gd | 1550 | 27.802 | 0.6311 | 0.0529 | 0.3159 |
| NS-25Gd | 1600 | 27.959 | 0.6311 | 0.0529 | 0.3159 |
| NS-5Tb | 1300 | 26.791 | 0.6603 | 0.0089 | 0.3308 |
| NS-5Tb | 1350 | 26.900 | 0.6603 | 0.0089 | 0.3308 |
| NS-5Tb | 1400 | 27.009 | 0.6603 | 0.0089 | 0.3308 |
| NS-5Tb | 1450 | 27.119 | 0.6603 | 0.0089 | 0.3308 |
| NS-5Tb | 1500 | 27.230 | 0.6603 | 0.0089 | 0.3308 |
| NS-5Tb | 1550 | 27.342 | 0.6603 | 0.0089 | 0.3308 |
| NS-5Tb | 1600 | 27.455 | 0.6603 | 0.0089 | 0.3308 |
| NS-25Tb | 1300 | 27.448 | 0.6173 | 0.0561 | 0.3266 |
| NS-25Tb | 1350 | 27.544 | 0.6173 | 0.0561 | 0.3266 |
| NS-25Tb | 1400 | 27.641 | 0.6173 | 0.0561 | 0.3266 |
| NS-25Tb | 1450 | 27.739 | 0.6173 | 0.0561 | 0.3266 |
| NS-25Tb | 1500 | 27.837 | 0.6173 | 0.0561 | 0.3266 |
| NS-25Tb | 1550 | 27.936 | 0.6173 | 0.0561 | 0.3266 |
| NS-25Tb | 1600 | 28.036 | 0.6173 | 0.0561 | 0.3266 |
| NS-5Dy | 1300 | 26.682 | 0.6618 | 0.0099 | 0.3284 |
| NS-5Dy | 1350 | 26.820 | 0.6618 | 0.0099 | 0.3284 |
| NS-5Dy | 1400 | 26.959 | 0.6618 | 0.0099 | 0.3284 |
| NS-5Dy | 1450 | 27.100 | 0.6618 | 0.0099 | 0.3284 |
| NS-5Dy | 1500 | 27.243 | 0.6618 | 0.0099 | 0.3284 |
| NS-5Dy | 1550 | 27.386 | 0.6618 | 0.0099 | 0.3284 |
| NS-5Dy | 1600 | 27.532 | 0.6618 | 0.0099 | 0.3284 |
| NS-25Dy | 1300 | 27.783 | 0.6245 | 0.0576 | 0.3179 |
| NS-25Dy | 1350 | 27.903 | 0.6245 | 0.0576 | 0.3179 |
| NS-25Dy | 1400 | 28.023 | 0.6245 | 0.0576 | 0.3179 |
| NS-25Dy | 1450 | 28.145 | 0.6245 | 0.0576 | 0.3179 |
| NS-25Dy | 1500 | 28.268 | 0.6245 | 0.0576 | 0.3179 |
| NS-25Dy | 1550 | 28.392 | 0.6245 | 0.0576 | 0.3179 |
| NS-25Dy | 1600 | 28.518 | 0.6245 | 0.0576 | 0.3179 |
| NS-5Ho | 1300 | 26.632 | 0.6626 | 0.0090 | 0.3284 |
| NS-5Ho | 1350 | 26.748 | 0.6626 | 0.0090 | 0.3284 |
| NS-5Ho | 1400 | 26.865 | 0.6626 | 0.0090 | 0.3284 |
| NS-5Ho | 1450 | 26.983 | 0.6626 | 0.0090 | 0.3284 |
| NS-5Ho | 1500 | 27.102 | 0.6626 | 0.0090 | 0.3284 |
| NS-5Ho | 1550 | 27.222 | 0.6626 | 0.0090 | 0.3284 |
| NS-5Ho | 1600 | 27.344 | 0.6626 | 0.0090 | 0.3284 |
| NS-25Ho | 1300 | 27.319 | 0.6293 | 0.0542 | 0.3164 |
| NS-25Ho | 1350 | 27.445 | 0.6293 | 0.0542 | 0.3164 |
| NS-25Ho | 1400 | 27.573 | 0.6293 | 0.0542 | 0.3164 |
| NS-25Ho | 1450 | 27.702 | 0.6293 | 0.0542 | 0.3164 |
| NS-25Ho | 1500 | 27.832 | 0.6293 | 0.0542 | 0.3164 |
| NS-25Ho | 1550 | 27.964 | 0.6293 | 0.0542 | 0.3164 |
| NS-25Ho | 1600 | 28.096 | 0.6293 | 0.0542 | 0.3164 |
| NS-5Er | 1300 | 26.616 | 0.6650 | 0.0084 | 0.3267 |
| NS-5Er | 1350 | 26.717 | 0.6650 | 0.0084 | 0.3267 |
| NS-5Er | 1400 | 26.819 | 0.6650 | 0.0084 | 0.3267 |
| NS-5Er | 1450 | 26.921 | 0.6650 | 0.0084 | 0.3267 |
| NS-5Er | 1500 | 27.025 | 0.6650 | 0.0084 | 0.3267 |
| NS-5Er | 1550 | 27.129 | 0.6650 | 0.0084 | 0.3267 |
| NS-5Er | 1600 | 27.234 | 0.6650 | 0.0084 | 0.3267 |
| NS-25Er | 1300 | 26.903 | 0.6321 | 0.0504 | 0.3176 |
| NS-25Er | 1350 | 27.036 | 0.6321 | 0.0504 | 0.3176 |
| NS-25Er | 1400 | 27.171 | 0.6321 | 0.0504 | 0.3176 |
| NS-25Er | 1450 | 27.306 | 0.6321 | 0.0504 | 0.3176 |
| NS-25Er | 1500 | 27.443 | 0.6321 | 0.0504 | 0.3176 |
| NS-25Er | 1550 | 27.582 | 0.6321 | 0.0504 | 0.3176 |
| NS-25Er | 1600 | 27.721 | 0.6321 | 0.0504 | 0.3176 |
| NS-5Tm | 1300 | 26.665 | 0.6638 | 0.0086 | 0.3276 |
| NS-5Tm | 1350 | 26.781 | 0.6638 | 0.0086 | 0.3276 |
| NS-5Tm | 1400 | 26.898 | 0.6638 | 0.0086 | 0.3276 |
| NS-5Tm | 1450 | 27.016 | 0.6638 | 0.0086 | 0.3276 |
| NS-5Tm | 1500 | 27.135 | 0.6638 | 0.0086 | 0.3276 |
| NS-5Tm | 1550 | 27.256 | 0.6638 | 0.0086 | 0.3276 |
| NS-5Tm | 1600 | 27.377 | 0.6638 | 0.0086 | 0.3276 |
| NS-25Tm | 1300 | 27.202 | 0.6208 | 0.0520 | 0.3272 |
| NS-25Tm | 1350 | 27.286 | 0.6208 | 0.0520 | 0.3272 |
| NS-25Tm | 1400 | 27.371 | 0.6208 | 0.0520 | 0.3272 |
| NS-25Tm | 1450 | 27.456 | 0.6208 | 0.0520 | 0.3272 |
| NS-25Tm | 1500 | 27.541 | 0.6208 | 0.0520 | 0.3272 |
| NS-25Tm | 1550 | 27.627 | 0.6208 | 0.0520 | 0.3272 |
| NS-25Tm | 1600 | 27.714 | 0.6208 | 0.0520 | 0.3272 |
| NS-5Yb | 1300 | 26.628 | 0.6673 | 0.0085 | 0.3242 |
| NS-5Yb | 1350 | 26.742 | 0.6673 | 0.0085 | 0.3242 |
| NS-5Yb | 1400 | 26.856 | 0.6673 | 0.0085 | 0.3242 |
| NS-5Yb | 1450 | 26.972 | 0.6673 | 0.0085 | 0.3242 |
| NS-5Yb | 1500 | 27.089 | 0.6673 | 0.0085 | 0.3242 |
| NS-5Yb | 1550 | 27.207 | 0.6673 | 0.0085 | 0.3242 |
| NS-5Yb | 1600 | 27.326 | 0.6673 | 0.0085 | 0.3242 |
| NS-25Yb | 1300 | 27.203 | 0.6374 | 0.0505 | 0.3121 |
| NS-25Yb | 1350 | 27.300 | 0.6374 | 0.0505 | 0.3121 |
| NS-25Yb | 1400 | 27.398 | 0.6374 | 0.0505 | 0.3121 |
| NS-25Yb | 1450 | 27.497 | 0.6374 | 0.0505 | 0.3121 |
| NS-25Yb | 1500 | 27.596 | 0.6374 | 0.0505 | 0.3121 |
| NS-25Yb | 1550 | 27.696 | 0.6374 | 0.0505 | 0.3121 |
| NS-25Yb | 1600 | 27.797 | 0.6374 | 0.0505 | 0.3121 |

#Concentrations are given in mol %.

*LanthOx is Ce2O3, Pr2O3, Nd2O3, Sm2O3, Eu2O3, Gd2O3, Tb2O3, Dy2O3, Ho2O3, Er2O3, Tm2O3 and Yb2O3.