Table 3: Unit-cell volumes, HO= Site A, framework density, water porosity,

and measured enthalpies of hydration of zeolites.

| Zeolite minerals | V u.c. anh. | Vu.c. hydr. | k | HO= | FD anh. | FD hyd. | WP | Al/Si | H hyd-W | Meth. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (Å3) |  |  | Site A |  |  |  |  | kJmol-1 |  |
|  |  | (Å3) |  | kJmol-1 |  |  |  |  | H2O |  |
| Analcime | 157.65 a | 161.45 a | 3.80 | 65.80 | 19.03 | 18.58 | 0.19 | 0.47 | -40.87 1 | HF |
| Clinoptilolite | 1009.99 b | 1044.51 b | 3.16 | -11.46 | 17.82 | 17.23 | 0.31 | 0.24 | -23.42 2 | HF |
| Mordenite | 344.59 c | 346.57 c | 0.57 | -31.40 | 17.41 | 17.31 | 0.30 | 0.19 | -29.74 3 | HF |
| Analcime | 157.65 a | 161.45 a | 3.80 | 66.84 | 18.94 | 18.49 | 0.19 | 0.46 | -41.70 4 | TTDC |
| Brewsterite | 830.79 d | 917.40 d | 8.58 | -29.72 | 19.26 | 17.44 | 0.33 | 0.333 | -35.84 5 | TTDC |
| Chabazite-Ca | 809.00 f | 822.40 f | 1.07 | -75.29 | 14.88 | 14.64 | 0.45 | 0.46 | -30.63 6 | TTDC |
| Chabazite-Ca | 809.00 f | 822.40 f | 1.07 | -81.85 | 14.83 | 14.59 | 0.46 | 0.37 | -33.10 7 | TTDC |
| Clinoptilolite-Na | 1000.00 f | 1070.00 f | 6.80 | 65.80 | 18.00 | 16.82 | 0.29 | 0.22 | -30.23 8 | TTDC |
| Clinoptilolite | 1000.00 f | 1070.00 f | 7.37 | -7.47 | 18.00 | 16.82 | 0.27 | 0.22 | -31.74 8 | TTDC |
| Clinoptilolite-Ca | 1009.99 f | 1044.51 f | 2.97 | -95.80 | 17.82 | 17.23 | 0.33 | 0.22 | -27.23 8 | TTDC |
| Clinoptilolite-K | 1000.00 f | 1070.00 f | 8.98 | 141.00 | 18.00 | 16.82 | 0.22 | 0.22 | -30.90 8 | TTDC |
| Clinopt. -K-Na | 1000.00 f | 1070.00 f | 7.86 | 100.92 | 18.00 | 16.82 | 0.25 | 0.22 | -28.32 8 | TTDC |
| Erionite | 2279.50 f | 2282.00 f | 0.09 | -35.62 | 15.71 | 15.69 | 0.35 | 0.311 | -20.17 9 | TTDC |
| Gmelinite | 1646.62 g | 1666.88 g | 0.83 | 61.67 | 14.53 | 14.35 | 0.44 | 0.527 | -27.50 10 | TTDC |
| Gonnardite | 458.38 h | 577.78 i | 20.59 | -85.88 | 21.82 | 17.31 | 0.31 | 0.67 | -52.63 11 | TTDC |
| Heulandite | 465.98 j | 524.16 j | 9.54 | -58.42 | 19.31 | 17.17 | 0.35 | 0.31 | -34.33 12 | TTDC |
| Laumonite | 331.50 k | 346.50 k | 3.75 | -92.10 | 18.10 | 17.32 | 0.35 | 0.50 | -35.85 13 | TTDC |
| Leonhardite | 331.50 k | 336.50 k | 1.42 | -90.66 | 18.05 | 17.79 | 0.31 | 0.50 | -39.86 13 | TTDC |
| Mesolite | 827.17 l | 853.21 l | 3.33 | -39.47 | 18.13 | 17.58 | 0.28 | 0.67 | -43.81 11 | TTDC |
| Morden.-Epist. | 399.34 m | 453.78 m | 14.14 | -58.51 | 15.02 | 13.22 | 0.25 | 0.33 | -30.31 14 | TTDC |
| Natrolite | 223.13 n | 281.25 n | 28.35 | 65.80 | 22.41 | 17.78 | 0.21 | 0.67 | -57.65 11 | TTDC |
| Tetranatrolite | 223.13 n | 281.25 n | 27.68 | 65.80 | 22.41 | 17.78 | 0.21 | 0.67 | -57.30 11 | TTDC |
| Scolecite | 279.48 l | 286.18 l | 2.33 | -92.10 | 17.82 | 17.47 | 0.31 | 0.67 | -40.53 11 | TTDC |
| Stellerite | 507.40 o | 551.02 o | 6.20 | -92.10 | 17.72 | 16.32 | 0.38 | 0.288 | -30.47 15 | TTDC |
| Stilbite | 512.13 p | 554.82 p | 5.87 | -83.25 | 17.57 | 16.22 | 0.39 | 0.31 | -31.53 12 | TTDC |
| Thomsonite | 548.43 q | 562.63 q | 2.24 | -60.52 | 18.23 | 17.77 | 0.32 | 1.00 | -55.57 11 | TTDC |
| Zeolite Y-Na | 79.31 r | 78.10 r | -0.97 | 55.89 | 12.61 | 12.80 | 0.47 | 0.40 | -16.98 16 | TTDC |
| Zeolite Y-Ca | 79.60 s | 78.49 t | -0.90 | -85.77 | 12.55 | 12.73 | 0.47 | 0.40 | -17.40 16 | TTDC |
| Zeolite Y-Rb | 79.69 s | 78.49 t | -1.18 | 108.69 | 12.54 | 12.73 | 0.39 | 0.40 | -17.48 16 | TTDC |
| Zeolite Y-K | 79.79 s | 78.58 t | -1.10 | 107.76 | 12.55 | 12.74 | 0.42 | 0.40 | -12.51 16 | TTDC |
| Zeolite Y-Cs | 79.69 s | 78.49 t | -1.18 | 131.54 | 12.55 | 12.74 | 0.39 | 0.40 | -15.78 16 | TTDC |
| Zeolite Y-Li | 79.31 s | 78.10 t | -0.96 | -28.49 | 12.62 | 12.82 | 0.48 | 0.41 | -18.43 16 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -75.34 | 15.30 | 15.30 | 0.35 | 0.07 | -11.45 17 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -75.34 | 15.30 | 15.30 | 0.03 | 0.07 | -21.50 17 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | -53.31 | 15.30 | 15.30 | 0.34 | 0.07 | -11.74 17 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | -53.31 | 15.30 | 15.30 | 0.04 | 0.07 | -21.38 17 | TTDC |
| Zeolite BEA-K | 65.36 u | 65.36 v | 0.00 | 19.65 | 15.30 | 15.30 | 0.33 | 0.07 | -6.73 17 | TTDC |
| Zeolite BEA-K | 65.36 u | 65.36 v | 0.00 | 19.65 | 15.30 | 15.30 | 0.02 | 0.07 | -12.75 17 | TTDC |
| Zeolite BEA-Rb | 65.36 u | 65.36 v | 0.00 | 118.63 | 15.30 | 15.30 | 0.32 | 0.07 | -5.29 17 | TTDC |
| Zeolite BEA-Rb | 65.36 u | 65.36 v | 0.00 | 118.63 | 15.30 | 15.30 | 0.02 | 0.07 | -10.00 17 | TTDC |
| Zeolite BEA-Cs | 65.36 u | 65.36 v | 0.00 | 76.56 | 15.30 | 15.30 | 0.31 | 0.07 | -8.03 17 | TTDC |
| Zeolite BEA-Cs | 65.36 u | 65.36 v | 0.00 | 76.56 | 15.30 | 15.30 | 0.03 | 0.07 | -14.83 17 | TTDC |
| Zeolite BEA-K | 65.36 u | 65.36 v | 0.00 | 45.17 | 15.30 | 15.30 | 0.33 | 0.07 | -6.73 17 | TTDC |
| Zeolite BEA-K | 65.36 u | 65.36 v | 0.00 | 45.17 | 15.30 | 15.30 | 0.02 | 0.07 | -12.75 17 | TTDC |
| Zeolite BEA-Rb | 65.36 u | 65.36 v | 0.00 | 143.46 | 15.30 | 15.30 | 0.32 | 0.07 | -5.29 17 | TTDC |
| Zeolite BEA-Rb | 65.36 u | 65.36 v | 0.00 | 143.46 | 15.30 | 15.30 | 0.02 | 0.07 | -10.00 17 | TTDC |

Table  3 (continued)

| Zeolite minerals | V u.c. anh. | Vu.c. hydr. | k | HO= | FD anh. | FD hyd. | WP | Al/Si | H hyd-W | Meth. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (Å3) | (Å3) |  | Site A |  |  |  |  | kJmol-1 |  |
|  |  |  |  | kJmol-1 |  |  |  |  | H2O |  |
| Zeolite BEA-Cs | 65.36 u | 65.36 v | 0.00 | 99.87 | 15.30 | 15.30 | 0.31 | 0.07 | -8.03 17 | TTDC |
| Zeolite BEA-Cs | 65.36 u | 65.36 v | 0.00 | 99.87 | 15.30 | 15.30 | 0.03 | 0.07 | -14.83 17 | TTDC |
| Zeolite BEA-Mg | 65.36 u | 65.36 v | 0.00 | -159.79 | 15.30 | 15.30 | 0.04 | 0.08 | -24.50 18 | TTDC |
| Zeolite BEA-Mg | 65.36 u | 65.36 v | 0.00 | -159.79 | 15.30 | 15.30 | 0.41 | 0.08 | -13.39 18 | TTDC |
| Zeolite BEA-Ca | 65.36 u | 65.36 v | 0.00 | -114.11 | 15.30 | 15.30 | 0.041 | 0.08 | -25.33 18 | TTDC |
| Zeolite BEA-Ca | 65.36 u | 65.36 v | 0.00 | -114.11 | 15.30 | 15.30 | 0.39 | 0.08 | -14.01 18 | TTDC |
| Zeolite BEA-Sr | 65.36 u | 65.36 v | 0.00 | -64.31 | 15.30 | 15.30 | 0.03 | 0.08 | -22.00 18 | TTDC |
| Zeolite BEA-Sr | 65.36 u | 65.36 v | 0.00 | -64.31 | 15.30 | 15.30 | 0.37 | 0.08 | -11.80 18 | TTDC |
| Zeolite BEA-Ba | 65.36 u | 65.36 v | 0.00 | -58.83 | 15.30 | 15.30 | 0.02 | 0.08 | -21.75 18 | TTDC |
| Zeolite BEA-Ba | 65.36 u | 65.36 v | 0.00 | -58.83 | 15.30 | 15.30 | 0.36 | 0.08 | -11.48 18 | TTDC |
| Zeolite BEA-Mg | 65.36 u | 65.36 v | 0.00 | -147.10 | 15.30 | 15.30 | 0.04 | 0.25 | -33.50 18 | TTDC |
| Zeolite BEA-Mg | 65.36 u | 65.36 v | 0.00 | -147.10 | 15.30 | 15.30 | 0.50 | 0.25 | -17.96 18 | TTDC |
| Zeolite BEA-Ca | 65.36 u | 65.36 v | 0.00 | -101.26 | 15.30 | 15.30 | 0.04 | 0.25 | -38.25 18 | TTDC |
| Zeolite BEA-Ca | 65.36 u | 65.36 v | 0.00 | -101.26 | 15.30 | 15.30 | 0.43 | 0.25 | -20.75 18 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.07 | 0.33 | -49.13 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.09 | 0.33 | -79.02 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.13 | 0.33 | -66.54 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.21 | 0.33 | -48.67 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.26 | 0.33 | -51.57 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.33 | 0.33 | -45.93 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.38 | 0.33 | -37.92 19 | TTDC |
| Zeolite BEA-Li | 65.36 u | 65.36 v | 0.00 | -72.50 | 15.30 | 15.30 | 0.47 | 0.33 | -33.15 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.03 | 0.27 | -17.67 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.05 | 0.27 | -30.50 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.11 | 0.27 | -29.62 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.13 | 0.27 | -25.95 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.16 | 0.27 | -24.35 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.21 | 0.27 | -24.50 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.24 | 0.27 | -22.19 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.30 | 0.27 | -16.96 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.33 | 0.27 | -16.75 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.39 | 0.27 | -14.91 19 | TTDC |
| Zeolite BEA-Na | 65.36 u | 65.36 v | 0.00 | 12.41 | 15.30 | 15.30 | 0.43 | 0.27 | -16.40 19 | TTDC |
| Clinoptilolite-Na | 2000.00 f | 2140.00 f | 6.57 | 51.39 | 18.02 | 16.84 | 0.30 | 0.23 | -23.40 20 | IC |
| Clinoptilolite-K | 2019.51 b | 2089.50 b | 3.78 | 109.16 | 17.82 | 17.22 | 0.26 | 0.24 | -22.40 20 | IC |
| Clinoptilolite-Ca | 2019.51 b | 2089.50 b | 3.20 | -64.60 | 17.78 | 17.19 | 0.31 | 0.23 | -30.40 20 | IC |
| Zeolite X-Na | 15811.40 w | 15811.40 x | 0.00 | 65.80 | 12.14 | 12.14 | 0.49 | 0.811 | -24.60 21 | IC |
| Zeolite X-Mn | 15550.10 y | 15550.10 x | 0.00 | -116.22 | 12.35 | 12.35 | 0.54 | 0.811 | -22.25 21 | IC |
| Zeolite X-Zn | 15550.10 y | 15550.10 x | 0.00 | -146.64 | 12.35 | 12.35 | 0.55 | 0.811 | -19.89 21 | IC |
| Zeolite X-Mg | 15550.10 y | 15550.10 x | 0.00 | -57.94 | 12.35 | 12.35 | 0.59 | 0.811 | -23.40 21 | IC |
| Zeolite Y-Na | 15227.20 r | 14996.13 r | -0.92 | 65.80 | 12.61 | 12.80 | 0.50 | 0.433 | -17.40 21 | IC |
| Zeolite Y-Mn | 14465.76 z | 14246.20 aa | -0.76 | -100.10 | 13.27 | 13.48 | 0.61 | 0.433 | -19.89 21 | IC |
| Zeolite Y-Zn | 14465.76 z | 14246.20 aa | -0.71 | -139.96 | 13.27 | 13.48 | 0.65 | 0.433 | -20.45 21 | IC |
| Zeolite Y-Mg | 14465.76 z | 14246.20 aa | -0.73 | -72.41 | 13.27 | 13.48 | 0.63 | 0.433 | -20.70 21 | IC |
| Zeolite L-K | 2199.00 ab | 2199.00 ab | 0.00 | 132.64 | 16.37 | 16.37 | 0.28 | 0.333 | -16.90 21 | IC |
| Zeolite L-Li | 2199.00 ab | 2199.00 ab | 0.00 | 96.89 | 16.37 | 16.37 | 0.29 | 0.333 | -21.40 21 | IC |
| Zeolite L-Na | 2199.00 ab | 2199.00 ab | 0.00 | 111.76 | 16.37 | 16.37 | 0.28 | 0.333 | -17.60 21 | IC |
| Zeolite L-Rb | 2199.00 ab | 2199.00 ab | 0.00 | 150.64 | 16.37 | 16.37 | 0.25 | 0.333 | -15.70 21 | IC |
| Zeolite A-Na | 1839.84 ac | 1860.87 ac | 0.81 | 65.80 | 13.04 | 12.90 | 0.42 | 1.000 | -25.90 21 | IC |

Table 3 (end)

| Zeolite minerals | V u.c. anh. | Vu.c. hydr. | k | HO= | FD anh. | FD hyd. | WP | Al/Si | H hyd-W | Meth. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (Å3) | (Å3) |  | Site A |  |  |  |  | kJmol-1 |  |
|  |  |  |  | kJmol-1 |  |  |  |  | H2O |  |
| Zeolite A-Mg | 1831.53 ad | 1853.89 ae | 0.66 | -31.06 | 13.10 | 12.95 | 0.55 | 1.000 | -26.75 21 | IC |
| Zeolite A-Zn | 1831.53 ad | 1853.89 ae | 0.65 | -168.59 | 13.10 | 12.95 | 0.56 | 1.00 | -22.03 21 | IC |
| Zeolite X-Na | 15811.40 w | 15811.40 x | 0.00 | 65.80 | 12.14 | 12.14 | 0.49 | 0.829 | -24.61 22 | IC |
| Zeolite X-Na | 15811.40 w | 15811.40 x | 0.00 | 65.80 | 12.14 | 12.14 | 0.37 | 0.83 | -26.71 22 | IC |
| Zeolite X-Li | 15811.40 w | 15811.40 x | 0.00 | -40.90 | 12.14 | 12.14 | 0.49 | 0.829 | -25.06 22 | IC |
| Zeolite X-K | 15866.20 af | 15866.20 x | 0.00 | 141.00 | 12.10 | 12.10 | 0.45 | 0.829 | -23.97 22 | IC |
| Zeolite X-Rb | 15445.70 ag | 15811.40 x | 1.39 | 140.82 | 12.43 | 12.14 | 0.50 | 0.829 | -23.41 22 | IC |
| Zeolite X-Cs | 15448.70 ag | 15811.40 x | 1.53 | 138.86 | 12.43 | 12.14 | 0.45 | 0.829 | -22.72 22 | IC |
| Zeolite X-Ca | 15550.10 z | 15550.10 ah | 0.00 | -92.10 | 12.35 | 12.35 | 0.54 | 0.829 | -28.21 22 | IC |
| Zeolite X-Mg | 15550.10 y | 15550.10 x | 0.00 | -81.62 | 12.35 | 12.35 | 0.56 | 0.829 | -24.34 22 | IC |
| Zeolite X-Sr | 16029.70 ai | 16029.70 x | 0.00 | -40.40 | 11.98 | 11.98 | 0.53 | 0.829 | -28.33 22 | IC |
| Zeolite X-Ba | 16029.70 ai | 16029.70 x | 0.00 | 3.11 | 11.98 | 11.98 | 0.49 | 0.829 | -27.34 22 | IC |
| Zeolite Y-Na | 15227.20 r | 14996.13 r | -0.94 | 30.64 | 12.61 | 12.80 | 0.49 | 0.422 | -17.53 22 | IC |
| Zeolite Y-Na | 15227.20 r | 14996.13 r | -1.26 | 30.64 | 12.61 | 12.80 | 0.37 | 0.42 | -19.59 22 | IC |
| Zeolite Y-Li | 15227.20 s | 14996.13 t | -0.92 | -65.39 | 12.61 | 12.80 | 0.50 | 0.422 | -17.22 22 | IC |
| Zeolite Y-K | 15320.01 s | 15087.53 t | -1.11 | 98.32 | 12.53 | 12.73 | 0.42 | 0.422 | -18.02 22 | IC |
| Zeolite Y-Rb | 15301.42 s | 15069.22 t | -1.10 | 90.98 | 12.55 | 12.74 | 0.42 | 0.422 | -17.43 22 | IC |
| Zeolite Y-Cs | 15301.42 s | 15069.22 t | -1.18 | 95.17 | 12.55 | 12.74 | 0.39 | 0.422 | -17.46 22 | IC |
| Zeolite Y-Ca | 15282.84 s | 15050.93 t | -0.94 | -67.15 | 12.56 | 12.76 | 0.49 | 0.422 | -21.15 22 | IC |
| Zeolite Y-Sr | 15282.84 s | 15050.93 t | -0.92 | -35.13 | 12.56 | 12.76 | 0.50 | 0.422 | -20.61 22 | IC |
| Zeolite Y-Ba | 15341.73 s | 14899.65 t | -1.80 | -19.77 | 12.51 | 12.89 | 0.49 | 0.422 | -21.48 22 | IC |
| Zeolite A-Na | 1839.84 ac | 1860.87 ac | 0.81 | 65.80 | 13.04 | 12.90 | 0.42 | 1.000 | -25.89 22 | IC |
| Zeolite A-Na | 1838.59 ac | 1860.87 ac | 1.13 | 65.80 | 13.05 | 12.90 | 0.32 | 1.00 | -30.05 22 | IC |
| Zeolite A-Li | 1709.10 aj | 1728.64 ae | 0.82 | -40.90 | 14.04 | 13.88 | 0.41 | 1.000 | -25.52 22 | IC |
| Zeolite A-K | 1860.86 ak | 1882.13 ae | 0.89 | 141.00 | 12.90 | 12.75 | 0.38 | 1.000 | -29.10 22 | IC |
| Zeolite A-Cs | 1843.23 al | 1864.30 ae | 0.88 | 113.73 | 13.02 | 12.87 | 0.38 | 1.000 | -22.88 22 | IC |
| Zeolite A-Ca | 1831.53 am | 1852.46 ae | 0.76 | -92.10 | 13.10 | 12.96 | 0.45 | 1.000 | -27.18 22 | IC |
| Zeolite A-Mg | 1824.80 an | 1845.65 ae | 0.62 | -67.80 | 13.15 | 13.00 | 0.54 | 1.000 | -27.13 22 | IC |
| Chabazite-Ca | 2427.00 f | 2467.20 f | 1.14 | -67.81 | 14.83 | 14.59 | 0.43 | 0.410 | -27.38 22 | IC |
| Chabazite-Na | 2427.00 f | 2467.20 f | 1.25 | 65.80 | 14.83 | 14.59 | 0.39 | 0.406 | -25.95 22 | IC |
| Chabazite-Na | 2427.00 f | 2467.20 f | 1.64 | 65.80 | 14.83 | 14.59 | 0.30 | 0.41 | -35.07 22 | IC |
| Chabazite-Li | 2427.00 f | 2467.20 f | 1.14 | -45.78 | 14.83 | 14.59 | 0.43 | 0.406 | -25.06 22 | IC |
| Chabazite-K | 2427.00 f | 2467.20 f | 1.35 | 118.80 | 14.83 | 14.59 | 0.36 | 0.406 | -22.72 22 | IC |
| Chabazite-Rb | 2427.00 f | 2467.20 f | 1.48 | 138.92 | 14.83 | 14.59 | 0.33 | 0.406 | -21.18 22 | IC |
| Chabazite-Cs | 2427.00 f | 2467.20 f | 1.56 | 117.58 | 14.83 | 14.59 | 0.31 | 0.406 | -18.61 22 | IC |
| Mordenite-Na | 2743.43 ao | 2796.65 ao | 2.07 | 30.64 | 17.50 | 17.16 | 0.27 | 0.200 | -26.30 22 | IC |
| Clinoptilol.-Na | 1911.42 ap | 2132.20 ap | 10.64 | 65.80 | 18.83 | 16.88 | 0.29 | 0.200 | -22.06 22 | IC |
| Ferrierite-Sr | 1974.89 aq | 2022.82 aq | 2.89 | -40.40 | 18.27 | 17.83 | 0.25 | 0.16 | -16.81 22 | IC |
| Ferrierite-Na | 1974.89 aq | 2022.82 aq | 2.46 | 65.80 | 18.27 | 17.83 | 0.29 | 0.16 | -17.25 22 | IC |
| Ferrierite-Li | 1974.89 aq | 2022.82 aq | 2.13 | -40.90 | 18.27 | 17.83 | 0.33 | 0.16 | -16.37 22 | IC |
| Ferrierite-Ca | 1974.89 aq | 2022.82 aq | 2.31 | -92.10 | 18.27 | 17.83 | 0.31 | 0.16 | -18.88 22 | IC |
| Clinoptilol. -Na | 2000.00 f | 2140.00 f | 6.42 | 63.84 | 17.90 | 16.73 | 0.30 | 0.185 | -23.00 23 | GAC |
| Clinoptilolite-K | 2029.98 ar | 2099.57 i | 4.02 | 119.27 | 17.64 | 17.06 | 0.25 | 0.193 | -19.00 23 | GAC |
| Clinoptilol. -Ca | 2019.98 b | 2089.01 b | 2.89 | -51.63 | 17.78 | 17.19 | 0.34 | 0.200 | -31.30 23 | GAC |
| Clinoptilol. -Na | 2000.00 f | 2140.00 f | 6.35 | 51.39 | 18.02 | 16.84 | 0.31 | 0.23 | -30.17 24 | PE |
| Clinoptilolite-K | 2019.51 b | 2089.50 b | 3.78 | 109.16 | 17.82 | 17.22 | 0.26 | 0.24 | -23.97 24 | PE |
| Clinoptilol. -Ca | 2019.51 b | 2089.50 b | 3.20 | -64.60 | 17.78 | 17.19 | 0.31 | 0.23 | -32.87 24 | PE |
| Clinoptilol. -Na | 333.33 f | 356.67 f | 6.70 | 67.18 | 17.97 | 16.79 | 0.29 | 0.22 | -40.77 25 | PE |
| Clinoptilolite-K | 336.59 b | 348.25 b | 4.40 | 140.29 | 17.83 | 17.23 | 0.23 | 0.22 | -36.97 25 | PE |
| Chabazite | 809.00 f | 822.40 f | 1.06 | -62.37 | 14.86 | 14.62 | 0.46 | 0.41 | -39.64 26 | PE |

Footnote added at the end of Table 3

For references 1 to 26, see footnotes added at the end of table 1.

a -  Cruciani and Gualtieri (1999); b - Armbruster (1993); c - Johnson et al. (1992a); d - Alberti et al. (2001); e - Alberti et al. (2001); f - Bish and Carey (2001); g - Benco et al. (2003); h - Estimated from Vu.c hyd. using van Reeuwijk (1974); i - Coombs et al. (1997); j -  Armbruster and Gunter (1991); k -  Fridriksson et al. (2003); l -  Stahl and Hanson (1994); m - Cruciani et al. (2003); n - Baur and Joswig (1996); o - Arletti et al. (2006); p - Cruciani et al. (1997); q -  Stahl and Thomasson (1992); r - Mortier et al. (1984); s - Estimated from Vu.c hyd. using Mortier et al. (1984); t - Yang and Navrotsky (2000); u – Assumed equal to Vu.c.  hyd. ); v –Sun et al. (2007);  w - Olson (1995); x - Estimated from Vu.c anh. using   Smolin et al. (1989 and Dooryhee et al. (1991); y - Pluth and Smith (1972); z - Dooryhee et al. (1991); aa - Estimated from Vu.c anh.. using Mortier et al. (1984); ab - Larlus and Valtchev (2004); ac - Bursill et al. (1981); ad - Porcher et al. (2000); ae - Estimated from Vu.c anh.. using Bursill et al. (1981); af - Jang and Kim (1995); ag - Jang et al. (1999); ah - Smolin et al. (1989); ai - Kim et al. (1999); aj - Jirak et al. (1983); ak - Pluth and Smith (1979); al - Pluth and Smith (1983a); am - Porcher et al. (2000); an - Pluth and Smith (1983b); ao - Martucci et al. (2003); ap - Johnson et al. (2003); aq -  Dalconi et al. (2003); ar - Estimated from Vu.c hyd. using Johnson et al. (2003).