Appendix

Table A. Comparison between observed (Popović et al. 2009) and calculated (from ionic radii of Shannon 1976) polyhedral bond lengths in gahnite–Co-aluminate solid solution as a function of the inversion parameter (x).

| ZnAl2O4–CoAl2O4 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| nominal cobalt content, y (apfu) | x | (T–O(Obs (Å) | (T–O(Calc (Å) | T(Obs-Calc) (Å) | (M–O(Obs (Å) | (M–O(Calc (Å) | M(Obs-Calc) (Å) |
| 0.00 | 0.000 | 1.953 | 1.950 | 0.003 | 1.913 | 1.915 | -0.002 |
| 0.25 | 0.070 | 1.937 | 1.939 | -0.002 | 1.925 | 1.922 | 0.003 |
| 0.50 | 0.095 | 1.932 | 1.937 | -0.005 | 1.926 | 1.925 | 0.001 |
| 0.75 | 0.150 | 1.929 | 1.929 | 0.000 | 1.929 | 1.931 | -0.002 |
| 1.00 | 0.248 | 1.914 | 1.913 | 0.001 | 1.939 | 1.941 | -0.002 |
| δ |  | 0.039 | 0.037 |  | 0.026 | 0.026 |  |
| Note: symbols and meaning of the values are the same as described in the notes of Table 2. |