Crystal structure refinements of borate dimorphs inderite and kurnakovite using 11B and 25Mg nuclear magnetic resonance and DFT calculations

Bing Zhou1, 2, Vladimir K. Michaelis3Ŧ, Yuanming Pan4, Yefeng Yao5, Kimberly T. Tait6, Brendt C. Hyde6, John E.C. Wren, Barbara L. Sherriff7 and Scott Kroeker3*

Supporting Information-

Powder x-ray diffraction data:

X-ray diffraction analysis used a Bruker D8 Advance with Da Vinci design at the Royal Ontario Museum.  This system employed a Cu source running at 40 kV and 40 mA and a LynxEye detector.  Small amounts of representative powder were dusted onto a low background plate and the samples were scanned in steps of 0.01° from 10 to 70° 2θ.