Scordari et al.: FLUOROPHLOGOPITE FROM PIANO DELLE CONCAZZE (Mt. ETNA, ITALY); Deposit material (7 total items); AM-13-046; American Mineralogist May June 2013

Table 5    Selected distortion parameters of the studied crystals.

|  | E0 | E1 | E2 | E3 |  |
| --- | --- | --- | --- | --- | --- |
| ttet [Å] | 2.234 | 2.236 | 2.237 | 2.236 |  |
| BLD T | 0.177 | 0.134 | 0.149 | 0.165 |  |
| Volume T [Å3] | 2.30 | 2.30 | 2.30 | 2.30 |  |
| TQE | 1.0005 | 1.0005 | 1.0005 | 1.0005 |  |
| TAV | 1.944 | 1.948 | 2.077 | 1.887 |  |
| τ [°] | 110.66 | 110.66 | 110.71 | 110.64 |  |
| α [°] | 4.83 | 4.87 | 4.80 | 4.81 |  |
| Δz [Å] | 0.003 | 0.006 | 0.005 | 0.007 |  |
| D.M. [Å] | 0.477 | 0.480 | 0.478 | 0.482 |  |
| ΨM1 [°] | 59.25 | 59.32 | 59.26 | 59.32 |  |
| ΨM2 [°] | 59.03 | 59.04 | 59.04 | 59.07 |  |
| BLDM1 | 1.043 | 1.020 | 1.054 | 1.044 |  |
| ELDM1 | 5.412 | 5.495 | 5.423 | 5.502 |  |
| BLDM2 | 1.785 | 1.945 | 1.779 | 1.828 |  |
| ELDM2 | 5.153 | 5.167 | 5.175 | 5.202 |  |
| ShiftM2 [Å] | 0.0250 | 0.0274 | 0.0240 | 0.0261 |  |
| Volume M1 [Å] | 11.71 | 11.75 | 11.68 | 11.72 |  |
| OQEM1 | 1.013 | 1.014 | 1.013 | 1.014 |  |
| OAVM1 | 42.616 | 44.107 | 43.018 | 44.219 |  |
| Volume M2 [Å3] | 11.50 | 11.49 | 11.49 | 11.49 |  |
| OQEM2 | 1.012 | 1.012 | 1.012 | 1.013 |  |
| OAVM2 | 39.242 | 39.598 | 39.476 | 39.938 |  |
| euM1/ esM1 | 1.114 | 1.116 | 1.115 | 1.117 |  |
| euM2/ esM2 | 1.109 | 1.109 | 1.109 | 1.110 |  |
| toct [Å] | 2.124 | 2.122 | 2.122 | 2.120 |  |
| tint [Å] | 3.290 | 3.293 | 3.288 | 3.292 |  |
| ΔK-O [Å] | 0.221 | 0.223 | 0.219 | 0.221 |  |
| tK-O4 [Å] | 3.920 | 3.929 | 3.922 | 3.923 |  |

Note: ttet: tetrahedral sheet thickness calculated from z coordinates of basal and apical O atoms; TQE: tetrahedral quadratic elongation calculated as TQE = ∑i(li/l0)2/4 where l0 is the center to vertex distance for an undistorted tetrahedron (Robinson et al. 1971); TAV: tetrahedral angle variance defined as TAV = ∑i(θi-109.47°)2/5 (Robinson et al. 1971); τ: tetrahedral flattening angle; α: tetrahedral rotation angle (Hazen and Burnham, 1973); Δz: departure from co planarity of the basal O atoms, calculated as Δz = (zo2 – zo1)csinβ (Güven 1971); D.M.: dimensional misfit between tetrahedral and octahedral sheets defined as D.M. = [23<O – O > bas - 32<M – O>] (Toraya 1981); Ψ: octahedral flattening angles (Donnay et al. 1964); BLD: bond-length distortions calculated as BLD = 100/n * ∑i I(M – O)i -<M – O> I / <M – O> (Renner and Lehmann 1986); ELD: edge-length distortion defined as ELD = 100/n * ∑i I(O – O)i -<O – O> I / <O – O>) (Renner and Lehman 1986); ShiftM2: off-center shift of the M2 cation defined as the distance between the refined position of cation and the geometrical center of M2 site (coordinates: x/a = 0.0, y/b = 0.8333, z/c = 0.5); OQE: octahedral quadratic elongation calculated as OQE = ∑i(li/l0)2/6 where l0 is the center to vertex distance for an undistorted octahedron (Robinson et al. 1971); OAV: octahedral angle variance defined as OAV = ∑i(θi-90°)2/11 (Robinson et al. 1971); eu,es: mean lengths of unshared and shared edges (Toraya 1981), respectively;  toct: octahedral sheet thickness (Toraya, 1981); tint calculated from the z coordinates of  basal O atoms; ΔK-O = <K-O>outer-<K-O>inner; tK-O4: projection of K-O4 distance along c*