Supplemental Table A1. List of studies reporting silician magnetite.

| Rock type | Locality | SiO2 wt%* |
| --- | --- | --- |
| Banded Iron Formation |  |  |
| Morris (1991) | Dales Gorge Member, Brockman Iron Formation, Hamersley Group, Paraburdoo, Western Australia | nr |
| Pecoits et al. (2009) | Dales Gorge Member, Brockman Iron Formation, Hamersley Group, Paraburdoo, Western Australia | 2.0 |
| Huberty et al. (2011, this study) | Dales Gorge Member, Brockman Iron Formation, Hamersley Group, Wittenoom, Western Australia | 3.0 |
| Serpentinite |  |  |
| Shcheka et al. (1977) | Serpentinized peridotites, Atlantic and Indian mid-ocean ridges | 5.4 |
| Volcanogenic Massive Sulfide |  |  |
| Oudin (1981) | Hydrothermal sulfide mounds, East Pacific Rise | 1.7 |
| Shimazaki (1998) | Yanahara deposit, Japan | 2.1 |
| Westendorp et al. (1991) | Cu-Zn Ansil mine, Noranda district, Quebec, Canada | 6.5 |
| Porphyry/Skarn |  |  |
| Ciobanu and Cook (2004) | Ocna de Fier-Dognecea deposit | 6.0 |
| Imai et al. (2001) | Cu-Au porphyry, Santo Thomas, Philippines | 8.9 |
| Imai and Anan (2000) | Cu-Au porphyry, Hol Kol & Tul Mi Ching, Korea | 1.4 |
| Modreski and Chou (1981) | Ortiz Au mine, New Mexico, USA | 2.4 |
| Ohkawa et al. (2007) | Kumano skarn, Japan | 3.8 |
| Petrova and Tatarsky (1975) | Korshunovskoye skarn, Russia | 3.8 |
| Pons et al. (2009) | Fe skarn, Vegas Paladas, Mendoza, Argentina | 2.9 |
| Schwartz and Melcher (2004) | Fe skarn, Karakaene-Ndi, Falémé Iron District, Senegal | 1.9 |
| Shcheka et al. (1977) | Korshunovskoye skarn, Russia | 3.9 |
| Shiga (1988, 1989) | Fe-Cu skarn, Kamaishi mine, Japan | 6.3 |
| Shimazaki (1998) | 23 skarn deposits in Japan, Korea, and USA | 5.4 |
| Wang et al. (2001) | Huanggang Fe-Sn deposit, Inner Mongolia, China | 5.0 |
| Igneous |  |  |
| Anderson (1966) | Labrieville anorthosite, Quebec, Canada | 0.6 |
| Basta (1959) | Kropferberg, Saxony, Germany | 1.5 |
| Bauer et al. (1973) | Kauaopuu ridge rhyodacite, Hawaii, USA | 0.9 |
| Igneous |  |  |
| Czamanske and Mihalik (1972) | Finnmarka Intrusive Complex, Oslo, Norway | 0.4 |
| Duchesne et al. (1972) | Bjerkrem-Sogndal Anorthosite Massif, Norway | 1.0 |
| Gold (1966) | Oka carbonatite complex, Quebec, Canada | 7.5 |
| Modreski and Chou (1981) | Rhyolite, Round Mountain, Nevada, USA | 3.7 |
| Newberry et al. (1982) | Ash flow tuff, Mickey Pass, Nevada, USA | 5.0 |
| Puffer (1972) | Pegmatite, Pegmatite Points area, Colorado, USA | 1.6 |
| Puffer (1975) | Pegmatite, St. Louis County, Minnesota, USA | 1.0 |
| Rodriguez-Losada et al (2004) | Trachytic–Phonolitic Complex, La Gomera, Canary Islands | 0.3 |
| Stout and Bayliss (1975) | McKinney lava flow, Snake River Plain, Idaho, USA | 0.2 |
| Takagi (1992) | Ukan granodiorite, San'yo belt, Okayama Prefecture, Japan | 5.4 |
| Vincent and Phillips (1954) | Layered gabbros, Skaergaard intrusion, Greenland | 0.2 |
| Whitney and Stormer (1976) | Albany quartz syenite, White Mountain batholith, New Hampshire, USA | 0.2 |
| Other |  |  |
| Gomes et al. (1999) | Silico-aluminous fly ash, Metz, France | 1.0 |
| Laboratory studies | Experimental technique |  |
| Modreski and Chou (1981) | Synthetic run products on the quartz-fayalite-magnetite buffer | 1.9 |

*maximum SiO2 wt%.

Notes:

nr = chemical analyses not reported.

REFERENCES

# Anderson, A.T. Jr. (1966) Mineralogy of the Labrieville anorthosite, Quebec. American

Mineralogist, 51, 1671-1711.

Basta, E.Z. (1959) Some mineralogical relationships in the system Fe2O3-Fe3O4 and the 	composition of titanomaghemite. Economic Geology, 54, 698-719.

Bauer, G.R., Fodor, R.V., Husler, J.W., and Keil, K. (1973) Contributions to the mineral

chemistry of Hawaiian rocks. III. Composition and mineralogy of a new rhyodacite 	occurrence. Contributions to Mineralogy and Petrology, 40, 183-194.

Ciobanu, C.L., and Cook, N.J. (2004) Skarn textures and a case study: the Ocna de Fier-	Dognecea orefield, Banat, Romania. Ore Geology Reviews, 24, 315-370.

Czamanske, G.K., and Mihalik, P. (1972) Oxidation during magmatic differentiation. 	Finnmarka Complex, Oslo area, Norway: Part I, The opaque oxides. Journal of 	Petrology, 14, 493-509.

Duchesne, J.C. (1972) Iron-titanium oxide minerals in the Bjerkrem-Sogndal Massif, south-

western Norway. Journal of Petrology, 13, 57-81.

Gold, D.P. (1966) The minerals of the Oka carbonatite and alkaline complex, Oka, Quebec. 	Mineralogical Society of India, IMA Volume (Fourth General Meeting), 109-125.

Gomes, S., François, M., Abdelmoula, M., Refait, Ph., Pellissier, C., and Evrard, O. (1999) 	Characterization of magnetite in silico-aluminous fly ash by SEM, TEM, XRD, magnetic 	susceptibility and Mössbauer spectroscopy. Cement and Concrete Research, 29, 1705-	1711.

Imai, A. (2001) Generation and evolution of ore fluids for porphyry Cu-Au mineralization of 	the Santo Tomas II (Philex) Deposit, Philippines. Resource Geology, 51, 2, 71-76.

Imai, A., and Anan, S. (2000) Sulfur isotope study and re-examination of ore mineral 	assemblage of the Hol Kol and the Tul Mi Chung skarn-type copper-gold deposits of 	the Suan Mining District, Korean Peninsula. Resource Geology, 50, 4, 213-228.

Modreski, P.J., and Chou, I.-M. (1981) The silica content of magnetite from the fayalite-

magnetite-quartz assemblage and from hydrothermal ore deposits. Geological Society of 	America Abstracts and Programs 13, 513.

Morris, R.C. (1991) The Marra Marmba Iron Formation of the Hamersley Group of Western 	Australia. CSIRO/AMIRA Iron Ores of the Hamersley Province Project P75F, 	Exploration Geoscience Restricted Report 158R, 229 p.

Newberry, N.G., Peacor, D.R., Essene, E.J. and Geissman, J.W. (1982) Silicon in magnetite: 	High-resolution microanalysis of magnetite-ilmenite intergrowths. Contributions to 	Mineralogy and Petrology, 80, 334-340.

Ohkawa, M., Miyahara, M., Ohta, E. and Hoshino, K. (2007) Silicon-substituted magnetite and 	accompanying iron oxides and hydroxides from the Kumano mine, Yamaguchi 	Prefecture, Japan: Reexamination of the so-called maghemite (-Fe2O3). Journal of 	Mineralogical and Petrological Sciences, 102, 182-193.

Oudin, E. (1981) Etude mineralogique et geochemique des depots sulfures sous-marins actuels 	de la ride Est-Pacifique (21°N). Bureau de Recherches Géologiques et Minières 	Documents 25, 241 p. (in French).

Pecoits, E., Gringas, M.K., Barley, M.E., Kappler, A., Posth, N.R. and Konhauser, K.O. (2009) 	Petrography and geochemistry of the Dales Gorge banded iron formation: Paragenetic 	sequence, source and implications for palaeo-ocean chemistry. Precambrian Research, 	172, 163-187.

Petrova, L.V., and Tatarsky, V.B. (1975) Silica-lime magnetite of Korshunovskoye deposit, 	Zapiski Vsesoyuznogo Mineralogy Obshchestva, 103, 3, 301-309 (in Russian).

Pons, J.M., Franchini, M.B., and Impiccini, A. (2009) Los Skarns de Fe de Vegas Peladas: 	Características Geológicas, Mineralógicas y Distribución de Las Paragénesis Minerales. 	Revista de la Associación Geológica Argentina, 64, 2, 329-351 (in Spanish).

Puffer, J.H. (1972) Iron-bearing minerals as indicators of intensive variables pertaining to 	granitic rocks from the Pegmatite points area, Colorado. American Journal of Science, 	272, 273-289.

Puffer J.H. (1975) Some North American iron-titanium oxide bearing pegmatites. American 	Journal of Science, 275, 708-732.

Rodriguez-Losada, J.A., and Martinez-Frias, J. (2004) The felsic complex of the Vallehermoso 	Caldera: interior of an ancient volcanic system (La Gomera, Canary Islands). Journal of 	Volcanology and Geothermal Research, 137, 261-284.

Schwartz, M.O., and Melcher, F. (2004) The Falémé Iron District, Senegal. Economic Geology, 	99, 917-939.

Shcheka, S.A., Romanenko, I.M. and Chubarov, V.M. (1977) Silica-bearing magnetites. 	Contributions to Mineralogy and Petrology, 63, 103-111.

Shiga, Y. (1988) Silician Magnetite from the Kamaishi Mine, Japan. Mining Geology, 38, 5, 	437-440.

Shiga, Y. (1989) Further study on silician magnetite. Mining Geology, 39, 5, 305-309.

Shimazaki, H. (1998) On the occurrence of silician magnetites. Resource Geology, 48, 1, 23-29.

Stout, M.Z., and Bayliss, P. (1975) Crystal structure of a natural titanomagnetite. Canadian

Mineralogist, 13, 86-88.

Takagi, T. (1992) Mineral equilibria and crystallization conditions of Ukan Granodiorite 	(imenite-series) and Kayo Granite (magnetite-series), San'yo Belt, Southwest Japan. 	Journal of the Geological Society of Japan, 98, 2, 102-124.

Vincent, E.A., and Philipps, R. (1954) Iron-titanium oxide minerals in layered gabbros of the

Skaergaard intrusion, east Greenland, part 1: Chemistry and ore-microscopy. Geochimica 	et Cosmochimica Acta, 6, 1-26.

Wang, L.J., Shimazaki, H., and Shiga, Y. (2001) Skarns and genesis of the Huanggang Fe-Sn 	deposit, Inner Mongolia, China. Resource Geology, 51, 4, 359-376.

Westendorp, R.W. and Watkinson, D.H. (1991) Silicon-bearing zoned magnetite crystals and the 	evolution of hydrothermal fluids at the Ansil Cu-Zn mine, Rouyn-Noranda, Quebec. 	Economic Geology, 86, 1110-1114.

Whitney, J.A., and Stormer, J.C. Jr, (1976) Geothermometry and geobarometry in epizonal 	granitic intrusions: A comparison of iron-titanium oxides and coexisting feldspars. 	American Mineralogist, 61, 751-763.

# Supplemental Table A2. Electron microprobe analyses of silician magnetite and magnetite.

| analysis # | Fe3O4 Oxide % | SiO2 Oxide % | MgO Oxide % | MnO Oxide % | TiO2 Oxide % | Al2O3 Oxide % | ZnO Oxide % | Fe Atoms | Si Atoms | Mg Atoms | Mn Atoms | Ti Atoms | Al Atoms | Zn Atoms | Total Cations |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Session 1: July 2008 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| BIF5 3-3A-d |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 137 | 98.95 | 1.95 | 0.11 | 0.03 | <0.02 | <0.04 | <0.15 | 2.882 | 0.073 | 0.006 | 0.002 |  |  |  | 2.963 |
| 138 | 99.28 | 0.65 | 0.20 | <0.03 | <0.02 | <0.04 | <0.15 | 2.950 | 0.025 | 0.011 |  |  |  |  | 2.986 |
| 139 | 99.53 | 0.44 | 0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.973 | 0.017 | 0.003 |  |  |  |  | 2.993 |
| 140 | 99.99 | 0.48 | 0.10 | <0.03 | <0.02 | <0.04 | <0.15 | 2.969 | 0.018 | 0.006 |  |  |  |  | 2.993 |
| 141 | 100.89 | 0.44 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.971 | 0.017 | 0.005 |  |  |  |  | 2.992 |
| 142 | 100.35 | 0.43 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.971 | 0.016 | 0.004 |  |  |  |  | 2.991 |
| 143 | 99.71 | 0.48 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.969 | 0.018 | 0.005 |  |  |  |  | 2.992 |
| 144 | 99.87 | 0.24 | <0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.982 | 0.009 |  |  | 0.001 |  |  | 2.992 |
| 145 | 99.33 | 0.61 | 0.08 | <0.03 | <0.02 | 0.04 | <0.15 | 2.959 | 0.023 | 0.005 |  |  |  |  | 2.987 |
| 146 | 97.59 | 2.44 | 0.17 | <0.03 | <0.02 | <0.04 | <0.15 | 2.856 | 0.092 | 0.010 |  |  |  |  | 2.957 |
| 147 | 98.16 | 2.40 | 0.14 | <0.03 | 0.04 | <0.04 | <0.15 | 2.858 | 0.090 | 0.008 |  | 0.001 |  |  | 2.957 |
| 148 | 99.08 | 2.26 | 0.08 | <0.03 | 0.02 | <0.04 | <0.15 | 2.867 | 0.084 | 0.004 |  | 0.001 |  |  | 2.956 |
| 149 | 98.37 | 1.44 | 0.12 | <0.03 | <0.02 | <0.04 | <0.15 | 2.912 | 0.055 | 0.007 |  |  |  |  | 2.974 |
| 150 | 98.80 | 0.77 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.955 | 0.030 |  |  |  |  |  | 2.984 |
| 151 | 100.03 | 0.65 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.959 | 0.025 |  |  |  | 0.002 |  | 2.986 |
| 152 | 99.58 | 0.60 | <0.05 | <0.03 | <0.02 | 0.06 | <0.15 | 2.961 | 0.023 |  |  |  | 0.003 |  | 2.986 |
| 153 | 99.21 | 0.61 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.965 | 0.024 |  |  |  |  |  | 2.988 |
| 154 | 99.56 | 0.49 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.968 | 0.019 |  |  |  |  |  | 2.987 |
| 155 | 99.76 | 0.63 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.963 | 0.024 |  |  |  |  |  | 2.987 |
| 156 | 99.19 | 0.51 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.966 | 0.020 |  |  |  |  |  | 2.985 |
| 157 | 99.09 | 0.46 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.966 | 0.018 |  |  |  |  |  | 2.984 |
| 158 | 98.77 | 0.77 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.952 | 0.029 |  |  |  |  |  | 2.982 |
| 159 | 98.87 | 1.37 | <0.05 | <0.03 | 0.02 | 0.05 | <0.15 | 2.920 | 0.052 |  |  | 0.001 | 0.002 |  | 2.975 |
| 160 | 97.61 | 1.89 | 0.15 | <0.03 | <0.02 | 0.05 | <0.15 | 2.884 | 0.072 | 0.008 |  |  | 0.002 |  | 2.966 |
| 161 | 97.42 | 2.05 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.877 | 0.078 | 0.004 |  |  |  |  | 2.959 |
| 162 | 97.78 | 2.07 | 0.13 | <0.03 | <0.02 | <0.04 | <0.15 | 2.876 | 0.078 | 0.007 |  |  |  |  | 2.961 |
| 163 | 98.14 | 2.27 | 0.13 | <0.03 | 0.03 | 0.05 | <0.15 | 2.864 | 0.085 | 0.007 |  | 0.001 | 0.002 |  | 2.959 |
| 164 | 99.14 | 0.35 | 0.07 | 0.03 | <0.02 | <0.04 | <0.15 | 2.974 | 0.013 | 0.004 | 0.002 |  |  |  | 2.993 |
| 165 | 98.08 | 2.09 | 0.18 | <0.03 | <0.02 | <0.04 | <0.15 | 2.876 | 0.079 | 0.010 |  |  |  |  | 2.964 |
| 166 | 98.75 | 2.33 | 0.15 | <0.03 | 0.03 | <0.04 | <0.15 | 2.861 | 0.087 | 0.008 |  | 0.001 |  |  | 2.956 |
| 167 | 98.92 | 2.02 | 0.11 | <0.03 | <0.02 | <0.04 | <0.15 | 2.882 | 0.075 | 0.006 |  |  |  |  | 2.964 |
| 168 | 98.75 | 2.11 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.880 | 0.079 | 0.004 |  |  |  |  | 2.963 |
| 169 | 97.91 | 1.45 | 0.09 | <0.03 | <0.02 | <0.04 | <0.15 | 2.911 | 0.055 | 0.005 |  |  |  |  | 2.972 |
| 170 | 98.86 | 1.24 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.927 | 0.047 |  |  |  |  |  | 2.974 |
| 171 | 98.35 | 0.95 | 0.17 | <0.03 | <0.02 | 0.05 | <0.15 | 2.934 | 0.037 | 0.010 |  |  | 0.002 |  | 2.983 |
| 173 | 99.27 | 0.17 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.990 | 0.007 |  |  |  |  |  | 2.997 |
| 174 | 99.85 | 0.71 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.956 | 0.027 |  |  |  |  |  | 2.983 |
| 175 | 99.64 | 1.17 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.935 | 0.044 |  |  |  |  |  | 2.979 |
| 176 | 98.36 | 1.92 | 0.12 | <0.03 | <0.02 | 0.04 | <0.15 | 2.882 | 0.072 | 0.007 |  |  | 0.002 |  | 2.963 |
| 177 | 98.77 | 1.99 | 0.14 | <0.03 | 0.02 | <0.04 | <0.15 | 2.880 | 0.075 | 0.008 |  | 0.001 |  |  | 2.963 |
| 178 | 98.42 | 1.03 | 0.15 | 0.03 | 0.02 | <0.04 | <0.15 | 2.929 | 0.039 | 0.008 | 0.002 | 0.001 |  |  | 2.980 |
| 179 | 98.16 | 2.23 | 0.12 | <0.03 | 0.03 | <0.04 | <0.15 | 2.870 | 0.084 | 0.007 |  | 0.001 |  |  | 2.961 |
| 180 | 100.38 | 0.54 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.968 | 0.021 |  |  |  |  |  | 2.988 |
| 181 | 99.76 | 0.37 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.974 | 0.014 |  |  |  |  |  | 2.988 |
| 182 | 99.19 | 0.56 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.963 | 0.021 | 0.004 |  |  |  |  | 2.989 |
| 183 | 98.45 | 2.30 | 0.13 | <0.03 | 0.02 | <0.04 | <0.15 | 2.863 | 0.086 | 0.007 |  | 0.001 |  |  | 2.957 |
| 184 | 98.61 | 2.15 | 0.11 | <0.03 | 0.03 | <0.04 | <0.15 | 2.871 | 0.081 | 0.006 |  | 0.001 |  |  | 2.959 |
| 185 | 99.36 | 1.81 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.893 | 0.068 | 0.004 |  |  |  |  | 2.965 |
| 186 | 99.90 | 0.67 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.962 | 0.026 |  |  |  |  |  | 2.988 |
| 187 | 100.23 | 0.56 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.966 | 0.021 |  |  |  |  |  | 2.987 |
| 189 | 99.01 | 0.21 | <0.05 | <0.03 | 0.07 | <0.04 | <0.15 | 2.985 | 0.008 |  |  | 0.002 |  |  | 2.995 |
| 190 | 100.36 | 0.40 | <0.05 | <0.03 | 0.04 | <0.04 | <0.15 | 2.976 | 0.015 |  |  | 0.001 |  |  | 2.992 |
| 191 | 99.96 | 0.60 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.963 | 0.023 |  |  |  |  |  | 2.986 |
| 192 | 99.86 | 1.04 | <0.05 | 0.03 | <0.02 | <0.04 | <0.15 | 2.938 | 0.039 |  | 0.002 |  |  |  | 2.979 |
| 193 | 99.68 | 0.82 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.952 | 0.031 |  |  |  |  |  | 2.984 |
| 194 | 99.43 | 1.70 | 0.10 | <0.03 | 0.03 | <0.04 | <0.15 | 2.898 | 0.063 | 0.005 |  | 0.001 |  |  | 2.968 |
| 196 | 100.16 | 1.74 | 0.13 | <0.03 | <0.02 | <0.04 | <0.15 | 2.897 | 0.065 | 0.007 |  |  |  |  | 2.969 |
| 197 | 99.81 | 0.44 | 0.09 | <0.03 | <0.02 | 0.05 | <0.15 | 2.966 | 0.017 | 0.005 |  |  | 0.002 |  | 2.990 |
| 198 | 99.85 | 0.68 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.956 | 0.026 |  |  |  |  |  | 2.982 |
| 199 | 99.69 | 0.90 | 0.44 | <0.03 | <0.02 | <0.04 | <0.15 | 2.926 | 0.034 | 0.025 |  |  |  |  | 2.985 |
| 200 | 98.41 | 2.41 | 0.13 | <0.03 | 0.05 | <0.04 | <0.15 | 2.860 | 0.090 | 0.007 |  | 0.001 |  |  | 2.959 |
| 201 | 98.19 | 2.18 | 0.14 | <0.03 | 0.04 | 0.05 | <0.15 | 2.868 | 0.082 | 0.008 |  | 0.001 | 0.002 |  | 2.960 |
| 202 | 99.61 | 2.04 | 0.14 | <0.03 | 0.03 | 0.04 | <0.15 | 2.877 | 0.076 | 0.008 |  | 0.001 | 0.002 |  | 2.963 |
| 203 | 99.08 | 2.03 | 0.12 | <0.03 | <0.02 | <0.04 | <0.15 | 2.877 | 0.076 | 0.007 |  |  |  |  | 2.960 |
| 204 | 99.46 | 1.68 | 0.07 | 0.04 | <0.02 | 0.05 | <0.15 | 2.902 | 0.063 | 0.004 | 0.001 |  | 0.002 |  | 2.972 |
| 205 | 98.95 | 1.15 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.936 | 0.044 |  |  |  |  |  | 2.980 |
| 206 | 100.34 | 0.82 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.950 | 0.031 |  |  |  |  |  | 2.981 |
| 207 | 99.95 | 0.53 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.970 | 0.020 |  |  |  |  |  | 2.990 |
| 208 | 99.27 | 0.54 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.965 | 0.021 |  |  |  |  |  | 2.986 |
| 209 | 98.82 | 2.09 | 0.15 | <0.03 | 0.04 | <0.04 | <0.15 | 2.875 | 0.078 | 0.009 |  | 0.001 |  |  | 2.963 |
| 210 | 97.86 | 1.03 | 0.14 | <0.03 | <0.02 | <0.04 | <0.15 | 2.930 | 0.040 | 0.008 |  |  |  |  | 2.978 |
| 211 | 98.14 | 1.97 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.880 | 0.074 | 0.004 |  |  |  |  | 2.959 |
| 212 | 98.54 | 1.28 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.922 | 0.049 |  |  |  |  |  | 2.971 |
| 213 | 99.71 | 1.23 | <0.05 | <0.03 | 0.03 | 0.05 | <0.15 | 2.926 | 0.046 |  |  | 0.001 | 0.002 |  | 2.976 |
| 214 | 97.73 | 1.74 | 0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.896 | 0.066 | 0.003 |  | 0.001 |  |  | 2.966 |
| 215 | 98.54 | 1.53 | 0.12 | <0.03 | <0.02 | <0.04 | 0.16 | 2.902 | 0.058 | 0.007 |  |  |  | 0.005 | 2.971 |
| 216 | 99.25 | 1.07 | 0.07 | <0.03 | 0.03 | <0.04 | <0.15 | 2.933 | 0.041 | 0.004 |  | 0.001 |  |  | 2.978 |
| 217 | 97.59 | 1.93 | 0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.888 | 0.074 | 0.003 |  |  |  |  | 2.964 |
| 218 | 98.24 | 1.62 | 0.09 | <0.03 | 0.02 | <0.04 | <0.15 | 2.904 | 0.062 | 0.005 |  | 0.001 |  |  | 2.971 |
| 219 | 98.08 | 1.65 | 0.11 | <0.03 | <0.02 | <0.04 | <0.15 | 2.900 | 0.063 | 0.006 |  |  |  |  | 2.969 |
| 220 | 97.37 | 0.97 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.940 | 0.038 | 0.004 |  |  |  |  | 2.981 |
| 221 | 99.60 | 0.43 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.971 | 0.016 |  |  |  |  |  | 2.987 |
| 222 | 98.20 | 1.78 | 0.13 | <0.03 | <0.02 | 0.04 | <0.15 | 2.892 | 0.067 | 0.008 |  |  | 0.002 |  | 2.969 |
| 223 | 96.96 | 2.03 | 0.24 | <0.03 | <0.02 | <0.04 | <0.15 | 2.872 | 0.077 | 0.014 |  |  |  |  | 2.963 |
| 224 | 98.11 | 0.94 | 0.12 | <0.03 | 0.02 | <0.04 | <0.15 | 2.940 | 0.036 | 0.007 |  | 0.001 |  |  | 2.983 |
| 225 | 98.48 | 0.54 | 0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.964 | 0.021 | 0.003 |  | 0.001 |  |  | 2.988 |
| 226 | 98.92 | 0.39 | 0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.972 | 0.015 | 0.003 |  |  |  |  | 2.990 |
| 227 | 99.50 | 0.76 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.955 | 0.029 |  |  |  |  |  | 2.984 |
| 228 | 99.15 | 0.69 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.956 | 0.026 | 0.004 |  |  |  |  | 2.986 |
| 229 | 94.62 | 1.77 | 0.66 | <0.03 | <0.02 | <0.04 | 0.16 | 2.862 | 0.069 | 0.038 |  |  |  | 0.005 | 2.974 |
| 233 | 97.47 | 0.71 | 0.07 | <0.03 | 0.02 | <0.04 | <0.15 | 2.956 | 0.027 | 0.004 |  | 0.001 |  |  | 2.988 |
| 234 | 97.64 | 1.68 | 0.10 | <0.03 | <0.02 | <0.04 | <0.15 | 2.900 | 0.064 | 0.006 |  |  |  |  | 2.970 |
| 235 | 98.88 | 1.16 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.928 | 0.044 | 0.003 |  |  |  |  | 2.976 |
| 236 | 98.48 | 1.34 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.921 | 0.051 |  |  |  |  |  | 2.972 |
| 237 | 99.91 | 0.73 | 0.34 | <0.03 | <0.02 | <0.04 | <0.15 | 2.940 | 0.028 | 0.019 |  |  |  |  | 2.987 |
| 238 | 99.32 | 1.40 | 0.10 | <0.03 | <0.02 | <0.04 | <0.15 | 2.912 | 0.053 | 0.005 |  |  |  |  | 2.970 |
| 239 | 99.78 | 0.20 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.982 | 0.008 |  |  |  | 0.002 |  | 2.992 |
| 240 | 98.39 | 0.58 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.963 | 0.023 |  |  |  |  |  | 2.986 |
| 241 | 97.95 | 1.61 | <0.05 | <0.03 | 0.02 | <0.04 | 0.18 | 2.900 | 0.061 |  |  | 0.001 |  | 0.005 | 2.967 |
| BIF5 3-3A-d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 98.93 | 1.20 | 0.13 | 0.03 | 0.03 | 0.05 | 0.16 |  |  |  |  |  |  |  |  |
| 2SD | 1.88 | 1.36 | 0.19 | 0.01 | 0.02 | 0.01 | 0.02 |  |  |  |  |  |  |  |  |
| 2SE | 0.189 | 0.137 | 0.024 | 0.004 | 0.004 | 0.003 | 0.011 |  |  |  |  |  |  |  |  |
| Max | 100.89 | 2.44 | 0.66 | 0.04 | 0.07 | 0.06 | 0.18 |  |  |  |  |  |  |  |  |
| Min | 94.62 | 0.17 | 0.05 | 0.03 | 0.02 | 0.04 | 0.16 |  |  |  |  |  |  |  |  |
| N | 99 | 99 | 62 | 5 | 26 | 14 | 3 |  |  |  |  |  |  |  |  |
| N / Fe3O4 | - | 1.00 | 0.63 | 0.05 | 0.26 | 0.14 | 0.03 |  |  |  |  |  |  |  |  |
| BIF5 2-2Z-a |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 242 | 97.76 | 0.88 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.946 | 0.034 |  |  |  |  |  | 2.981 |
| 243 | 97.72 | 1.11 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.937 | 0.043 |  |  |  |  |  | 2.980 |
| 244 | 98.58 | 1.27 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.923 | 0.049 |  |  |  | 0.002 |  | 2.974 |
| 245 | 98.67 | 0.96 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.944 | 0.037 |  |  |  |  |  | 2.981 |
| 247 | 97.53 | 2.18 | 0.12 | 0.03 | <0.02 | <0.04 | <0.15 | 2.869 | 0.083 | 0.007 | 0.001 |  |  |  | 2.960 |
| 248 | 97.86 | 1.91 | 0.12 | <0.03 | <0.02 | <0.04 | <0.15 | 2.886 | 0.072 | 0.007 |  |  |  |  | 2.965 |
| 249 | 97.68 | 2.01 | 0.09 | <0.03 | <0.02 | <0.04 | <0.15 | 2.882 | 0.076 | 0.005 |  |  |  |  | 2.963 |
| 250 | 97.10 | 2.14 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.873 | 0.081 | 0.005 |  |  |  |  | 2.959 |
| 251 | 98.54 | 1.45 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.916 | 0.055 |  |  |  | 0.002 |  | 2.973 |
| 252 | 97.49 | 0.45 | 0.12 | <0.03 | <0.02 | <0.04 | <0.15 | 2.965 | 0.018 | 0.007 |  |  |  |  | 2.990 |
| 253 | 98.04 | 0.65 | 0.23 | <0.03 | <0.02 | <0.04 | <0.15 | 2.947 | 0.025 | 0.013 |  |  |  |  | 2.986 |
| 254 | 97.15 | 0.55 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.967 | 0.022 |  |  |  |  |  | 2.989 |
| 255 | 99.64 | 0.34 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.977 | 0.013 |  |  |  |  |  | 2.990 |
| 256 | 99.12 | 0.89 | <0.05 | <0.03 | <0.02 | 0.05 | <0.15 | 2.947 | 0.034 |  |  |  | 0.002 |  | 2.983 |
| 260 | 99.06 | 1.08 | <0.05 | 0.04 | <0.02 | <0.04 | <0.15 | 2.936 | 0.041 |  | 0.001 |  |  |  | 2.978 |
| 261 | 98.42 | 1.72 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.901 | 0.065 |  |  |  |  |  | 2.966 |
| 262 | 98.21 | 0.69 | 0.13 | <0.03 | 0.02 | <0.04 | <0.15 | 2.957 | 0.027 | 0.007 |  | 0.001 |  |  | 2.991 |
| 263 | 97.03 | 0.88 | 0.10 | <0.03 | <0.02 | <0.04 | <0.15 | 2.947 | 0.034 | 0.006 |  |  |  |  | 2.987 |
| 264 | 98.05 | 0.36 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.974 | 0.014 | 0.003 |  |  |  |  | 2.991 |
| 265 | 97.44 | 0.58 | 0.11 | <0.03 | <0.02 | <0.04 | <0.15 | 2.960 | 0.023 | 0.007 |  |  |  |  | 2.989 |
| 266 | 98.92 | 0.55 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.966 | 0.021 |  |  |  |  |  | 2.987 |
| 267 | 99.02 | 0.67 | 0.07 | <0.03 | <0.02 | 0.04 | <0.15 | 2.957 | 0.026 | 0.004 |  |  | 0.002 |  | 2.989 |
| 268 | 98.28 | 0.47 | 0.12 | <0.03 | <0.02 | <0.04 | <0.15 | 2.967 | 0.018 | 0.007 |  |  |  |  | 2.992 |
| 269 | 98.38 | 0.90 | 0.08 | <0.03 | 0.02 | 0.05 | <0.15 | 2.942 | 0.035 | 0.005 |  | 0.001 | 0.002 |  | 2.984 |
| 270 | 97.96 | 1.06 | 0.16 | <0.03 | <0.02 | 0.04 | <0.15 | 2.928 | 0.041 | 0.009 |  |  | 0.002 |  | 2.980 |
| 271 | 98.08 | 0.48 | <0.05 | <0.03 | 0.04 | <0.04 | <0.15 | 2.967 | 0.019 |  |  | 0.001 |  |  | 2.987 |
| 273 | 100.09 | 0.75 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.960 | 0.029 |  |  |  |  |  | 2.988 |
| 274 | 98.64 | 0.65 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.959 | 0.025 |  |  |  |  |  | 2.984 |
| 275 | 98.73 | 0.94 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.943 | 0.036 |  |  |  |  |  | 2.979 |
| 276 | 99.23 | 0.62 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.962 | 0.024 |  |  |  | 0.002 |  | 2.988 |
| 277 | 98.28 | 1.97 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.886 | 0.074 | 0.004 |  |  |  |  | 2.963 |
| 278 | 98.28 | 1.12 | 0.30 | <0.03 | 0.02 | <0.04 | <0.15 | 2.920 | 0.043 | 0.017 |  | 0.001 |  |  | 2.981 |
| 283 | 98.38 | 1.35 | 0.06 | <0.03 | <0.02 | <0.04 | 0.19 | 2.916 | 0.051 | 0.004 |  |  |  | 0.005 | 2.977 |
| 284 | 97.81 | 0.91 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.942 | 0.035 |  |  |  |  |  | 2.977 |
| 285 | 97.95 | 1.14 | 0.05 | <0.03 | <0.02 | 0.05 | <0.15 | 2.926 | 0.044 | 0.003 |  |  | 0.002 |  | 2.976 |
| 286 | 98.08 | 1.20 | <0.05 | <0.03 | <0.02 | 0.05 | <0.15 | 2.929 | 0.046 |  |  |  | 0.002 |  | 2.977 |
| 288 | 98.56 | 0.91 | 0.36 | <0.03 | <0.02 | <0.04 | <0.15 | 2.928 | 0.035 | 0.020 |  |  |  |  | 2.983 |
| 289 | 97.83 | 1.00 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.942 | 0.039 |  |  |  |  |  | 2.981 |
| 290 | 97.73 | 1.68 | 0.11 | <0.03 | 0.03 | <0.04 | <0.15 | 2.902 | 0.064 | 0.006 |  | 0.001 |  |  | 2.973 |
| 291 | 98.57 | 0.51 | 0.33 | <0.03 | <0.02 | <0.04 | <0.15 | 2.957 | 0.020 | 0.019 |  |  |  |  | 2.996 |
| 292 | 98.61 | 0.85 | <0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.947 | 0.033 |  |  | 0.001 |  |  | 2.980 |
| 293 | 98.99 | 0.85 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.949 | 0.033 | 0.004 |  |  |  |  | 2.986 |
| 294 | 98.24 | 2.02 | 0.12 | <0.03 | 0.03 | <0.04 | <0.15 | 2.878 | 0.076 | 0.007 |  | 0.001 |  |  | 2.962 |
| 295 | 98.42 | 1.36 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.919 | 0.052 |  |  |  |  |  | 2.971 |
| 296 | 98.70 | 0.52 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.970 | 0.020 |  |  |  |  |  | 2.990 |
| 303 | 96.72 | 0.67 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.959 | 0.026 | 0.004 |  |  |  |  | 2.989 |
| 304 | 96.38 | 1.48 | 0.32 | <0.03 | <0.02 | 0.10 | <0.15 | 2.895 | 0.057 | 0.019 |  |  | 0.005 |  | 2.976 |
| 306 | 98.03 | 0.83 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.947 | 0.032 |  |  |  |  |  | 2.980 |
| 307 | 98.68 | 0.30 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.977 | 0.011 | 0.004 |  |  |  |  | 2.992 |
| 308 | 98.79 | 0.29 | <0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.978 | 0.011 |  |  | 0.001 |  |  | 2.990 |
| 309 | 98.14 | 0.38 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.974 | 0.015 |  |  |  |  |  | 2.989 |
| 310 | 97.80 | 1.40 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.918 | 0.054 |  |  |  |  |  | 2.971 |
| 312 | 98.92 | 0.35 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.979 | 0.014 |  |  |  |  |  | 2.992 |
| 313 | 98.82 | 0.84 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.947 | 0.032 |  |  |  |  |  | 2.979 |
| 314 | 99.18 | 1.37 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.917 | 0.052 |  |  |  |  |  | 2.969 |
| 315 | 98.49 | 2.02 | 0.11 | <0.03 | <0.02 | <0.04 | <0.15 | 2.883 | 0.076 | 0.006 |  |  |  |  | 2.965 |
| 316 | 97.83 | 2.02 | 0.15 | <0.03 | <0.02 | <0.04 | <0.15 | 2.877 | 0.076 | 0.009 |  |  |  |  | 2.962 |
| 317 | 98.66 | 1.82 | 0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.894 | 0.068 | 0.003 |  | 0.001 |  |  | 2.965 |
| 318 | 97.72 | 1.93 | 0.11 | <0.03 | <0.02 | 0.04 | <0.15 | 2.881 | 0.073 | 0.006 |  |  | 0.002 |  | 2.962 |
| 319 | 98.91 | 1.74 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.896 | 0.066 |  |  |  | 0.002 |  | 2.964 |
| 320 | 98.69 | 1.72 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.899 | 0.065 | 0.003 |  |  |  |  | 2.967 |
| 321 | 98.49 | 1.11 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.933 | 0.042 |  |  |  |  |  | 2.976 |
| 322 | 98.66 | 0.61 | 0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.960 | 0.023 | 0.003 |  | 0.001 |  |  | 2.987 |
| 323 | 98.67 | 0.79 | 0.18 | 0.04 | 0.02 | <0.04 | <0.15 | 2.945 | 0.030 | 0.010 | 0.001 | 0.001 |  |  | 2.987 |
| 324 | 98.52 | 0.75 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.952 | 0.029 |  |  |  |  |  | 2.981 |
| 325 | 98.42 | 0.56 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.963 | 0.021 |  |  |  |  |  | 2.984 |
| 326 | 98.28 | 0.74 | <0.05 | <0.03 | 0.02 | <0.04 | 0.18 | 2.951 | 0.028 |  |  | 0.001 |  | 0.005 | 2.985 |
| 327 | 99.28 | 0.05 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.994 | 0.002 |  |  |  |  |  | 2.996 |
| 328 | 97.62 | 1.63 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.900 | 0.062 | 0.004 |  |  |  |  | 2.966 |
| 330 | 98.83 | 1.27 | 0.06 | 0.03 | <0.02 | <0.04 | <0.15 | 2.925 | 0.048 | 0.004 | 0.001 |  |  |  | 2.978 |
| 331 | 99.06 | 0.62 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.962 | 0.024 |  |  |  |  |  | 2.986 |
| 332 | 96.92 | 0.85 | 0.09 | 0.03 | <0.02 | <0.04 | <0.15 | 2.942 | 0.033 | 0.005 | 0.001 |  |  |  | 2.982 |
| 333 | 99.76 | 0.52 | <0.05 | <0.03 | <0.02 | <0.04 | 0.18 | 2.963 | 0.020 |  |  |  |  | 0.005 | 2.988 |
| 334 | 98.22 | 2.03 | 0.16 | <0.03 | 0.02 | <0.04 | <0.15 | 2.875 | 0.076 | 0.009 |  | 0.001 |  |  | 2.961 |
| 335 | 98.35 | 1.95 | 0.11 | <0.03 | 0.03 | <0.04 | <0.15 | 2.881 | 0.073 | 0.006 |  | 0.001 |  |  | 2.961 |
| 337 | 99.12 | 1.37 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.916 | 0.052 | 0.004 |  |  |  |  | 2.972 |
| 338 | 99.20 | 0.77 | <0.05 | <0.03 | 0.02 | <0.04 | 0.15 | 2.949 | 0.030 |  |  | 0.001 |  | 0.004 | 2.983 |
| 339 | 99.03 | 0.80 | <0.05 | <0.03 | 0.04 | <0.04 | <0.15 | 2.952 | 0.031 |  |  | 0.001 |  |  | 2.984 |
| 340 | 97.51 | 1.97 | 0.17 | <0.03 | <0.02 | <0.04 | <0.15 | 2.878 | 0.075 | 0.009 |  |  |  |  | 2.962 |
| 341 | 98.37 | 1.70 | 0.13 | <0.03 | <0.02 | <0.04 | <0.15 | 2.899 | 0.064 | 0.007 |  |  |  |  | 2.971 |
| 342 | 97.90 | 1.87 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.890 | 0.071 | 0.004 |  |  |  |  | 2.964 |
| 343 | 99.12 | 1.08 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.936 | 0.041 |  |  |  |  |  | 2.977 |
| 344 | 98.75 | 0.55 | 0.14 | <0.03 | 0.03 | <0.04 | <0.15 | 2.959 | 0.021 | 0.008 |  | 0.001 |  |  | 2.989 |
| 345 | 98.66 | 1.78 | 0.12 | <0.03 | <0.02 | <0.04 | <0.15 | 2.895 | 0.067 | 0.007 |  |  |  |  | 2.969 |
| 346 | 100.06 | 0.64 | <0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.961 | 0.024 |  |  | 0.001 |  |  | 2.986 |
| 347 | 99.34 | 0.74 | 0.05 | <0.03 | 0.03 | 0.05 | <0.15 | 2.951 | 0.028 | 0.003 |  | 0.001 | 0.002 |  | 2.985 |
| 348 | 98.53 | 1.07 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.935 | 0.041 |  |  |  |  |  | 2.976 |
| 352 | 97.02 | 2.10 | 0.24 | <0.03 | <0.02 | <0.04 | <0.15 | 2.869 | 0.080 | 0.014 |  |  |  |  | 2.962 |
| 353 | 97.47 | 1.32 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.921 | 0.051 | 0.005 |  |  |  |  | 2.976 |
| 354 | 97.77 | 0.76 | 0.05 | 0.04 | <0.02 | <0.04 | <0.15 | 2.954 | 0.029 | 0.003 | 0.001 |  |  |  | 2.988 |
| 355 | 99.39 | 0.80 | 0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.952 | 0.031 | 0.003 |  | 0.001 |  |  | 2.986 |
| 356 | 96.57 | 0.91 | 0.45 | <0.03 | <0.02 | <0.04 | <0.15 | 2.926 | 0.035 | 0.026 |  |  |  |  | 2.988 |
| 357 | 99.26 | 1.45 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.910 | 0.054 | 0.005 |  |  |  |  | 2.969 |
| 358 | 96.64 | 1.98 | 0.08 | <0.03 | 0.03 | <0.04 | <0.15 | 2.879 | 0.076 | 0.005 |  | 0.001 |  |  | 2.960 |
| 359 | 99.03 | 0.65 | 0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.960 | 0.025 | 0.003 |  |  |  |  | 2.988 |
| 360 | 99.01 | 0.32 | 0.08 | <0.03 | <0.02 | <0.04 | <0.15 | 2.979 | 0.012 | 0.004 |  |  |  |  | 2.996 |
| 361 | 99.79 | 0.41 | 0.06 | <0.03 | <0.02 | 0.05 | <0.15 | 2.971 | 0.016 | 0.004 |  |  | 0.002 |  | 2.993 |
| 362 | 98.12 | 0.35 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.977 | 0.014 |  |  |  |  |  | 2.991 |
| 363 | 98.01 | 1.42 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.915 | 0.054 |  |  |  |  |  | 2.970 |
| 370 | 99.01 | 1.15 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.935 | 0.044 |  |  |  |  |  | 2.979 |
| 371 | 99.64 | 0.45 | 0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.973 | 0.017 | 0.003 |  |  |  |  | 2.993 |
| 372 | 98.93 | 0.33 | 0.19 | <0.03 | <0.02 | <0.04 | <0.15 | 2.968 | 0.013 | 0.011 |  |  |  |  | 2.991 |
| 373 | 99.18 | 0.25 | 0.10 | <0.03 | <0.02 | <0.04 | <0.15 | 2.979 | 0.010 | 0.006 |  |  |  |  | 2.994 |
| 374 | 99.04 | 0.77 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.950 | 0.030 | 0.004 |  |  |  |  | 2.984 |
| 375 | 98.78 | 0.75 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.954 | 0.029 | 0.004 |  |  |  |  | 2.986 |
| 376 | 98.60 | 1.08 | 0.14 | <0.03 | <0.02 | <0.04 | <0.15 | 2.931 | 0.041 | 0.008 |  |  |  |  | 2.980 |
| 377 | 97.87 | 1.00 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.943 | 0.039 |  |  |  |  |  | 2.982 |
| 378 | 97.68 | 1.88 | 0.10 | <0.03 | 0.03 | <0.04 | <0.15 | 2.885 | 0.071 | 0.006 |  | 0.001 |  |  | 2.963 |
| 379 | 98.30 | 1.51 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.913 | 0.058 |  |  |  |  |  | 2.971 |
| 380 | 98.60 | 0.75 | 0.18 | <0.03 | <0.02 | <0.04 | <0.15 | 2.944 | 0.029 | 0.010 |  |  |  |  | 2.983 |
| BIF5 2-2Z-a |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 98.39 | 1.05 | 0.12 | 0.03 | 0.03 | 0.05 | 0.18 |  |  |  |  |  |  |  |  |
| 2SD | 1.49 | 1.10 | 0.17 | <0.01 | 0.01 | 0.03 | 0.04 |  |  |  |  |  |  |  |  |
| 2SE | 0.142 | 0.105 | 0.021 | 0.001 | 0.002 | 0.008 | 0.018 |  |  |  |  |  |  |  |  |
| Max | 100.09 | 2.18 | 0.45 | 0.04 | 0.04 | 0.10 | 0.19 |  |  |  |  |  |  |  |  |
| Min | 96.38 | 0.05 | 0.05 | 0.03 | 0.02 | 0.04 | 0.15 |  |  |  |  |  |  |  |  |
| N | 110 | 110 | 63 | 6 | 22 | 14 | 4 |  |  |  |  |  |  |  |  |
| N / Fe3O4 | - | 1.00 | 0.57 | 0.05 | 0.20 | 0.13 | 0.04 |  |  |  |  |  |  |  |  |
| BIF5 2-2C-b |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 383 | 100.02 | 1.02 | <0.05 | <0.03 | <0.02 | 0.05 | <0.15 | 2.937 | 0.038 |  |  |  |  |  | 2.975 |
| 384 | 98.78 | 1.32 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.920 | 0.050 | 0.003 |  |  |  |  | 2.973 |
| 385 | 98.43 | 1.37 | <0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.920 | 0.052 |  |  | 0.001 |  |  | 2.972 |
| 386 | 99.57 | 0.71 | <0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.957 | 0.027 |  |  | 0.001 |  |  | 2.984 |
| 387 | 100.21 | 1.45 | <0.05 | 0.04 | 0.03 | <0.04 | <0.15 | 2.918 | 0.054 |  | 0.001 | 0.001 |  |  | 2.974 |
| 388 | 99.90 | 1.00 | <0.05 | <0.03 | <0.02 | <0.04 | 0.19 | 2.937 | 0.038 |  |  |  |  | 0.005 | 2.979 |
| 389 | 100.37 | 0.84 | <0.05 | 0.04 | <0.02 | <0.04 | 0.21 | 2.946 | 0.032 |  | 0.001 |  |  | 0.006 | 2.985 |
| 390 | 100.02 | 0.61 | <0.05 | 0.04 | 0.02 | <0.04 | <0.15 | 2.960 | 0.023 |  | 0.001 | 0.001 |  |  | 2.985 |
| 391 | 99.73 | 0.48 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.969 | 0.018 |  |  |  |  |  | 2.988 |
| 393 | 99.42 | 1.18 | 0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.932 | 0.045 | 0.003 |  |  |  |  | 2.979 |
| 394 | 98.86 | 1.90 | <0.05 | <0.03 | 0.02 | 0.07 | 0.17 | 2.884 | 0.071 |  |  | 0.001 | 0.003 | 0.005 | 2.964 |
| 395 | 98.48 | 1.45 | <0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.912 | 0.055 |  |  | 0.001 |  |  | 2.967 |
| 396 | 99.18 | 1.83 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.892 | 0.069 | 0.004 |  |  |  |  | 2.964 |
| 397 | 98.53 | 1.72 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.901 | 0.065 |  |  |  |  |  | 2.966 |
| 398 | 98.61 | 0.84 | <0.05 | <0.03 | <0.02 | 0.04 | <0.15 | 2.949 | 0.032 |  |  |  | 0.002 |  | 2.983 |
| 403 | 99.61 | 0.76 | <0.05 | 0.05 | <0.02 | 0.04 | <0.15 | 2.951 | 0.029 |  | 0.002 |  | 0.002 |  | 2.983 |
| 404 | 99.44 | 0.86 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.950 | 0.033 |  |  |  |  |  | 2.983 |
| 405 | 99.28 | 1.35 | 0.06 | <0.03 | <0.02 | <0.04 | <0.15 | 2.919 | 0.051 | 0.003 |  |  |  |  | 2.973 |
| 406 | 97.96 | 1.60 | 0.07 | <0.03 | <0.02 | <0.04 | <0.15 | 2.905 | 0.061 | 0.004 |  |  |  |  | 2.969 |
| 407 | 98.82 | 0.81 | 0.11 | 0.03 | 0.05 | 0.05 | <0.15 | 2.944 | 0.031 | 0.006 | 0.001 | 0.001 | 0.002 |  | 2.986 |
| 408 | 98.65 | 0.90 | 0.09 | 0.05 | <0.02 | <0.04 | <0.15 | 2.940 | 0.035 | 0.005 | 0.002 |  |  |  | 2.981 |
| 409 | 98.81 | 1.32 | <0.05 | 0.04 | 0.04 | <0.04 | <0.15 | 2.920 | 0.050 |  | 0.001 | 0.001 |  |  | 2.972 |
| 410 | 99.54 | 0.95 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.950 | 0.036 |  |  |  |  |  | 2.986 |
| 411 | 99.70 | 1.48 | <0.05 | <0.03 | 0.02 | <0.04 | <0.15 | 2.916 | 0.056 |  |  | 0.001 |  |  | 2.972 |
| 412 | 98.45 | 1.33 | <0.05 | <0.03 | 0.03 | <0.04 | <0.15 | 2.923 | 0.051 |  |  | 0.001 |  |  | 2.974 |
| 415 | 98.31 | 1.54 | 0.10 | <0.03 | 0.02 | <0.04 | 0.17 | 2.904 | 0.058 | 0.006 |  | 0.001 |  | 0.005 | 2.973 |
| 416 | 98.76 | 1.31 | <0.05 | <0.03 | <0.02 | <0.04 | <0.15 | 2.922 | 0.050 |  |  |  |  |  | 2.971 |
| 417 | 100.11 | 0.70 | <0.05 | 0.03 | 0.03 | <0.04 | <0.15 | 2.958 | 0.026 |  | 0.001 | 0.001 |  |  | 2.986 |
| 418 | 98.76 | 1.46 | 0.06 | <0.03 | <0.02 | <0.04 | 0.17 | 2.911 | 0.055 | 0.003 |  |  |  | 0.005 | 2.974 |
| BIF5 2-2C-b |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 99.18 | 1.18 | 0.07 | 0.04 | 0.03 | 0.05 | 0.18 |  |  |  |  |  |  |  |  |
| 2SD | 1.32 | 0.77 | 0.04 | 0.01 | 0.02 | 0.02 | 0.03 |  |  |  |  |  |  |  |  |
| 2SE | 0.245 | 0.142 | 0.013 | 0.005 | 0.004 | 0.011 | 0.014 |  |  |  |  |  |  |  |  |
| Max | 100.37 | 1.90 | 0.11 | 0.05 | 0.05 | 0.07 | 0.21 |  |  |  |  |  |  |  |  |
| Min | 97.96 | 0.48 | 0.05 | 0.03 | 0.02 | 0.04 | 0.17 |  |  |  |  |  |  |  |  |
| N | 29 | 29 | 9 | 8 | 12 | 4 | 5 |  |  |  |  |  |  |  |  |
| N / Fe3O4 | - | 1.00 | 0.31 | 0.28 | 0.41 | 0.14 | 0.17 |  |  |  |  |  |  |  |  |
| BIF5 Total |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 98.71 | 1.13 | 0.12 | 0.04 | 0.03 | 0.05 | 0.18 |  |  |  |  |  |  |  |  |
| 2SD | 1.75 | 1.19 | 0.17 | 0.01 | 0.02 | 0.02 | 0.03 |  |  |  |  |  |  |  |  |
| 2SE | 0.113 | 0.077 | 0.015 | 0.003 | 0.002 | 0.004 | 0.009 |  |  |  |  |  |  |  |  |
| Max | 100.89 | 2.44 | 0.66 | 0.05 | 0.07 | 0.10 | 0.21 |  |  |  |  |  |  |  |  |
| Min | 94.62 | 0.05 | 0.05 | 0.03 | 0.02 | 0.04 | 0.15 |  |  |  |  |  |  |  |  |
| N | 238 | 238 | 134 | 19 | 60 | 32 | 12 |  |  |  |  |  |  |  |  |
| N / Fe3O4 | - | 1.00 | 0.56 | 0.08 | 0.25 | 0.13 | 0.05 |  |  |  |  |  |  |  |  |
| Session 2: May 2010 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| BIF12 9-12 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 128 | 99.48 | 0.76 | <0.05 | nd | nd | nd | nd | 2.956 | 0.029 |  |  |  |  |  | 2.985 |
| 129 | 99.39 | 0.81 | <0.05 | nd | nd | nd | nd | 2.954 | 0.031 |  |  |  |  |  | 2.985 |
| 130 | 99.27 | 1.01 | <0.05 | nd | nd | nd | nd | 2.942 | 0.038 |  |  |  |  |  | 2.981 |
| 131 | 99.05 | 1.26 | <0.05 | nd | nd | nd | nd | 2.928 | 0.048 |  |  |  |  |  | 2.976 |
| 132 | 98.96 | 1.60 | 0.08 | nd | nd | nd | nd | 2.906 | 0.060 | 0.004 |  |  |  |  | 2.971 |
| 133 | 98.29 | 1.48 | 0.07 | nd | nd | nd | nd | 2.912 | 0.056 | 0.004 |  |  |  |  | 2.973 |
| 134 | 98.67 | 1.30 | 0.06 | nd | nd | nd | nd | 2.923 | 0.050 | 0.003 |  |  |  |  | 2.976 |
| 135 | 98.30 | 1.72 | 0.13 | nd | nd | nd | nd | 2.897 | 0.065 | 0.007 |  |  |  |  | 2.969 |
| 136 | 98.34 | 1.57 | 0.05 | nd | nd | nd | nd | 2.908 | 0.060 | 0.003 |  |  |  |  | 2.971 |
| 137 | 99.24 | 1.36 | <0.05 | nd | nd | nd | nd | 2.923 | 0.051 |  |  |  |  |  | 2.974 |
| 138 | 99.29 | 1.52 | 0.05 | nd | nd | nd | nd | 2.912 | 0.057 | 0.003 |  |  |  |  | 2.972 |
| 139 | 99.10 | 1.79 | 0.10 | nd | nd | nd | nd | 2.895 | 0.067 | 0.005 |  |  |  |  | 2.968 |
| 140 | 98.03 | 1.80 | 0.05 | nd | nd | nd | nd | 2.895 | 0.068 | 0.003 |  |  |  |  | 2.967 |
| 141 | 99.95 | 0.72 | <0.05 | nd | nd | nd | nd | 2.959 | 0.027 |  |  |  |  |  | 2.986 |
| 142 | 98.48 | 0.82 | 0.15 | nd | nd | nd | nd | 2.946 | 0.032 | 0.008 |  |  |  |  | 2.986 |
| 143 | 98.70 | 1.60 | 0.11 | nd | nd | nd | nd | 2.905 | 0.061 | 0.006 |  |  |  |  | 2.971 |
| 144 | 99.44 | 1.11 | 0.07 | nd | nd | nd | nd | 2.934 | 0.042 | 0.004 |  |  |  |  | 2.980 |
| 145 | 98.88 | 1.58 | <0.05 | nd | nd | nd | nd | 2.910 | 0.060 |  |  |  |  |  | 2.970 |
| 146 | 97.95 | 1.59 | <0.05 | nd | nd | nd | nd | 2.909 | 0.061 |  |  |  |  |  | 2.970 |
| 147 | 98.74 | 1.53 | <0.05 | nd | nd | nd | nd | 2.912 | 0.058 |  |  |  |  |  | 2.971 |
| 148 | 99.26 | 1.34 | <0.05 | nd | nd | nd | nd | 2.924 | 0.051 |  |  |  |  |  | 2.975 |
| 149 | 99.91 | 1.23 | 0.07 | nd | nd | nd | nd | 2.928 | 0.046 | 0.004 |  |  |  |  | 2.978 |
| 150 | 98.87 | 1.31 | <0.05 | nd | nd | nd | nd | 2.925 | 0.050 |  |  |  |  |  | 2.975 |
| 151 | 99.02 | 1.14 | <0.05 | nd | nd | nd | nd | 2.935 | 0.043 |  |  |  |  |  | 2.978 |
| 152 | 99.68 | 0.97 | <0.05 | nd | nd | nd | nd | 2.945 | 0.037 |  |  |  |  |  | 2.982 |
| BIF12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 98.97 | 1.32 | 0.08 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2SD | 1.09 | 0.66 | 0.06 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2SE | 0.218 | 0.131 | 0.019 |  |  |  |  |  |  |  |  |  |  |  |  |
| Max | 99.95 | 1.80 | 0.15 |  |  |  |  |  |  |  |  |  |  |  |  |
| Min | 97.95 | 0.72 | 0.05 |  |  |  |  |  |  |  |  |  |  |  |  |
| N | 25 | 25 | 12 |  |  |  |  |  |  |  |  |  |  |  |  |
| N / Fe3O4 |  | 1.00 | 0.48 |  |  |  |  |  |  |  |  |  |  |  |  |
| BIF14 22-3 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 98.45 | 1.27 | 0.06 | nd | nd | nd | nd | 2.924 | 0.049 | 0.004 |  |  |  |  | 2.977 |
| 155 | 98.61 | 1.59 | 0.08 | nd | nd | nd | nd | 2.906 | 0.060 | 0.005 |  |  |  |  | 2.971 |
| 156 | 98.63 | 1.82 | 0.10 | nd | nd | nd | nd | 2.893 | 0.068 | 0.005 |  |  |  |  | 2.967 |
| 157 | 97.72 | 1.83 | 0.08 | nd | nd | nd | nd | 2.892 | 0.069 | 0.004 |  |  |  |  | 2.966 |
| 158 | 98.55 | 1.13 | <0.05 | nd | nd | nd | nd | 2.934 | 0.043 |  |  |  |  |  | 2.977 |
| 159 | 98.71 | 0.48 | 0.10 | nd | nd | nd | nd | 2.968 | 0.018 | 0.006 |  |  |  |  | 2.992 |
| 160 | 98.75 | 0.62 | 0.10 | nd | nd | nd | nd | 2.960 | 0.024 | 0.006 |  |  |  |  | 2.990 |
| 161 | 99.21 | 0.65 | 0.09 | nd | nd | nd | nd | 2.959 | 0.025 | 0.005 |  |  |  |  | 2.989 |
| 162 | 98.78 | 0.57 | 0.06 | nd | nd | nd | nd | 2.965 | 0.022 | 0.003 |  |  |  |  | 2.990 |
| 163 | 98.65 | 0.96 | 0.12 | nd | nd | nd | nd | 2.940 | 0.037 | 0.007 |  |  |  |  | 2.983 |
| 164 | 98.09 | 0.74 | 0.16 | nd | nd | nd | nd | 2.950 | 0.029 | 0.009 |  |  |  |  | 2.988 |
| 165 | 99.58 | 0.59 | <0.05 | nd | nd | nd | nd | 2.966 | 0.023 |  |  |  |  |  | 2.989 |
| 166 | 97.66 | 2.03 | 0.08 | nd | nd | nd | nd | 2.881 | 0.077 | 0.005 |  |  |  |  | 2.963 |
| 167 | 97.90 | 1.67 | 0.08 | nd | nd | nd | nd | 2.901 | 0.064 | 0.005 |  |  |  |  | 2.969 |
| 168 | 97.40 | 1.76 | 0.06 | nd | nd | nd | nd | 2.897 | 0.067 | 0.003 |  |  |  |  | 2.967 |
| 169 | 98.05 | 1.74 | 0.15 | nd | nd | nd | nd | 2.895 | 0.066 | 0.008 |  |  |  |  | 2.969 |
| 171 | 98.02 | 1.34 | <0.05 | nd | nd | nd | nd | 2.923 | 0.051 |  |  |  |  |  | 2.974 |
| 172 | 98.17 | 1.52 | 0.08 | nd | nd | nd | nd | 2.910 | 0.058 | 0.005 |  |  |  |  | 2.972 |
| 173 | 98.89 | 1.50 | 0.08 | nd | nd | nd | nd | 2.911 | 0.057 | 0.005 |  |  |  |  | 2.973 |
| 174 | 97.73 | 1.49 | 0.07 | nd | nd | nd | nd | 2.911 | 0.057 | 0.004 |  |  |  |  | 2.972 |
| 175 | 97.84 | 1.91 | 0.11 | nd | nd | nd | nd | 2.887 | 0.073 | 0.006 |  |  |  |  | 2.965 |
| 176 | 95.65 | 2.96 | 0.37 | nd | nd | nd | nd | 2.817 | 0.112 | 0.021 |  |  |  |  | 2.949 |
| 177 | 99.76 | 0.22 | <0.05 | nd | nd | nd | nd | 2.987 | 0.009 |  |  |  |  |  | 2.996 |
| 178 | 98.94 | 0.67 | 0.12 | nd | nd | nd | nd | 2.956 | 0.026 | 0.007 |  |  |  |  | 2.989 |
| 180 | 99.96 | 0.24 | <0.05 | nd | nd | nd | nd | 2.986 | 0.009 |  |  |  |  |  | 2.995 |
| 181 | 97.13 | 2.09 | 0.12 | nd | nd | nd | nd | 2.876 | 0.079 | 0.007 |  |  |  |  | 2.962 |
| 182 | 99.14 | 1.81 | 0.12 | nd | nd | nd | nd | 2.893 | 0.068 | 0.007 |  |  |  |  | 2.968 |
| 183 | 98.21 | 1.66 | <0.05 | nd | nd | nd | nd | 2.904 | 0.063 |  |  |  |  |  | 2.967 |
| 184 | 98.92 | 1.52 | <0.05 | nd | nd | nd | nd | 2.914 | 0.058 |  |  |  |  |  | 2.971 |
| 185 | 98.74 | 1.28 | <0.05 | nd | nd | nd | nd | 2.927 | 0.049 |  |  |  |  |  | 2.976 |
| 186 | 98.88 | 0.80 | <0.05 | nd | nd | nd | nd | 2.954 | 0.031 |  |  |  |  |  | 2.985 |
| 187 | 97.51 | 1.27 | <0.05 | nd | nd | nd | nd | 2.927 | 0.049 |  |  |  |  |  | 2.976 |
| 188 | 97.72 | 0.87 | <0.05 | nd | nd | nd | nd | 2.949 | 0.034 |  |  |  |  |  | 2.983 |
| 189 | 98.27 | 0.92 | <0.05 | nd | nd | nd | nd | 2.945 | 0.035 |  |  |  |  |  | 2.983 |
| 190 | 97.85 | 1.45 | <0.05 | nd | nd | nd | nd | 2.916 | 0.056 |  |  |  |  |  | 2.972 |
| 191 | 98.77 | 1.18 | <0.05 | nd | nd | nd | nd | 2.932 | 0.045 |  |  |  |  |  | 2.977 |
| 192 | 98.05 | 1.55 | <0.05 | nd | nd | nd | nd | 2.911 | 0.059 |  |  |  |  |  | 2.970 |
| 193 | 98.38 | 1.63 | 0.07 | nd | nd | nd | nd | 2.904 | 0.062 | 0.004 |  |  |  |  | 2.970 |
| 194 | 98.42 | 1.41 | 0.06 | nd | nd | nd | nd | 2.917 | 0.053 | 0.003 |  |  |  |  | 2.974 |
| 195 | 98.23 | 1.94 | 0.07 | nd | nd | nd | nd | 2.887 | 0.073 | 0.004 |  |  |  |  | 2.964 |
| 196 | 97.13 | 1.82 | 0.06 | nd | nd | nd | nd | 2.893 | 0.070 | 0.003 |  |  |  |  | 2.966 |
| 197 | 97.60 | 1.98 | 0.11 | nd | nd | nd | nd | 2.883 | 0.075 | 0.006 |  |  |  |  | 2.964 |
| 198 | 99.23 | 0.23 | 0.06 | nd | nd | nd | nd | 2.984 | 0.009 | 0.003 |  |  |  |  | 2.996 |
| 199 | 98.61 | 0.29 | <0.05 | nd | nd | nd | nd | 2.983 | 0.011 |  |  |  |  |  | 2.994 |
| 200 | 98.12 | 0.44 | 0.10 | nd | nd | nd | nd | 2.970 | 0.017 | 0.006 |  |  |  |  | 2.993 |
| 201 | 99.24 | 0.25 | 0.07 | nd | nd | nd | nd | 2.982 | 0.010 | 0.004 |  |  |  |  | 2.996 |
| 202 | 99.30 | 0.26 | 0.06 | nd | nd | nd | nd | 2.982 | 0.010 | 0.003 |  |  |  |  | 2.996 |
| 203 | 99.18 | 0.21 | <0.05 | nd | nd | nd | nd | 2.988 | 0.008 |  |  |  |  |  | 2.996 |
| 204 | 99.11 | 0.29 | <0.05 | nd | nd | nd | nd | 2.983 | 0.011 |  |  |  |  |  | 2.994 |
| 205 | 99.40 | 0.15 | <0.05 | nd | nd | nd | nd | 2.991 | 0.006 |  |  |  |  |  | 2.997 |
| 206 | 99.57 | 0.21 | <0.05 | nd | nd | nd | nd | 2.988 | 0.008 |  |  |  |  |  | 2.996 |
| 207 | 99.58 | 0.24 | 0.08 | nd | nd | nd | nd | 2.983 | 0.009 | 0.005 |  |  |  |  | 2.997 |
| 208 | 98.69 | 0.38 | 0.12 | nd | nd | nd | nd | 2.973 | 0.015 | 0.007 |  |  |  |  | 2.994 |
| BIF14 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 98.47 | 1.12 | 0.10 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2SD | 1.58 | 1.35 | 0.11 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2SE | 0.217 | 0.186 | 0.019 |  |  |  |  |  |  |  |  |  |  |  |  |
| Max | 99.96 | 2.96 | 0.37 |  |  |  |  |  |  |  |  |  |  |  |  |
| Min | 95.65 | 0.15 | 0.06 |  |  |  |  |  |  |  |  |  |  |  |  |
| N | 53 | 53 | 33 |  |  |  |  |  |  |  |  |  |  |  |  |
| N / Fe3O4 |  | 1.00 | 0.62 |  |  |  |  |  |  |  |  |  |  |  |  |
| All BIFs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Avg | 98.69 | 1.14 | 0.11 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2SD | 1.69 | 1.19 | 0.16 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2SE | 0.10 | 0.07 | 0.01 |  |  |  |  |  |  |  |  |  |  |  |  |
| Max | 100.89 | 2.96 | 0.66 |  |  |  |  |  |  |  |  |  |  |  |  |
| Min | 94.62 | 0.05 | 0.05 |  |  |  |  |  |  |  |  |  |  |  |  |
| N | 316 | 316 | 179 |  |  |  |  |  |  |  |  |  |  |  |  |
| N / Fe3O4 |  | 1.00 | 0.57 |  |  |  |  |  |  |  |  |  |  |  |  |

# Notes:

nd = not detected.

# Atoms per formula unit (ideal=3) per 4 oxygens.

# Data are normalized to 4 oxygens.

# Oxygen was not analyzed.