Appendix A

Supplemental Information for paper titled Synthesis and characterization of the Mars-relevant phosphate minerals Fe- and Mg-whitlockite and merrillite and a possible mechanism that maintains charge balance during whitlockite to merrillite transformation. Christopher T. Adcock*, Elisabeth M. Hausrath,  Paul M. Forster, Oliver Tschauner, and Kirellos J. Sefein.

Effects of parameter variation during whitlockite synthesis.

In order to synthesize Mg-whitlockite, the Hughes et al. (2008) experiment was replicated, but Mg2+ was intentionally supplied to the system in the form of magnesium nitrate hexahydrate (Mg(NO3)2·6H2O) (J. T. Baker, ACS grade).  To simplify the method, 40 mesh reagent grade calcium hydroxyapatite (HAP) powder (Spectrum, reagent grade) was used rather than pre-synthesizing this phase.  The ratio of HAP to magnesium nitrate hexahydrate by mass was generally 3.33: 1 to provide sufficient Mg2+ based on whitlockite stoichiometry, but not excess Mg2+ that might lead to the formation of additional Mg phases.  Variables during the preliminary experiments included incubation time at 240 °C (5-14 days), adjusted pH (2.1 to 2.8), and the total concentration of solids used in the experiments (6.7 to 90 g/L).  Early experiments were run in 23 ml Teflon lined acid digestion vessels (Parr 4749) and later scaled up to 125 ml vessels (Parr 4748).  Preliminary experiments were carried out with the goal of first producing Mg-whitlockite crystals, and then refining the synthesis method for phase purity, larger crystal size, and sufficient output mass to carry out crystallographic and chemical characterization as well as supply Mg-whitlockite for use in the synthesis of Mg-merrillite.

Insight gained during synthesis of Mg-whitlockite was used to develop a procedure for Fe-whitlockite synthesis.  Initially, FeCl2 was used as a source of Fe2+ in place of the Mg(NO3)2·6H2O used in Mg-whitlockite synthesis.  After experiments using FeCl2 failed to produce significant whitlockite, Fe(II)S was utilized as the Fe2+ source and whitlockite crystals were produced along with hydroxyapatite and opaque phases (presumably Fe phases).  Variables during the preliminary experiments included incubation time at 240 °C (5-9 days), and total concentration of solids (9.0 to 17.8 g/L).  In addition, the production of iron sulfide phases prompted varying the ratio of HAP to Fe(II)S from 9.6:1 (near stoichiometric ideal) to 28.6:1 by mass to limit their formation.  The pH value was not significantly varied from 2.8 as results from Mg-whitlockite synthesis indicated it had no effect.

Although endmember whitlockite and merrillite are useful for different studies, natural whitlockite and merrillite generally contain both Mg2+ and Fe2+.  We therefore applied the results of endmember synthesis experiments to synthesize non-endmember whitlockites and from them mixed Fe/Mg-merrillite.  Variables included the ratio of Mg and Fe, as well as the concentration of total solids in solution (10.2 to 17.8 g/L).  Sodium (as NaCl) was also included in some experiments.  Though sodium is not typical within terrestrial whitlockite, it is present in most natural merrillite, particularly martian merrillite, in what is a partially filled calcium site in synthetic merrillite (Jolliff et al., 2006).  The methods documented in the accompanying paper are those which successfully produced the material characterized and used for mixed Fe/Mg-merrillite synthesis in this study and include sodium (as NaCl), however, sodium was not incorporated into the whitlockite structure in any of multiple attempts.   Additional experiments showed sodium to neither inhibit nor aid the production of mixed Mg/Fe-whitlockite.  Deposited Table A1 contains parameter values for all whitlockite synthesis experiments in this study, including those used to make mixed Fe/Mg-whitlockite and subsequent Fe/Mg-merrillite.

Table A1.  Batch parameters for whitlockite synthesis experiments.  For paper titled Synthesis and characterization of the Mars-relevant phosphate minerals Fe- and Mg-whitlockite and merrillite and a possible mechanism that maintains charge balance during whitlockite to merrillite transformation. Christopher T. Adcock*, Elisabeth M. Hausrath,  Paul M. Forster, Oliver Tschauner and Kirellos J. Sefein.

|  | Vessel | MgNO3·6H2O | FeCl2 | FeS | NaCl | HAP | Mass | DI |  | pH |  | pH | Mass |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ID | Size | (g) | (g) | (g) | (g) | (g) | Tot (g) | (mL) | g/L* | start | Days | end | Out (g) |  | Note |
| Mg-1 | 23 ml | 0.0153 |  |  |  | 0.0518 | 0.0671 | 10 | 6.7 | 2.70 | 5 | - | - | Whit. |  |
| Mg-2 | 23 ml | 0.2210 |  |  |  | 0.7716 | 0.9926 | 11 | 90.2 | 2.78 | 5 | - | - | Monetite |  |
| Mg-3 | 23 ml | 0.0159 |  |  |  | 0.0519 | 0.0678 | 10 | 6.8 | 2.66 | 10 | 2.80 | 0.016 | Whit. |  |
| Mg-4 | 23 ml | 0.0461 |  |  |  | 0.1541 | 0.2002 | 10 | 20.0 | 2.69 | 11 | 2.80 | 0.113 | Whit. |  |
| Mg-5 | 23 ml | 0.1093 |  |  |  | 0.3630 | 0.4723 | 13.5 | 35.0 | 2.81 | 14 | 2.16 | 0.189 | Monetite |  |
| Mg-6 | 23 ml | 0.2190 |  |  |  | 0.7280 | 0.9470 | 13.5 | 70.1 | 2.80 | 14 | 1.92 | 0.607 | Monetite |  |
| Mg-7 | 125 ml | 0.4599 |  |  |  | 1.5432 | 2.0031 | 90 | 22.3 | 2.80 | 7 | 2.09 | 1.150 | Monetite |  |
| Mg-8 | 125 ml | 0.4588 |  |  |  | 1.5423 | 2.0011 | 90 | 22.2 | 2.78 | 6 | 1.85 | 1.320 | Monetite |  |
| Mg-9 | 125 ml | 0.4595 |  |  |  | 1.5452 | 2.0047 | 90 | 22.3 | 2.80 | 5 | 1.86 | 1.370 | Monetite |  |
| Mg-10 | 125 ml | 0.4601 |  |  |  | 1.5426 | 2.0027 | 90 | 22.3 | 2.77 | 5 | 1.85 | 1.300 | Monetite |  |
| Mg-11 | 125 ml | 0.4595 |  |  |  | 1.5423 | 2.0018 | 90 | 22.2 | 2.80 | 5 | 1.90 | 1.220 | Monetite |  |
| Mg-12 | 125 ml | 0.2298 |  |  |  | 0.7709 | 1.0007 | 90 | 11.1 | 2.70 | 7 | 2.10 | 0.240 | Whit. |  |
| Mg-13 | 125 ml | 0.3890 |  |  |  | 1.2813 | 1.6703 | 90 | 18.6 | 2.79 | 5 | 2.01 | 0.834 | Crypto-xtal mix |  |
| Mg-14 | 23 ml | 0.0158 |  |  |  | 0.0512 | 0.0670 | 10 | 6.7 | 2.10 | 7 | 1.85 | 0.030 | Whit. |  |
| Mg-15 | 23 ml | 0.2006 |  |  |  | 0.0000 | 0.2006 | 10 | 20.1 | 2.70 | 5 | 2.12 | 0.125 | Whit. |  |
| Mg-16 | 125 ml | 0.3004 |  |  |  | 1.0014 | 1.3018 | 90 | 14.5 | 2.77 | 7 | 1.70 | 1.131 | Whit. |  |
| Mg-17 | 125 ml | 0.3000 |  |  |  | 1.0000 | 1.3000 | 90 | 14.4 | 2.76 | 7 | 1.84 | 0.899 | Whit. |  |
| Mg-18 | 125 ml | 0.3000 |  |  |  | 1.0000 | 1.3000 | 90 | 14.4 | 2.74 | 7 | - | - | Whit. |  |
| Mg-19 | 125 ml | 0.3000 |  |  |  | 1.0000 | 1.3000 | 90 | 14.4 | 2.78 | 7 | - | - | Whit. |  |
| Mg-22 | 125 ml | 0.3004 |  |  |  | 1.0000 | 1.3004 | 90 | 14.4 | 2.72 | 7 | 1.78 | 0.800 | Whit. |  |
| Mg-23 | 125 ml | 0.3000 |  |  |  | 1.0070 | 1.3070 | 90 | 14.5 | 2.79 | 7 | 2.10 | 0.555 | Whit. |  |
| Mg-24 | 125 ml | 0.3000 |  |  |  | 1.0000 | 1.3000 | 80 | 16.3 | 2.74 | 7 | 2.11 | 0.588 | Leaked/Failed |  |
| Mg-25 | 125 ml | 0.3004 |  |  |  | 1.0007 | 1.3011 | 90 | 14.5 | 2.73 | 7 | 1.97 | 0.510 | Whit. |  |
| Mg-26 | 125 ml | 0.3005 |  |  |  | 1.0011 | 1.3016 | 90 | 14.5 | 2.70 | 7 | 1.98 | 0.480 | Whit. |  |
| Mg-27 | 125 ml | 0.3003 |  |  |  | 1.0010 | 1.3013 | 90 | 14.5 | 2.79 | 7 | 1.81 | 0.720 | Whit. |  |
| Mg-28 | 125 ml | 0.3000 |  |  |  | 1.0000 | 1.3000 | 90 | 14.4 | 2.78 | 7 | 1.88 | 0.699 | Whit. |  |
| Mg-29 | 125 ml | 0.3000 |  |  |  | 1.0000 | 1.3000 | 90 | 14.4 | 2.65 | 7 | 1.74 | 0.702 | Whit. |  |
| Mg-31 | 125 ml | 0.3026 |  |  |  | 1.0004 | 1.3030 | 90 | 14.5 | 2.65 | 12 | 1.76 | 0.810 | Whit. |  |
| Mg-32 | 125 ml | 0.3016 |  |  |  | 1.0006 | 1.3022 | 90 | 14.5 | 2.69 | 12 | 1.77 | 0.710 | Whit. |  |
| Mg-33 | 125 ml | 0.2997 |  |  |  | 1.0012 | 1.3009 | 90 | 14.5 | 2.71 | 12 | 1.72 | 0.730 | Whit. |  |
| Mg-34 | 125 ml | 0.2994 |  |  |  | 0.9996 | 1.299 | 90 | 14.4 | 2.74 | 6 | 1.78 | 0.770 | Whit. |  |
| Mg-35 | 125 ml | 0.3013 |  |  |  | 0.9998 | 1.3011 | 90 | 14.5 | 2.80 | 6 | 1.75 | 0.720 | Whit. |  |
| Mg-36 | 125 ml | 0.2997 |  |  |  | 1.0009 | 1.3006 | 90 | 14.5 | 2.75 | 6 | 1.74 | 0.810 | Whit. |  |
| Mg-37 | 125 ml | 0.3004 |  |  |  | 1.0005 | 1.3009 | 90 | 14.5 | 2.68 | 7 | 1.89 | 0.730 | Whit. |  |
| Mg-38 | 125 ml | 0.3002 |  |  |  | 1.0001 | 1.3003 | 90 | 14.4 | 2.72 | 7 | 1.82 | 0.700 | Whit. |  |
| Mg-39 | 125 ml | 0.3003 |  |  |  | 1.0001 | 1.3004 | 90 | 14.4 | 2.40 | 7 | 1.78 | 0.760 | Whit. |  |
| Mg-40 | 125 ml | 0.3004 |  |  |  | 1.0004 | 1.3008 | 90 | 14.5 | 2.74 | 8 | 1.89 | 0.665 | Whit. |  |
| Mg-41 | 125 ml | 0.2994 |  |  |  | 0.9999 | 1.2993 | 90 | 14.4 | 2.78 | 8 | 1.82 | 0.706 | Whit. |  |
| Mg-42 | 125 ml | 0.3008 |  |  |  | 1.0002 | 1.301 | 90 | 14.5 | 2.75 | 8 | 1.78 | 0.825 | Whit. |  |
| Mg-44 | 125 ml | 0.3002 |  |  |  | 1.0012 | 1.3014 | 90 | 14.5 | 2.73 | 7 | - | 0.632 | Whit. |  |
| Mg-45 | 125 ml | 0.3003 |  |  |  | 1.0008 | 1.3011 | 90 | 14.5 | 2.76 | 7 | 1.83 | 0.676 | Whit. |  |
| Mg-46 | 125 ml | 0.3005 |  |  |  | 1.0005 | 1.3010 | 90 | 14.5 | 2.74 | 7 | 1.77 | 0.775 | Whit. |  |
| Mg-47 | 125 ml | 0.2998 |  |  |  | 1.0003 | 1.3001 | 90 | 14.4 | 2.74 | 7 | 1.77 | 0.723 | Whit. |  |
| Mg-48 | 125 ml | 0.2998 |  |  |  | 1.0005 | 1.3003 | 90 | 14.4 | 2.76 | 7 | 1.76 | 0.726 | Whit. |  |
| Mg-49 | 125 ml | 0.2990 |  |  |  | 1.0000 | 1.2990 | 90 | 14.4 | 2.75 | 7 | 1.69 | 0.813 | Whit. |  |
| Mg-50 | 125 ml | 0.3002 |  |  |  | 1.0001 | 1.3003 | 90 | 14.4 | 2.66 | 8 | 1.80 | 0.627 | Whit. |  |
| Mg-51 | 125 ml | 0.3003 |  |  |  | 1.0001 | 1.3004 | 90 | 14.4 | 2.73 | 8 | 1.73 | 0.734 | Whit. |  |
| Mg-52 | 125 ml | 0.3001 |  |  |  | 1.0000 | 1.3001 | 90 | 14.4 | 2.75 | 8 | 1.68 | 0.776 | Whit. |  |
| Mg-53 | 125 ml | 0.3008 |  |  |  | 1.0000 | 1.3008 | 90 | 14.5 | 2.66 | 6 | 1.84 | 0.594 | Whit. |  |
| Mg-54 | 125 ml | 0.3009 |  |  |  | 1.0003 | 1.3012 | 90 | 14.5 | 2.79 | 6 | 1.75 | 0.690 | Whit. |  |
| Mg-55 | 125 ml | 0.3412 |  |  |  | 1.0006 | 1.3418 | 90 | 14.9 | 2.76 | 6 | 1.74 | 0.715 | Whit. |  |
| Mg-56 | 125 ml | 0.3003 |  |  |  | 0.9994 | 1.2997 | 90 | 14.4 | 2.69 | 7 | 1.85 | 0.702 | Whit. |  |
| Mg-57 | 125 ml | 0.3002 |  |  |  | 0.9995 | 1.2997 | 90 | 14.4 | 2.76 | 7 | 1.74 | 0.715 | Whit. |  |
| Mg-58 | 125 ml | 0.2999 |  |  |  | 1.0003 | 1.3002 | 90 | 14.4 | 2.74 | 7 | 1.70 | 0.734 | Whit. |  |
| Mg-59 | 125 ml | 0.3002 |  |  |  | 0.9998 | 1.3000 | 90 | 14.4 | 2.77 | 7 | 1.83 | 0.460 | Whit. |  |
| Mg-60 | 125 ml | 0.2998 |  |  |  | 0.9998 | 1.2996 | 90 | 14.4 | 2.74 | 7 | 1.85 | 0.437 | Whit. |  |
| Mg-61 | 125 ml | 0.3003 |  |  |  | 1.0012 | 1.3015 | 90 | 14.5 | 2.74 | 7 | 1.83 | 0.566 | Whit. |  |
| Fe-1 | 23 ml |  | 0.0287 |  |  | 0.2307 | 0.2594 | 16 | 16.2 | 2.68 | 9 | 2.26 | 0.148 | No Whit. |  |
| Fe-2 | 23 ml |  | 0.0290 |  |  | 0.2311 | 0.2601 | 16 | 16.3 | 2.77 | 9 | 2.20 | 0.143 | No Whit. |  |
| Fe-3 | 23 ml | 0.0356 | 0.0173 |  |  | 0.2312 | 0.2841 | 16 | 17.8 | 2.74 | 8 | 2.11 | 0.114 | No Whit. |  |
| Fe-4 | 23 ml | 0.0357 |  | 0.0129 |  | 0.2311 | 0.2797 | 16 | 17.5 | 2.77 | 8 | 2.00 | 0.173 | minor Whit. |  |
| Fe-5 | 23 ml |  |  | 0.0249 |  | 0.2334 | 0.2583 | 16 | 16.1 | 2.75 | 8 | 1.80 | - | aggregates Whit. |  |
| Fe-6 | 23 ml |  |  | 0.0183 |  | 0.1739 | 0.1922 | 16 | 12.0 | 2.74 | 8 | 1.80 | - | Cleaner Whit |  |
| Fe-7 | 125 ml |  |  | 0.0763 |  | 0.7300 | 0.8063 | 90 | 9.0 | 2.76 | 7 | 2.06 | 0.427 | Fe-Whit. |  |
| Fe-8 | 125 ml |  |  | 0.0769 |  | 1.0012 | 1.0781 | 90 | 12.0 | 2.77 | 7 | 2.10 | 0.520 | Fe-Whit. |  |
| Fe-9 | 125 ml |  |  | 0.0600 |  | 0.9994 | 1.0594 | 90 | 11.8 | 2.78 | 7 | 2.05 | 0.630 | Fe-Whit. |  |
| Fe-10 | 125 ml |  |  | 0.0500 |  | 1.0001 | 1.0501 | 90 | 11.7 | 2.77 | 7 | 2.17 | 0.520 | Fe-whit+agg. |  |
| Fe-11 | 125 ml |  |  | 0.0347 |  | 1.0009 | 1.0356 | 90 | 11.5 | 2.78 | 7 | 1.87 | 0.500 |  |  |
| Fe-12 | 125 ml |  |  | 0.0392 |  | 1.0000 | 1.0392 | 90 | 11.5 | 2.69 | 7 | 1.96 | 0.471 | Lg xtals Fe-whit. |  |
| Fe-13 | 125 ml |  |  | 0.0450 |  | 1.0000 | 1.0450 | 90 | 11.6 | 2.74 | 7 | 1.87 | 0.785 | Lg xtals Fe-whit. |  |
| Fe-14 | 125 ml |  |  | 0.0767 |  | 1.0008 | 1.0775 | 90 | 12.0 | 2.75 | 7 | 1.90 | 0.731 | Fe-whit+agg. |  |
| Fe-15 | 125 ml |  |  | 0.1003 |  | 1.0004 | 1.1007 | 90 | 12.2 | 2.72 | 7 | 1.92 | 0.846 | Fe-Whit. |  |
| Fe-16 | 125 ml |  |  | 0.0349 |  | 0.9999 | 1.0348 | 90 | 11.5 | 2.69 | 7 | 1.89 | 0.609 | Fe-Whit. |  |
| Fe-17 | 125 ml |  | 0.0800 |  |  | 1.0003 | 1.0803 | 90 | 12.0 | 2.75 | 7 | 1.94 | 0.451 | No-Whit. |  |
| Fe-18 | 125 ml |  |  | 0.0849 |  | 1.1003 | 1.1852 | 90 | 13.2 | 2.75 | 7 | 1.89 | 0.726 | Fe-Whit. |  |
| Fe-19 | 125 ml |  |  | 0.1101 |  | 1.2004 | 1.3105 | 90 | 14.6 | 2.68 | 7 | 1.97 | 0.845 | Fe-whit+agg. |  |
| Fe-20 | 125 ml |  |  | 0.0549 |  | 1.0004 | 1.0553 | 90 | 11.7 | 2.76 | 7 | 1.95 | 0.419 | Fe-Whit. |  |
| Fe-21 | 125 ml |  |  | 0.0558 |  | 1.0001 | 1.0559 | 90 | 11.7 | 2.69 | 7 | 1.92 | 0.452 | Fe-Whit. |  |
| Fe-22 | 125 ml |  |  | 0.0544 |  | 1.0004 | 1.0548 | 90 | 11.7 | 2.71 | 7 | 1.96 | 0.444 | Fe-Whit. |  |
| Mix-1 | 125ml | 0.0500 |  | 0.0500 | 0.0667 | 1.0000 | 1.1667 | 90 | 13.0 | 2.64 | 7 | 2.05 | 0.761 | Whit. |  |
| Mix-2 | 125ml | 0.1000 |  | 0.0500 |  | 1.0000 | 1.1500 | 90 | 12.8 | 2.73 | 7 | 2.15 | 0.694 | Whit. |  |
| Mix-3 | 125ml | 0.1000 |  |  | 0.1000 | 1.0000 | 1.2000 | 90 | 13.3 | 2.78 | 7 | - | - | No Whit. |  |
| Mix-4 | 125ml | 0.1000 |  | 0.0495 |  | 0.9997 | 1.1492 | 90 | 12.8 | 2.78 | 7 | 2.2 | 0.688 | No Whit. (HAP) |  |
| Mix-5 | 125ml | 0.1103 |  | 0.0403 |  | 1.0000 | 1.1506 | 90 | 12.8 | 2.70 | 7 | 2.01 | 0.821 | No Whit. (HAP) |  |
| Mix-6 | 125ml | 0.1207 |  | 0.0305 |  | 1.0005 | 1.1517 | 90 | 12.8 | 2.78 | 7 | 2.27 | 0.591 | Rare Whit. |  |
| Mix-7 | 125 ml | 0.0505 |  | 0.0499 | 0.0668 | 1.0000 | 1.1672 | 90 | 13.0 | 2.75 | 7 | 1.8 | 0.811 | Whit. |  |
| Mix-8 | 125 ml | 0.0505 |  | 0.0499 |  | 1.0005 | 1.1009 | 90 | 12.2 | 2.74 | 7 | 1.84 | 0.915 | Whit. |  |
| Mix-9 | 125 ml | 0.1505 |  | 0.0500 |  | 1.2000 | 1.4005 | 90 | 15.6 | 2.78 | 7 | 2.1 | 0.974 | No Whit. |  |
| Mix-10 | 125 ml | 0.1000 |  | 0.0500 |  | 1.0000 | 1.1500 | 90 | 12.8 | 2.72 | 7 | 2.05 | 0.700 | Rare Whit. |  |
| Mix-11 | 125 ml | 0.0800 |  | 0.0400 |  | 0.8000 | 0.9200 | 90 | 10.2 | 2.78 | 7 | 2.04 | 0.550 | Rare Whit. |  |
| Mix-12 | 125 ml | 0.0900 |  | 0.0300 |  | 0.8000 | 0.9200 | 90 | 10.2 | 2.78 | 7 | 2.02 | - | Minor Whit. |  |
| Mix-13 | 125 ml | 0.0500 |  | 0.0501 |  | 1.0002 | 1.1003 | 90 | 12.2 | 2.75 | 7 | 1.89 | 0.799 | Whit. (lg) |  |
| Mix-14 | 125 ml | 0.0399 |  | 0.0601 |  | 0.9999 | 1.0999 | 90 | 12.2 | 2.78 | 7 | - | 0.765 | Whit. |  |
| Mix-15 | 125 ml | 0.0600 |  | 0.0400 |  | 1.0000 | 1.1000 | 90 | 12.2 | 2.77 | 7 | 2.04 | 0.707 | Whit. |  |
| Mix-16 | 125 ml | 0.0501 |  | 0.0500 | 0.0601 | 1.0001 | 1.1603 | 90 | 12.9 | 2.77 | 7 | 1.99 | 0.785 | Whit. well fm. |  |
| Mix-17 | 125 ml | 0.0251 |  | 0.0501 |  | 0.9000 | 0.9752 | 90 | 10.8 | 2.76 | 7 | - | 0.556 | Whit. |  |
| Mix-18 | 125 ml | 0.0300 |  | 0.0700 |  | 1.0000 | 1.1000 | 90 | 12.2 | 2.77 | 7 | 2.01 | 0.644 | Whit. |  |
| Mix-19 | 125 ml | 0.0351 |  | 0.0501 |  | 1.0001 | 1.0853 | 90 | 12.1 | 2.77 | 7 | 1.98 | 0.689 | Whit. |  |
| Mix-20 | 125 ml | 0.0350 |  | 0.0502 |  | 1.0000 | 1.0852 | 90 | 12.1 | 2.78 | 7 | 1.96 | 0.674 | A.W./Whit. |  |
| Mix-21 | 125 ml | 0.0901 |  | 0.0302 |  | 0.9002 | 1.0205 | 90 | 11.3 | 2.78 | 7 | 2.2 | 0.470 | Rare Whit. |  |

Vessel Size = the volume of the Teflon lines Parr reaction vessel used.  All chemistry weights are in grams.  Mass Tot = Total mass of solids in grams used in the experiment.  DI = volume of 18 MΩ water used in experiment. g/L = ratio of total mass of solids (g) in solution (L). pH Start = the adjusted pH at the start of the experiment.  Days = number of days of incubation.  pH end = measured pH at end of experiment.  Mass Out = total mass (g)of material recovered after experiment including  impurities.  Abbreviations in  notes: Whit.=whitlockite, agg. = polycrystalline aggregates, lg = large, HAP = hydroxyapatite, well fm. = well formed crystals. Crypto-xtal mix = mix of microcrystalline phases. A.W. = reaction vessel underwent additional cleaning including additional acid washing to investigate any affect on nucleation.

Table A2.  Microprobe analyses of Mg/Fe-whitlockite synthesized with varied Fe: Mg ratios.  For paper titled Synthesis and characterization of the Mars-relevant phosphate minerals Fe- and Mg-whitlockite and merrillite and a possible mechanism that maintains charge balance during whitlockite to merrillite transformation. Christopher T. Adcock*, Elisabeth M. Hausrath,  Paul M. Forster, Oliver Tschauner and Kirellos J. Sefein.

| Mg/Fe-Whitlockite Synthesis Experiment ID |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mix-6 |  |  | Mix-21 |  |  |  |  |  | Mix-1 |  |  |
| CaO | 48.40 | (0.26) |  |  |  | 47.73 |  | (1.31) |  | 46.54 | (0.59) |  |
| P2O5 | 45.83 | (0.28) |  |  |  | 45.59 |  | (0.92) |  | 45.83 | (0.36) |  |
| MgO | 3.43 | (0.32) |  |  |  | 2.63 |  | (0.05) |  | 1 | (0.20) |  |
| FeO | 0.18 | (0.24) |  |  |  | 1.92 |  | (2.51) |  | 4.62 | (0.71) |  |
| Na2O | B.D. | - |  |  |  | B.D. |  | - |  | B.D. | - |  |
| H2Oa | 0.86 | - |  |  |  | 0.86 |  | - |  | 0.86 | - |  |
| Total | 98.69 | (0.42) |  |  |  | 98.73 |  | (0.79) |  | 98.85 | (0.49) |  |
| n | 11 |  |  |  |  |  | 7 |  |  | 18 |  |  |
| Stoic. | Ca9.2Fe0.0Mg0.9(PO3OH)(PO4)5.9 |  |  |  |  |  | Ca9.1Fe0.3Mg0.7(PO3OH)(PO4)5.9 |  |  | Ca9.0Fe0.7Mg0.3(PO3OH)(PO4)6 |  |  |
| Fe:Mg Soln.b | 0.74 |  |  |  |  |  | 0.98 |  |  | 2.91 |  |  |
| Fe:Mg Prod.c | 0.00 |  |  |  |  |  | 0.43 |  |  | 2.33 |  |  |

Parenthetical values are 1 standard deviation. n = number of analyses averaged chemistry is based on. B.D. = below detection.

aH2O is based on ideal whitlockite (Hughes et al., 2008) and is included in these EMP totals.

bThe molar ratio of Fe: Mg added to the solution of the experiment.

cThe molar ratio of Fe: Mg in the stoichiometry of the resulting whitlockite.

Table A3.  Atomic parameters for synthesized whitlockite and merrillite.  For paper titled Synthesis and characterization of the Mars-relevant phosphate minerals Fe- and Mg-whitlockite and merrillite and a possible mechanism that maintains charge balance during whitlockite to merrillite transformation. Christopher T. Adcock*, Elisabeth M. Hausrath,  Paul M. Forster, Oliver Tschauner and Kirellos J. Sefein.

| Atom | Fe-whitlockite | Fe/Mg-whitlockite | Ferric Fe-merrillite (Pt cruc.) | Ferrous Fe-merrillite (SiO2 tube) | Ferric Fe/Mg-merrillite (Pt cruc.) | Ferrous Fe/Mg-merrillite (SiO2 tube) |
| --- | --- | --- | --- | --- | --- | --- |
| Fe(1) | Fe1.00 | Fe0.637 | Fe1.00 | Fe1.00 | Fe0.754 | Fe0.646 |
| x | 0.6667 | 0.6667 | 0.6667 | 0.6667 | 0.6667 | 0.6667 |
| y | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 |
| z | 0.1137(1) | 0.1138(1) | 0.1151(1) | 0.1142(1) | 0.1149(1) | 0.1150(1) |
| U(eq) | 0.008(1) | 0.003(1) | 0.005(1) | 0.006(1) | 0.002(1) | 0.004(1) |
| Mg(1) |  | Mg0.363 |  |  | Mg0.246 | Mg0.354 |
| x | NA | 0.6667 | NA | NA | 0.6667 | 0.6667 |
| y | NA | 0.3333 | NA | NA | 0.3333 | 0.3333 |
| z | NA | 0.1138(1) | NA | NA | 0.1149(1) | 0.1150(1) |
| U(eq) | NA | 0.002 | NA | NA | 0.002 | 0.004 |
| Ca(1) | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 |
| x | 0.7191(1) | 0.7192(1) | 0.7224(1) | 0.7245(1) | 0.7226(1) | 0.7239(1) |
| y | 0.8534(1) | 0.8534(1) | 0.8547(1) | 0.8571(1) | 0.8548(1) | 0.8566(1) |
| z | 0.2150(1) | 0.2150(1) | 0.2140(1) | 0.2133(1) | 0.2140(1) | 0.2144(1) |
| U(eq) | 0.005(1) | 0.004(1) | 0.004(1) | 0.005(1) | 0.004(1) | 0.005(1) |
| Ca(2) | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 |
| x | 0.5125(1) | 0.5122(1) | 0.5081(1) | 0.5099(1) | 0.5088(1) | 0.5103(1) |
| y | 0.0542(1) | 0.0537(1) | 0.0442(1) | 0.0502(1) | 0.0451(1) | 0.0509(1) |
| z | 0.1792(1) | 0.1793(1) | 0.1798(1) | 0.1785(1) | 0.1796(1) | 0.1794(1) |
| U(eq) | 0.005(1) | 0.005(1) | 0.004(1) | 0.005(1) | 0.004(1) | 0.006(1) |
| Ca(3) | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 | Ca1.00 |
| x | 1.1580(1) | 1.1573(1) | 1.1483(1) | 1.1495(1) | 1.1489(1) | 1.1506(1) |
| y | 0.8643(1) | 0.8646(1) | 0.8714(1) | 0.8731(1) | 0.8709(1) | 0.8717(1) |
| z | 0.1080(1) | 0.1080(1) | 0.1072(1) | 0.1064(1) | 0.1071(1) | 0.1074(1) |
| U(eq) | 0.012(1) | 0.011(1) | 0.006(1) | 0.015(1) | 0.007(1) | 0.016(1) |
| P(2) | P1.00 | P1.00 | P1.00 | P1.00 | P1.00 | P1.00 |
| x | 0.4761(1) | 0.4761(1) | 0.4745(1) | 0.4713(1) | 0.4746(1) | 0.4725(1) |
| y | -0.0162(1) | -0.0160(1) | -0.0175(1) | -0.0201(1) | -0.0174(1) | -0.0193(1) |
| z | 0.0827(1) | 0.0827(1) | 0.0841(1) | 0.0820(1) | 0.0837(1) | 0.0830(1) |
| U(eq) | 0.005(1) | 0.004(1) | 0.003(1) | 0.005(1) | 0.003(1) | 0.005(1) |
| P(1) | P1.00 | P1.00 | P1.00 | P1.00 | P1.00 | P1.00 |
| x | 0.8606(1) | 0.8601(1) | 0.8562(1) | 0.8602(1) | 0.8564(1) | 0.8601(1) |
| y | 0.6848(1) | 0.6841(1) | 0.6761(1) | 0.6794(1) | 0.6767(1) | 0.6798(1) |
| z | 0.1464(1) | 0.1464(1) | 0.1459(1) | 0.1455(1) | 0.1458(1) | 0.1464(1) |
| U(eq) | 0.004(1) | 0.004(1) | 0.003(1) | 0.004(1) | 0.003(1) | 0.005(1) |
| P(3A) | P0.890 | P0.840 | P0.029 | P0.239 | P0.065 | P0.309 |
| x | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 |
| y | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 |
| z | 0.1934(1) | 0.1934(1) | 0.2178(1) | 0.2138(1) | 0.2170(1) | 0.2146(1) |
| U(eq) | 0.005(1) | 0.005(1) | 0.004(1) | 0.005(1) | 0.005(1) | 0.006(1) |
| P(3B) | P0.110 | P0.160 | P0.971 | P0.761 | P0.935 | P0.691 |
| x | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 |
| y | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 |
| z | 0.2160(2) | 0.2165(1) | 0.1952(13) | 0.1932(2) | 0.1933(5) | 0.1936(1) |
| U(eq) | 0.005 | 0.005 | 0.004 | 0.005 | 0.005 | 0.004(1) |
| O(10A) | O0.890 | O0.840 | O0.029 | O0.239 | O0.065 | O0.309 |
| x | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 |
| y | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 |
| z | 0.1508(1) | 0.1508(1) | 0.2594(1) | 0.2555(2) | 0.2586(1) | 0.1523(2) |
| U(eq) | 0.013(1) | 0.012(1) | 0.006(1) | 0.009(1) | 0.007(1) | 0.015(3) |
| O(10B) | O0.110 | O0.160 | O0.970 | O0.761 | O0.935 | O0.691 |
| x | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 | 0.3333 |
| y | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 | -0.3333 |
| z | 0.2568(8) | 0.2579(3) | 0.1549(15) | 0.1520(2) | 0.1511(8) | 0.2560(2) |
| U(eq) | 0.013 | 0.004(2) | 0.007 | 0.009 | 0.007 | 0.011(1) |
| O(6) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.5657(2) | 0.5658(1) | 0.5682(2) | 0.5602(3) | 0.5677(2) | 0.5620(2) |
| y | -0.0877(2) | -0.0872 | -0.0826(2) | -0.0930(3) | -0.0831(2) | -909(2) |
| z | 0.0696(1) | 0.0695(1) | 0.0696(1) | 0.0684(1) | 0.0691(1) | 0.0694(1) |
| U(eq) | 0.008(1) | 0.007(1) | 0.006(1) | 0.016(1) | 0.006(1) | 0.013(1) |
| O(9) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.3533(2) | 0.3526(1) | 0.3444(2) | 0.3420(3) | 0.3436(2) | 0.3431(3) |
| y | -0.1832(2) | -0.1834(1) | -0.1866(2) | -0.1882(3) | -0.0187(2) | -0.1876(2) |
| z | 0.2056(1) | 0.2054(1) | 0.2050(1) | 0.2018(1) | 0.2044(1) | 0.2030(1) |
| U(eq) | 0.009(1) | 0.008(1) | 0.007(1) | 0.016(1) | 0.009(1) | 0.017(1) |
| O(8) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.3344(2) | 0.3345(1) | 0.3365(2) | 0.3317(3) | 0.3356(2) | 0.3325(2) |
| y | -0.0606(2) | -0.0606(1) | -0.0552(2) | -0.0575(3) | -0.0559(2) | -0.0579(2) |
| z | 0.0604(1) | 0.0604(1) | 0.0606(1) | 0.0594(1) | 0.0605(1) | 0.0604(1) |
| U(eq) | 0.006(1) | 0.005(1) | 0.005(1) | 0.006(1) | 0.005(1) | 0.006(1) |
| O(5) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.5754(2) | 0.5756(1) | 0.5763(2) | 0.5746(3) | 0.5762(2) | 0.5750(2) |
| y | 0.1551(2) | 0.1556(1) | 0.1589(2) | 0.1516(3) | 0.1582(2) | 0.1529(2) |
| z | 0.0774(1) | 0.0778(1) | 0.0808(1) | 0.0781(1) | 0.0803(1) | 0.0792(1) |
| U(eq) | 0.007(1) | 0.007(1) | 0.005(1) | 0.009(1) | 0.004(1) | 0.010(1) |
| O(2) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.8747(2) | 0.8737(1) | 0.8599(2) | 0.8660(3) | 0.8613(2) | 0.8670(2) |
| y | 0.7381(2) | 0.7360(1) | 0.7100(2) | 0.7168(3) | 0.7119(3) | 0.7198(3) |
| z | 0.1068(1) | 0.1068(1) | 0.1058(1) | 0.1054(1) | 0.1057(1) | 0.1063(1) |
| U(eq) | 0.009(1) | 0.009(1) | 0.006(1) | 0.010(1) | 0.007(1) | 0.013(1) |
| O(3) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 1.0193(2) | 1.0188(1) | 1.0161(2) | 1.0204(2) | 1.0161(2) | 1.0203(2) |
| y | 0.7337(2) | 0.7330(1) | 0.7289(2) | 0.7308(3) | 0.7291(2) | 0.7311(2) |
| z | 0.1598(1) | 0.1597(1) | 0.1589(1) | 0.1580(1) | 0.1590(1) | 0.1590(1) |
| U(eq) | 0.007(1) | 0.006(1) | 0.006(1) | 0.007(1) | 0.006(1) | 0.007(1) |
| O(1) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.7795(2) | 0.7792(1) | 0.7803(2) | 0.7857(3) | 0.7800(2) | 0.7846(2) |
| y | 0.7504(2) | 0.7499(1) | 0.7482(2) | 0.7538(3) | 0.7486(2) | 0.7528(2) |
| z | 0.1674(1) | 0.1672(1) | 0.1665(1) | 0.1657(1) | 0.1663(1) | 0.1667(1) |
| U(eq) | 0.008(1) | 0.007(1) | 0.006(1) | 0.009(1) | 0.007(1) | 0.009(1) |
| O(4) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.7675(2) | 0.7671(1) | 0.7619(2) | 0.7656(3) | 0.7623(2) | 0.7655(2) |
| y | 0.5128(2) | 0.5122(1) | 0.5034(2) | 0.5096(3) | 0.5041(2) | 0.5093(2) |
| z | 0.1506(1) | 0.1506(1) | 0.1519(1) | 0.1523(1) | 0.1516(1) | 0.1524(1) |
| U(eq) | 0.007(1) | 0.007(1) | 0.005(1) | 0.007(1) | 0.005(1) | 0.008(1) |
| O(7) | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 | O1.00 |
| x | 0.4261(2) | 0.4260(1) | 0.4214(2) | 0.4176(3) | 0.4222(3) | 0.4189(2) |
| y | -0.0543(2) | -0.0550(1) | -0.0610(2) | -0.0657(3) | -0.0616(2) | -0.0650(3) |
| z | 0.1219(1) | 0.1219(1) | 0.1227(1) | 0.1208(1) | 0.1224(1) | 0.1218(1) |
| U(eq) | 0.009(1) | 0.008(1) | 0.006(1) | 0.014(1) | 0.008(1) | 0.0015(1) |
| Ca(4A) |  |  |  | Ca0.148 |  | Ca0.098 |
| x | NA | NA | NA | 0.3333 | NA | 0.3333 |
| y | NA | NA | NA | -0.3333 | NA | -0.3333 |
| z | NA | NA | NA | 0.1360(1) | NA | 0.1041(3) |
| U(eq) | NA | NA | NA | 0.011(1) | NA | 0.019(3) |
| Ca(4B) |  |  |  | Ca0.296 |  | Ca0.264 |
| x | NA | NA | NA | 0.3333 | NA | 0.3333 |
| y | NA | NA | NA | -0.3333 | NA | -0.3333 |
| z | NA | NA | NA | 0.1028(3) | NA | 0.1369(1) |
| U(eq) | NA | NA | NA | 0.013(3) | NA | 0.007(1) |

Parenthetic values are standard deviations. Pt cruc. = merrillite produced by heating in open air in a platinum crucible.  SiO2 tube = merrillite produced in a triple argon purged and sealed silica glass tube.

Table A4.  Bond lengths for synthesized whitlockite and merrillite in angstroms.  For paper titled Synthesis and characterization of the Mars-relevant phosphate minerals Fe- and Mg-whitlockite and merrillite and a possible mechanism that maintains charge balance during whitlockite to merrillite transformation. Christopher T. Adcock*, Elisabeth M. Hausrath,  Paul M. Forster, Oliver Tschauner and Kirellos J. Sefein.

|  |  | Fe-whitlockite | Fe/Mg-whitlockite | Ferric Fe-merrillite (Pt cruc.) | Ferrous Fe-merrillite (SiO2 tube) | Ferric Fe/Mg-merrillte (Pt cruc.) | Ferrous Fe/Mg-merrillite (SiO2 tube) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ca(1)- | O(1) | 2.3062(14) | 2.3115(11) | 2.308(2) | 2.313(3) | 2.310(2) | 2.3128(19) |
|  | O(2)#6 | 2.4348(17) | 2.4268(13) | 2.340(2) | 2.386(3) | 2.345(2) | 2.385(2) |
|  | O(3)#8 | 2.4482(15) | 2.4548(11) | 2.468(2) | 2.456(2) | 2.467(2) | 2.4568(19) |
|  | O(5)#7 | 2.4401(14) | 2.4445(11) | 2.511(2) | 2.449(3) | 2.506(2) | 2.449(2) |
|  | O(5)#9 | 2.4724(14) | 2.4763(11) | 2.495(2) | 2.487(3) | 2.484(2) | 2.485(2) |
|  | O(6)#7 | 2.7753(15) | 2.7703(11) | 2.740(2) | 2.849(3) | 2.741(2) | 2.823(2) |
|  | O(8)#9 | 2.5050(14) | 2.5065(11) | 2.470(2) | 2.469(2) | 2.474(2) | 2.4742(19) |
|  | O(9)#2 | 2.4570(14) | 2.4530(11) | 2.409(2) | 2.437(3) | 2.409(2) | 2.437(2) |
| Ca(2)- | O(1)#14 | 2.6522(15) | 2.6481(11) | 2.638(2) | 2.627(3) | 2.631(2) | 2.630(2) |
|  | O(10B)#15 | 2.717(7) | 2.699(3) | 2.5360(11) | 2.544(2) | 2.578(2) | 2.542(2) |
|  | O(2) | 2.5441(15) | 2.5465(11) | 2.586(2) | 2.475(3) | 2.492(2) | 2.469(2) |
|  | O(2)#14 | 2.4649(14) | 2.4675(11) | 2.492(2) | 2.377(2) | 2.389(2) | 2.3720(18) |
|  | O(3) | 2.3727(14) | 2.3736(11) | 2.388(2) | 2.564(2) | 2.5518(12) | 2.5888(17) |
|  | O(6)#1 | 2.3934(15) | 2.4009(12) | 2.458(2) | 2.484(3) | 2.463(2) | 2.468(2) |
|  | O(7)#13 | 2.5186(16) | 2.5251(12) | 2.609(2) | 2.573(3) | 2.610(2) | 2.567(2) |
|  | O(8)#13 | 2.3717(15) | 2.3762(11) | 2.418(2) | 2.399(3) | 2.412(2) | 2.3957(19) |
|  | O(9)#16 | 2.9456(15) | 2.9483(11) | 2.899(2) | 2.998(3) | 2.926(2) | 2.994(3) |
| Ca(3)- | O(1)#1 | 2.6373(15) | 2.6345(11) | 2.634(2) | 2.681(3) | 2.638(2) | 2.669(2) |
|  | O(3)#2 | 2.6570(14) | 2.6507(11) | 2.602(2) | 2.633(2) | 2.602(2) | 2.6348(18) |
|  | O(4)#1 | 2.4591(14) | 2.4612(11) | 2.501(2) | 2.439(2) | 2.497(2) | 2.4444(19) |
|  | O(4)#2 | 2.4278(14) | 2.4313(11) | 2.463(2) | 2.414(3) | 2.458(2) | 2.4191(19) |
|  | O(6)#12 | 2.4604(14) | 2.4616(11) | 2.473(2) | 2.450(3) | 2.468(2) | 2.449(2) |
|  | O(7) | 2.3600(15) | 2.3633(11) | 2.345(2) | 2.407(3) | 2.350(2) | 2.401(2) |
|  | O(8)#11 | 2.3685(14) | 2.3691(11) | 2.378(2) | 2.368(2) | 2.374(2) | 2.3675(18) |
|  | O(9) | 2.3782(14) | 2.3748(11) | 2.320(2) | 2.358(3) | 2.327(2) | 2.360(2) |
| Ca(4A)- | O(6)#18 | NA | NA | NA | 2.736(5) | NA | 2.758(6) |
|  | O(6)#19 | NA | NA | NA | 2.736(5) | NA | 2.758(6) |
|  | O(7)#18 | NA | NA | NA | 2.541(4) | NA | 2.541(4) |
|  | O(7)#19 | NA | NA | NA | 2.541(4) | NA | 2.541(4) |
| Ca(4B)- | O(6)#18 | NA | NA | NA | 2.516(3) | NA | 2.518(2) |
|  | O(6)#19 | NA | NA | NA | 2.516(3) | NA | 2.518(2) |
|  | O(7)#18 | NA | NA | NA | 2.846(5) | NA | 2.851(4) |
|  | O(7)#19 | NA | NA | NA | 2.846(5) | NA | 2.851(4) |
| Fe(1)- | O(4) | 2.1131(16) | 2.1067(13) | 2.046(2) | 2.122(3) | 2.048(2) | 2.104(2) |
|  | O(4)#1 | 2.1130(16) | 2.1068(13) | 2.046(2) | 2.122(3) | 2.048(2) | 2.104(2) |
|  | O(4)#2 | 2.1130(16) | 2.1068(13) | 2.046(2) | 2.122(3) | 2.048(2) | 2.104(2) |
|  | O(5) | 2.0893(16) | 2.0806(12) | 2.011(2) | 2.108(3) | 2.023(2) | 2.092(2) |
|  | O(5)#1 | 2.0893(16) | 2.0806(12) | 2.011(2) | 2.108(3) | 2.023(2) | 2.092(2) |
|  | O(5)#2 | 2.0893(16) | 2.0806(12) | 2.011(2) | 2.108(3) | 2.023(2) | 2.092(2) |
| P(1)- | O(1) | 1.5281(15) | 1.5257(11) | 1.528(2) | 1.528(3) | 1.530(2) | 1.528(2) |
|  | O(2) | 1.5484(16) | 1.5456(13) | 1.521(2) | 1.532(3) | 1.523(2) | 1.535(2) |
|  | O(3) | 1.5393(14) | 1.5382(11) | 1.535(2) | 1.537(2) | 1.535(2) | 1.5377(18) |
|  | O(4) | 1.5512(16) | 1.5497(12) | 1.562(2) | 1.546(3) | 1.561(2) | 1.546(2) |
| P(2)- | O(5) | 1.5538(16) | 1.5552(12) | 1.588(2) | 1.556(3) | 1.583(2) | 1.558(2) |
|  | O(6) | 1.5261(15) | 1.5260(12) | 1.527(2) | 1.537(3) | 1.526(2) | 1.531(2) |
|  | O(7) | 1.5284(15) | 1.5256(12) | 1.516(2) | 1.529(3) | 1.520(2) | 1.529(2) |
|  | O(8) | 1.5385(15) | 1.5381(11) | 1.544(2) | 1.543(2) | 1.546(2) | 1.5422(19) |
| P(3A)- | O(10A) | 1.582(3) | 1.578(3) | 1.540(4) | 1.530(3) | 1.57(3) | 1.530(7) |
|  | O(9) | 1.5297(14) | 1.5291(11) | 1.5366(19) | 1.493(3) | 1.518(6) | 1.500(2) |
|  | O(9)#18 | 1.5298(14) | 1.5292(11) | 1.5366(19) | 1.493(3) | 1.518(6) | 1.500(2) |
|  | O(9)#19 | 1.5298(14) | 1.5292(11) | 1.5366(19) | 1.493(3) | 1.518(6) | 1.500(2) |
| P(3B)- | O(10B) | 1.51(3) | 1.534(14) | 1.49(3) | 1.546(7) | 1.543(5) | 1.535(6) |
|  | O(9) | 1.512(3) | 1.5187(16) | 1.507(12) | 1.526(2) | 1.534(2) | 1.5209(19) |
|  | O(9)#18 | 1.512(3) | 1.5187(16) | 1.507(12) | 1.526(2) | 1.534(2) | 1.5209(19) |
|  | O(9)#19 | 1.512(3) | 1.5187(16) | 1.507(12) | 1.526(2) | 1.534(2) | 1.5209(19) |

Parenthetic values are standard deviations. Pt cruc. = merrillite produced by heating in open air in a platinum crucible.  SiO2 tube = merrillite produced in a triple argon purged and sealed silica glass tube.