Revision 1.

MSA DEPOSITORY ITEMS:

TABLE 1. Experiment 1 refined unit cell parameters of dry talc. The errors are the 95% confidence limits determined in the Unitcell refinement (Holland and Redfern 1997) for a triclinic system plus experimental error.

| File | P (GPa) | a (Å) | b (Å) | c (Å) |  (°) |  (°) |  (°) | V (Å3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Talc | 0 | 5.289(7) | 9.172(11) | 9.477(10) | 90.63(22) | 99.34(25) | 90.13(18) | 453.6(4) |
| 001 | 0.16(10) | 5.284(9) | 9.156(11) | 9.467(11) | 90.52(19) | 99.10(21) | 90.02(19) | 452.2(6) |
| 002 | 1.15(40) | 5.265(7) | 9.118(8) | 9.304(9) | 90.78(16) | 99.98(19) | 89.94(15) | 439.9(4) |
| 003 | 2.4(6) | 5.251(8) | 9.081(11) | 9.189(11) | 90.47(19) | 100.76(24) | 90.04(17) | 430.5(5) |
| 004 | 3.16(70) | 5.241(6) | 9.057(8) | 9.123(10) | 90.15(22) | 100.81(28) | 90.08(16) | 425.4(4) |
| 005 | 4.5(10) | 5.226(7) | 9.036(10) | 9.059(10) | 90.21(19) | 101.25(22) | 90.03(16) | 419.5(4) |
| 006 | 5.3(10) | 5.224(17) | 9.025(18) | 9.038(19) | 90.24(27) | 101.36(34) | 90.09(34) | 417.8(10) |
| 007 | 6.6(12) | 5.215(15) | 9.028(21) | 8.977(19) | 90.46(27) | 101.60(33) | 90.13(27) | 414.0(9) |
| 008 | 8.0(11) | 5.236(13) | 8.971(16) | 8.923(15) | 90.29(23) | 101.53(28) | 90.14(23) | 410.6(7) |
| 009 | 8.8(11) | 5.254(16) | 8.951(20) | 8.872(29) | 90.79(29) | 100.58(40) | 90.35(29) | 410.1(12) |
| 010 | 10.0(14) | 5.233(12) | 8.932(13) | 8.856(18) | 90.45(24) | 101.43(28) | 90.14(23) | 405.7(7) |

Note: the c lattice parameter for the triclinic fit is roughly half that of the monoclinic 2M polytype fit as listed in MSA Depository Tables 3 and 4.

TABLE 2. Experiment 1 refined unit cell parameters of wet talc with errors of 95% confidence limits determined in the Unitcell refinement (Holland and Redfern 1997) for a triclinic system plus experimental error.

| File | P (GPa) | a (Å) | b (Å) | c (Å) |  (°) |  (°) |  (°) | V (Å3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 001 | 0 | 5.289(7) | 9.145(8) | 9.453(12) | 90.73(21) | 98.84(27) | 89.80(18) | 451.80(48) |
| 002 | 0.12(17) | 5.291(6) | 9.154(8) | 9.456(11) | 90.60(18) | 99.04(24) | 89.95(17) | 452.24(49) |
| 003 | 0.14(14) | 5.291(7) | 9.144(9) | 9.455(8) | 90.52(17) | 99.07(21) | 89.98(17) | 451.72(43) |
| 004 | 0.52(20) | 5.256(6) | 9.142(5) | 9.403(6) | 90.87(15) | 99.26(15) | 89.97(15) | 445.85(29) |
| 005 | 1.03(21) | 5.232(22) | 9.117(7) | 9.321(24) | 91.20(25) | 99.22(37) | 89.57(24) | 438.8(16) |
| 006 | 1.35(35) | 5.253(11) | 9.124(8) | 9.294(13) | 90.87(23) | 99.81(24) | 89.90(21) | 438.87(71) |
| 007 | 1.73(42) | 5.262(10) | 9.114(6) | 9.255(12) | 90.80(21) | 100.06(28) | 89.96(19) | 436.96(78) |
| 008 | 2.21(54) | 5.236(5) | 9.075(6) | 9.193(8) | 91.42(17) | 100.10(17) | 89.86(16) | 429.86(33) |
| 009 | 2.21(54) | 5.235(6) | 9.072(10) | 9.186(9) | 91.45(19) | 100.10(17) | 89.48(17) | 429.31(46) |
| 010 | 2.76(46) | 5.228(7) | 9.047(15) | 9.151(11) | 91.57(26) | 99.83(22) | 89.48(18) | 426.29(70) |
| 011 | 3.87(84) | 5.203(10) | 9.029(10) | 9.053(14) | 91.46(23) | 99.46(21) | 89.41(23) | 419.34(65) |
| 012 | 5.5(10) | 5.195(9) | 9.016(12) | 8.990(15) | 90.55(24) | 99.87(27) | 89.72(28) | 414.8(21) |
| 013 | 6.28(93) | 5.184(15) | 8.992(16) | 8.941(10) | 90.63(25) | 99.89(32) | 89.52(27) | 410.5(20) |
| 014 | 7.07(91) | 5.192(12) | 8.976(18) | 8.944(23) | 90.21(31) | 100.48(38) | 89.46(27) | 409.9(21) |
| 015 | 8.0(10) | 5.202(11) | 8.964(16) | 8.898(20) | 89.68(36) | 100.60(27) | 89.68(23) | 407.9(22) |
| 016 | 8.9(11) | 5.216(13) | 8.943(14) | 8.893(29) | 89.59(35) | 101.11(49) | 89.81(26) | 407.0(29) |
| 017 | 8.8(14) | 5.188(12) | 8.935(16) | 8.923(27) | 90.49(33) | 101.67(45) | 89.28(27) | 405.0(21) |
| 018 | 9.9(11) | 5.217(17) | 8.942(16) | 8.851(30) | 89.54(47) | 100.84(41) | 89.7(4) | 405.5(35) |
| 019 | 6.89(86) | 5.210(16) | 8.971(18) | 8.980(32) | 90.32(33) | 101.19(38) | 89.48(28) | 411.7(26) |
| 020 | 0.41(15) | 5.296(24) | 9.160(14) | 9.435(29) | 90.53(26) | 98.90(64) | 90.26(39) | 452.2(50) |

TABLE 3. Experiment 2 refined unit cell parameters of dry talc; errors of 95% confidence limits determined in the Le Bail refinement.  Basal spacing, c*, is measured directly from diffraction pattern.

| File | P (GPa) | T (oC) |  | a (Å) | b (Å) | c (Å) | β (°) | c* (Å) |  | V (Å3) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 20.0(5) |  | 5.27(2) | 9.26(4) | 19.20(1) | 102.5(1) | 18.75(1) |  | 915(8) |  |
| 2 | 1.2(1) | 20.0(5) |  | 5.277(9) | 9.14(2) | 18.60(2) | 100.0(2) | 18.32(1) |  | 884(10) |  |
| 3 | 1.3(1) | 20.0(5) |  | 5.271(9) | 9.14(2) | 18.60(2) | 100.0(2) | 18.32(1) |  | 882(10) |  |
| 4 | 1.3(2) | 20.0(5) |  | 5.271(9) | 9.13(1) | 18.58(1) | 100.0(1) | 18.30(1) |  | 881(8) |  |
| 5 | 1.3(2) | 20.0(5) |  | 5.269(9) | 9.13(1) | 18.58(1) | 100.0(2) | 18.30(1) |  | 880(8) |  |
| 6 | 1.4(2) | 20.0(5) |  | 5.271(9) | 9.13(1) | 18.58(2) | 100.0(2) | 18.30(2) |  | 881(11) |  |
| 7 | 1.6(1) | 20.0(5) |  | 5.269(8) | 9.14(1) | 18.54(2) | 100.2(3) | 18.24(2) |  | 879(14) |  |
| 8 | 1.8(1) | 20.0(5) |  | 5.268(7) | 9.14(1) | 18.50(2) | 100.2(2) | 18.20(2) |  | 876(11) |  |
| 9 | 2.1(1) | 20.0(5) |  | 5.248(7) | 9.09(1) | 18.59(2) | 102.6(2) | 18.14(2) |  | 866(11) |  |
| 10 | 3.0(2) | 20.0(5) |  | 5.254(8) | 9.12(1) | 18.24(2) | 100.3(2) | 17.95(2) |  | 860(13) |  |
| 11 | 3.1(1) | 20.0(5) |  | 5.256(8) | 9.11(1) | 18.23(2) | 100.2(2) | 17.94(2) |  | 859(12) |  |
| 12 | 3.1(2) | 20.0(5) |  | 5.244(7) | 9.10(1) | 18.24(2) | 100.4(2) | 17.94(2) |  | 856(13) |  |
| 13 | 3.2(2) | 20.0(5) |  | 5.253(7) | 9.10(1) | 18.22(2) | 100.1(2) | 17.94(1) |  | 857(10) |  |
| 14 | 3.4(2) | 20.0(5) |  | 5.254(7) | 9.10(1) | 18.21(2) | 100.1(2) | 17.93(2) |  | 857(11) |  |
| 15 | 3.5(1) | 20.0(5) |  | 5.258(7) | 9.09(1) | 18.19(2) | 100.0(2) | 17.91(1) |  | 856(9) |  |
| 16 | 3.5(2) | 20.0(5) |  | 5.288(7) | 9.09(1) | 18.17(2) | 99.7(2) | 17.91(1) |  | 861(10) |  |
| 17 | 3.5(3) | 20.0(5) |  | 5.288(5) | 9.10(1) | 18.17(1) | 99.8(1) | 17.905(9) |  | 861(6) |  |
| 18 | 3.8(2) | 20.0(5) |  | 5.290(8) | 9.08(1) | 18.13(2) | 99.4(1) | 17.880(9) |  | 859(6) |  |
| 19 | 4.3(3) | 20.0(5) |  | 5.281(7) | 9.07(1) | 18.05(2) | 99.7(2) | 17.80(1) |  | 853(10) |  |
| 20 | 5.1(2) | 20.0(5) |  | 5.271(7) | 9.06(2) | 18.00(3) | 99.7(1) | 17.74(1) |  | 847(7) |  |
| 21 | 5.6(2) | 20.0(5) |  | 5.27(1) | 9.05(3) | 17.92(3) | 99.9(3) | 17.65(2) |  | 841(14) |  |
| 22 | 6.3(2) | 20.0(5) |  | 5.249(9) | 9.12(2) | 17.84(3) | 100.1(2) | 17.57(1) |  | 841(8) |  |
| 23 | 6.7(2) | 20.0(5) |  | 5.241(8) | 9.12(2) | 17.86(2) | 100.50(9) | 17.561(7) |  | 839(5) |  |
| 24 | 7.4(3) | 20.0(5) |  | 5.235(8) | 9.11(2) | 17.77(2) | 100.5(1) | 17.475(8) |  | 833(5) |  |
| 25 | 7.8(3) | 20.0(5) |  | 5.206(9) | 9.13(3) | 17.71(1) | 100.7(1) | 17.396(9) |  | 827(6) |  |
| 26 | 8.4(3) | 20.0(5) |  | 5.23(1) | 9.17(1) | 17.63(3) | 100.2(4) | 17.36(3) |  | 831(21) |  |
| 27 | 9.2(3) | 20.0(5) |  | 5.22(2) | 9.06(4) | 17.53(4) | 99.8(5) | 17.27(4) |  | 816(24) |  |
| 28 | 10.0(2) | 20.0(5) |  | 5.185(8) | 9.09(2) | 17.58(2) | 100.9(1) | 17.26(1) |  | 813(8) |  |
| 29 | 10.4(3) | 20.0(5) |  | 5.15(1) | 9.03(2) | 17.44(5) | 100.8(2) | 17.13(2) |  | 796(11) |  |

TABLE 4. Experiment 2 refined unit cell parameters of wet talc at ambient and high temperatures; errors of 95% confidence limits determined in the Le Bail refinement. Basal spacing, c*, is measured directly from diffraction pattern.

| File | P (GPa) |  | T (oC) |  | a (Å) |  | b (Å) |  | c (Å) |  | β (°) |  | c* (Å) |  | V (Å3) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 |  | 20.0(5) |  | 5.280(5) |  | 9.143(5) |  | 19.06(2) |  | 100.42(9) |  | 18.744(8) |  | 905(5) |  |
| 2 | 0.8(2) |  | 20.0(5) |  | 5.277(8) |  | 9.21(2) |  | 18.78(30 |  | 100.7(3) |  | 18.45(2) |  | 897(14) |  |
| 3 | 0.8(2) |  | 20.0(5) |  | 5.278(8) |  | 9.21(3) |  | 18.79(4) |  | 100.7(3) |  | 18.46(2) |  | 898(16) |  |
| 4 | 0.8(1) |  | 20.0(5) |  | 5.276(8) |  | 9.22(2) |  | 18.78(3) |  | 100.7(2) |  | 18.45(2) |  | 897(13) |  |
| 5 | 1.0(2) |  | 20.0(5) |  | 5.26(2) |  | 9.16(3) |  | 18.70(6) |  | 100.6(6) |  | 18.38(5) |  | 885(32) |  |
| 6 | 1.3(2) |  | 20.0(5) |  | 5.27(1) |  | 9.20(3) |  | 18.79(4) |  | 100.7(3) |  | 18.46(3) |  | 896(18) |  |
| 7 | 1.4(2) |  | 20.0(5) |  | 5.278(9) |  | 9.14(2) |  | 18.71(3) |  | 100.2(2) |  | 18.42(2) |  | 889(13) |  |
| 8 | 1.5(3) |  | 20.0(5) |  | 5.269(8) |  | 9.19(2) |  | 18.75(4) |  | 100.7(3) |  | 18.42(2) |  | 892(16) |  |
| 9 | 1.5(2) |  | 20.0(5) |  | 5.270(7) |  | 9.18(2) |  | 18.66(3) |  | 100.8(3) |  | 18.33(2) |  | 887(15) |  |
| 10 | 1.6(2) |  | 20.0(5) |  | 5.270(7) |  | 9.18(2) |  | 18.68(3) |  | 100.8(2) |  | 18.34(2) |  | 888(13) |  |
| 11 | 1.7(2) |  | 20.0(5) |  | 5.269(8) |  | 9.19(2) |  | 18.69(3) |  | 100.8(3) |  | 18.37(2) |  | 889(16) |  |
| 12 | 1.9(3) |  | 20.0(5) |  | 5.26(1) |  | 9.15(3) |  | 18.60(4) |  | 100.6(4) |  | 18.29(3) |  | 881(22) |  |
| 13 | 2.0(2) |  | 20.0(5) |  | 5.27(1) |  | 9.13(2) |  | 18.51(4) |  | 99.8(3) |  | 18.25(2) |  | 877(16) |  |
| 14 | 2.2(2) |  | 20.0(5) |  | 5.26(1) |  | 9.12(2) |  | 18.50(4) |  | 99.8(3) |  | 18.23(2) |  | 874(15) |  |
| 15 | 2.3(3) |  | 20.0(5) |  | 5.26(1) |  | 9.14(3) |  | 18.54(5) |  | 100.7(4) |  | 18.22(4) |  | 875(25) |  |
| 16 | 2.4(2) |  | 20.0(5) |  | 5.26(1) |  | 9.14(2) |  | 18.53(3) |  | 99.9(2) |  | 18.25(2) |  | 878(12) |  |
| 17 | 2.7(2) |  | 20.0(5) |  | 5.281() |  | 9.11(2) |  | 18.42(4) |  | 99.8(3) |  | 18.15(2) |  | 873(14) |  |
| 18 | 2.8(2) |  | 20.0(5) |  | 5.26(2) |  | 9.10(2) |  | 18.38(4) |  | 99.9(3) |  | 18.11(2) |  | 866(15) |  |
| 19 | 2.9(2) |  | 20.0(5) |  | 5.26(1) |  | 9.11(2) |  | 18.37(3) |  | 100.2(3) |  | 18.08(2) |  | 866(15) |  |
| 20 | 3.0(3) |  | 20.0(5) |  | 5.272(8) |  | 9.13(2) |  | 18.44(4) |  | 100.1(2) |  | 18.15(1) |  | 874(9) |  |
| 21 | 3.3(2) |  | 20.0(5) |  | 5.25(1) |  | 9.11(2) |  | 18.35(3) |  | 100.1(2) |  | 18.06(2) |  | 863(12) |  |
| 22 | 3.8(2) |  | 20.0(5) |  | 5.25(1) |  | 9.10(2) |  | 18.27(3) |  | 100.3(3) |  | 17.97(2) |  | 858(14) |  |
| 23 | 4.3(2) |  | 20.0(5) |  | 5.29(1) |  | 9.10(2) |  | 18.24(4) |  | 99.5(2) |  | 17.99(1) |  | 865(9) |  |
| 24 | 4.3(2) |  | 20.0(5) |  | 5.285(4) |  | 9.071(6) |  | 18.11(1) |  | 99.70(7) |  | 17.858(5) |  | 856(4) |  |
| 25 | 4.5(2) |  | 20.0(5) |  | 5.284(4) |  | 9.071(7) |  | 18.10(2) |  | 99.71(7) |  | 17.843(5) |  | 855(4) |  |
| 26 | 5.1(3) |  | 20.0(5) |  | 5.277(4) |  | 9.067(8) |  | 18.09(2) |  | 99.80(8) |  | 17.827(6) |  | 853(4) |  |
| 27 | 5.2(2) |  | 20.0(5) |  | 5.276(4) |  | 9.068(8) |  | 18.09(3) |  | 99.66(8) |  | 17.831(6) |  | 853(4) |  |
| 28 | 5.5(2) |  | 20.0(5) |  | 5.272(5) |  | 9.054(9) |  | 18.09(3) |  | 99.7(1) |  | 17.829(8) |  | 851(5) |  |
| 29 | 5.6(2) |  | 20.0(5) |  | 5.257(6) |  | 9.049(8) |  | 18.01(2) |  | 100.1(1) |  | 17.736(8) |  | 844(5) |  |
| 30 | 6.0(2) |  | 20.0(5) |  | 5.267(5) |  | 9.04(1) |  | 18.01(3) |  | 99.8(1) |  | 17.744(9) |  | 845(6) |  |
| 31 | 6.2(2) |  | 20.0(5) |  | 5.257(6) |  | 9.03(1) |  | 18.00(3) |  | 99.9(1) |  | 17.73(1) |  | 842(7) |  |
| 32 | 6.5(3) |  | 20.0(5) |  | 5.212(7) |  | 9.03(1) |  | 17.92(2) |  | 100.5(1) |  | 17.62(1) |  | 829(8) |  |
| 33 | 6.7(2) |  | 20.0(5) |  | 5.236(8) |  | 9.13(2) |  | 17.94(3) |  | 100.3(1) |  | 17.66(1) |  | 844(8) |  |
| 34 | 6.8(2) |  | 20.0(5) |  | 5.220(6) |  | 9.13(1) |  | 17.92(2) |  | 100.6(1) |  | 17.61(1) |  | 840(7) |  |
| 35 | 7.2(3) |  | 20.0(5) |  | 5.212(6) |  | 9.12(2) |  | 17.87(2) |  | 100.7(2) |  | 17.55(1) |  | 835(9) |  |
| 36 | 8.0(3) |  | 20.0(5) |  | 5.227(7) |  | 9.10(1) |  | 17.84(3) |  | 100.2(1) |  | 17.56(1) |  | 836(7) |  |
| 37 | 8.1(3) |  | 20.0(5) |  | 5.224(8) |  | 9.10(2) |  | 17.79(3) |  | 100.3(2) |  | 17.50(1) |  | 832(10) |  |
| 38 | 8.4(3) |  | 20.0(5) |  | 5.214(8) |  | 9.10(1) |  | 17.79(2) |  | 100.4(1) |  | 17.497(9) |  | 829(6) |  |
| 39 | 9.0(3) |  | 20.0(5) |  | 5.185(8) |  | 9.06(2) |  | 17.75(2) |  | 101.1(3) |  | 17.42(2) |  | 819(15) |  |
| 40 | 9.3(3) |  | 20.0(5) |  | 5.205(7) |  | 9.10(2) |  | 17.74(3) |  | 100.5(1) |  | 17.45(1) |  | 826(8) |  |
| 41 | 9.4(3) |  | 20.0(5) |  | 5.194(5) |  | 9.20(2) |  | 17.83(2) |  | 100.7(2) |  | 17.52(1) |  | 837(10) |  |
| 42 | 10.0(3) |  | 20.0(5) |  | 5.201(9) |  | 9.12(2) |  | 17.73(3) |  | 100.8(3) |  | 17.41(2) |  | 826(15) |  |
| 43 | 10.1(3) |  | 20.0(5) |  | 5.193(6) |  | 9.05(1) |  | 17.28(3) |  | 100.6(2) |  | 17.18(2) |  | 807(12) |  |
| 44 | 10.6(3) |  | 20.0(5) |  | 5.192(6) |  | 9.06(1) |  | 17.58(2) |  | 100.5(2) |  | 17.37(2) |  | 817(12) |  |
| 45 | 11.1(3) |  | 20.0(5) |  | 5.192(6) |  | 9.06(1) |  | 17.58(2) |  | 100.5(2) |  | 17.28(2) |  | 813(12) |  |
| 46 | 11.6(3) |  | 20.0(5) |  | 5.183(7) |  | 9.05(1) |  | 17.71(2) |  | 100.4(3) |  | 17.42(2) |  | 817(14) |  |
| 47 | 0.8(5) |  | 100(10) |  | 5.28(1) |  | 9.15(2) |  | 19.09(2) |  | 101.1(2) |  | 18.73(2) |  | 905(12) |  |
| 48 | 0.9(5) |  | 100(10) |  | 5.28(1) |  | 9.14(2) |  | 19.08(3) |  | 101.1(2) |  | 18.72(2) |  | 904(14) |  |
| 49 | 1.4(5) |  | 100(10) |  | 5.25(1) |  | 9.20(3) |  | 18.70(3) |  | 100.4(2) |  | 18.39(2) |  | 888(12) |  |
| 50 | 3.8(5) |  | 100(10) |  | 5.32(3) |  | 9.07(7) |  | 18.13(7) |  | 99.5(4) |  | 17.89(3) |  | 862(18) |  |
| 51 | 3.9(5) |  | 100(10) |  | 5.26(1) |  | 9.10(2) |  | 18.29(3) |  | 100.0(2) |  | 18.01(2) |  | 861(11) |  |
| 52 | 4.4(5) |  | 100(10) |  | 5.19(2) |  | 9.07(5) |  | 18.15(4) |  | 100.3(4) |  | 17.86(3) |  | 840(21) |  |
| 53 | 5.7(5) |  | 100(10) |  | 5.27(2) |  | 9.07(5) |  | 17.96(7) |  | 99.3(4) |  | 17.73(3) |  | 847(17) |  |
| 54 | 6.3(5) |  | 100(10) |  | 5.180(8) |  | 9.19(3) |  | 17.88(3) |  | 99.2(2) |  | 17.65(2) |  | 841(11) |  |
| 55 | 7.6(5) |  | 100(10) |  | 5.20(2) |  | 9.48(4) |  | 17.79(5) |  | 99.4(2) |  | 17.55(1) |  | 866(8) |  |
| 56 | 7.6(5) |  | 100(10) |  | 5.191(8) |  | 9.19(2) |  | 17.81(3) |  | 100.7(2) |  | 17.50(2) |  | 835(13) |  |
| 57 | 9.3(5) |  | 100(10) |  | 5.17(2) |  | 9.20(4) |  | 17.51(6) |  | 100.3(3) |  | 17.23(3) |  | 819(17) |  |
| 58 | 10.4(5) |  | 100(10) |  | 5.160(6) |  | 9.15(2) |  | 17.53(2) |  | 100.2(1) |  | 17.25(1) |  | 815(7) |  |
| 59 | 0.3(5) |  | 200(20) |  | 5.29(1) |  | 9.15(1) |  | 19.12(2) |  | 101.1(2) |  | 18.76(2) |  | 908(11) |  |
| 60 | 0.6(5) |  | 200(20) |  | 5.29(1) |  | 9.13(2) |  | 19.07(3) |  | 100.2(3) |  | 18.76(2) |  | 906(14) |  |
| 61 | 0.7(5) |  | 200(20) |  | 5.274(8) |  | 9.16(1) |  | 19.13(2) |  | 101.2(1) |  | 18.76(1) |  | 907(8) |  |
| 62 | 0.7(5) |  | 200(20) |  | 5.24(2) |  | 9.1(3) |  | 18.93(3) |  | 99.8(3) |  | 18.65(3) |  | 890(21) |  |
| 63 | 1.0(5) |  | 200(20) |  | 5.24(3) |  | 9.12(7) |  | 18.98(5) |  | 100.1(5) |  | 18.69(4) |  | 893(30) |  |
| 64 | 1.0(5) |  | 200(20) |  | 5.28(2) |  | 9.16(3) |  | 18.93(4) |  | 100.0(3) |  | 18.64(3) |  | 902(19) |  |
| 65 | 1.3(5) |  | 200(20) |  | 5.273(9) |  | 9.15(2) |  | 18.76(3) |  | 100.3(2) |  | 18.46(1) |  | 890(10) |  |
| 66 | 1.3(5) |  | 200(20) |  | 5.22(1) |  | 9.13(4) |  | 19.06(2) |  | 101.8(2) |  | 18.66(2) |  | 890(13) |  |
| 67 | 2.5(5) |  | 200(20) |  | 5.40(2) |  | 9.08(4) |  | 18.31(4) |  | 99.3(2) |  | 18.07(2) |  | 886(12) |  |
| 68 | 2.7(5) |  | 200(20) |  | 5.26(1) |  | 9.11(1) |  | 18.37(3) |  | 99.7(2) |  | 18.11(2) |  | 868(12) |  |
| 69 | 4.3(5) |  | 200(20) |  | 5.19(1) |  | 9.09(1) |  | 18.07(3) |  | 98.7(2) |  | 17.86(1) |  | 843(7) |  |
| 70 | 5.6(5) |  | 200(20) |  | 5.251(7) |  | 9.05(1) |  | 18.06(3) |  | 99.9(2) |  | 17.79(1) |  | 846(8) |  |
| 71 | 6.5(5) |  | 200(20) |  | 5.27(4) |  | 8.97(4) |  | 17.98(4) |  | 100.0(4) |  | 17.65(3) |  | 835(21) |  |
| 72 | 6.7(5) |  | 200(20) |  | 5.216(9) |  | 9.03(2) |  | 17.91(3) |  | 99.6(2) |  | 17.66(2) |  | 832(11) |  |
| 73 | 6.9(5) |  | 200(20) |  | 5.29(2) |  | 9.16(5) |  | 17.83(7) |  | 99.5(4) |  | 17.58(3) |  | 852(19) |  |
| 74 | 7.7(5) |  | 200(20) |  | 5.191(9) |  | 9.60(2) |  | 17.73(3) |  | 99.6(1) |  | 17.48(1) |  | 871(7) |  |
| 75 | 7.7(5) |  | 200(20) |  | 5.179(8) |  | 9.01(1) |  | 17.79(3) |  | 100.0(2) |  | 17.52(2) |  | 817(12) |  |
| 76 | 8.1(5) |  | 200(20) |  | 5.21(1) |  | 9.07(2) |  | 17.46(5) |  | 99.3(2) |  | 17.23(1) |  | 813(8) |  |
| 77 | 8.7(5) |  | 200(20) |  | 5.178(9) |  | 9.01(2) |  | 17.65(2) |  | 100.1(2) |  | 17.37(2) |  | 810(12) |  |
| 78 | 9.7(5) |  | 200(20) |  | 5.204(6) |  | 9.08(2) |  | 17.60(2) |  | 99.5(1) |  | 17.36(1) |  | 820(8) |  |
| 79 | 11.3(5) |  | 200(20) |  | 5.156(8) |  | 9.02(2) |  | 17.52(2) |  | 100.5(2) |  | 17.23(2) |  | 801(10) |  |
| 80 | 12.0(5) |  | 200(20) |  | 5.139(9) |  | 9.11(2) |  | 17.52(2) |  | 100.7(2) |  | 17.22(1) |  | 806(9) |  |
| 81 | 13.6(5) |  | 200(20) |  | 5.167(7) |  | 9.04(2) |  | 17.39(2) |  | 100.4(2) |  | 17.11(1) |  | 799(8) |  |
| 82 | 0.2(5) |  | 300(30) |  | 5.29(2) |  | 9.14(3) |  | 19.10(4) |  | 100.2(4) |  | 18.79(3) |  | 909(20) |  |
| 83 | 1.6(5) |  | 300(30) |  | 5.272(9) |  | 9.15(3) |  | 18.67(3) |  | 100.1(2) |  | 18.38(1) |  | 887(10) |  |
| 84 | 3.3(5) |  | 300(30) |  | 5.279(5) |  | 9.12(2) |  | 18.54(3) |  | 100.01(6) |  | 18.262(5) |  | 879(3) |  |
| 85 | 3.6(5) |  | 300(30) |  | 5.27(1) |  | 9.11(2) |  | 18.28(2) |  | 99.6(1) |  | 18.03(1) |  | 866(7) |  |
| 86 | 4.0(5) |  | 300(30) |  | 5.27(2) |  | 9.08(5) |  | 18.01(8) |  | 99.2(4) |  | 17.78(3) |  | 851(19) |  |
| 87 | 4.1(5) |  | 300(30) |  | 5.43(1) |  | 9.12(4) |  | 18.29(4) |  | 99.4(2) |  | 18.05(2) |  | 894(11) |  |
| 88 | 5.1(5) |  | 300(30) |  | 5.260(8) |  | 9.07(1) |  | 18.05(3) |  | 99.8(2) |  | 17.79(2) |  | 848(10) |  |
| 89 | 5.7(5) |  | 300(30) |  | 5.43(2) |  | 8.80(4) |  | 18.32(6) |  | 104.4(3) |  | 17.75(3) |  | 849(19) |  |
| 90 | 6.2(5) |  | 300(30) |  | 5.227(8) |  | 9.04(1) |  | 17.96(2) |  | 99.5(2) |  | 17.71(1) |  | 837(8) |  |
| 91 | 7.4(5) |  | 300(30) |  | 5.200(9) |  | 9.03(1) |  | 17.81(3) |  | 100.1(3) |  | 17.53(2) |  | 823(14) |  |
| 92 | 8.9(5) |  | 300(30) |  | 5.171(8) |  | 9.02(1) |  | 17.71(3) |  | 100.6(2) |  | 17.41(2) |  | 812(12) |  |
| 93 | 11.4(5) |  | 300(30) |  | 5.155(6) |  | 9.01(1) |  | 17.49(2) |  | 100.8(1) |  | 17.18(1) |  | 798(7) |  |
| 94 | 13.6(5) |  | 300(30) |  | 5.144(8) |  | 9.01(2) |  | 17.58(2) |  | 100.9(2) |  | 17.26(1) |  | 800(8) |  |
| 95 | 3.9(5) |  | 400(40) |  | 5.28(2) |  | 9.09(4) |  | 18.05(6) |  | 99.4(3) |  | 17.81(2) |  | 855(16) |  |
| 96 | 4.1(5) |  | 400(40) |  | 5.33(2) |  | 9.26(4) |  | 18.22(6) |  | 99.7(2) |  | 17.96(2) |  | 886(11) |  |
| 97 | 4.3(5) |  | 400(40) |  | 5.284(7) |  | 9.09(4) |  | 18.02(7) |  | 99.4(3) |  | 17.78(2) |  | 854(17) |  |
| 98 | 4.8(5) |  | 400(40) |  | 5.22(2) |  | 9.28(5) |  | 17.87(8) |  | 99.4(4) |  | 17.63(3) |  | 854(18) |  |
| 99 | 5.3(5) |  | 400(40) |  | 5.33(3) |  | 9.30(4) |  | 18.02(6) |  | 99.7(2) |  | 17.76(2) |  | 881(11) |  |
| 100 | 6.2(5) |  | 400(40) |  | 5.24(2) |  | 9.04(4) |  | 17.88(4) |  | 100.2(3) |  | 17.59(2) |  | 833(14) |  |
| 101 | 7.1(5) |  | 400(40) |  | 5.20(1) |  | 9.26(5) |  | 17.69(6) |  | 99.8(2) |  | 17.43(2) |  | 839(12) |  |
| 102 | 7.4(5) |  | 400(40) |  | 5.20(2) |  | 9.26(5) |  | 17.69(6) |  | 99.8(3) |  | 17.43(2) |  | 839(13) |  |
| 103 | 10.7(5) |  | 400(40) |  | 5.21(1) |  | 9.07(3) |  | 17.33(6) |  | 99.9(2) |  | 17.07(2) |  | 807(10) |  |