3 Supplementary Tables for Paper Geiger et al. Aug/Sept Am Min 2012

AM-12-059

Supplementary Table 1. (supplementary information) Smoothed molar thermodynamic

functions for end-member grossular between 5 and 298.15 K

(M = 450.454 g/mol). Φ ≡ (ST - S0) - (HT - H0)/T

| T | Cp | (ST-S0) | (HT-H0)/T | Φ |
| --- | --- | --- | --- | --- |
| (K) | (J/mol∙K) | (J/mol∙K) | (J/mol∙K) | (J/mol∙K) |
| 5 | 0.012 | 0.004 | 0.003 | 0.0010 |
| 6 | 0.021 | 0.007 | 0.005 | 0.0018 |
| 7 | 0.034 | 0.011 | 0.008 | 0.0028 |
| 8 | 0.051 | 0.017 | 0.013 | 0.0042 |
| 9 | 0.073 | 0.024 | 0.018 | 0.0060 |
| 10 | 0.101 | 0.033 | 0.025 | 0.0082 |
| 11 | 0.137 | 0.044 | 0.033 | 0.0110 |
| 12 | 0.179 | 0.058 | 0.044 | 0.0143 |
| 13 | 0.230 | 0.074 | 0.056 | 0.0183 |
| 14 | 0.290 | 0.094 | 0.071 | 0.0230 |
| 15 | 0.360 | 0.116 | 0.087 | 0.0284 |
| 20 | 0.879 | 0.283 | 0.214 | 0.0690 |
| 25 | 1.810 | 0.569 | 0.431 | 0.1381 |
| 30 | 3.341 | 1.024 | 0.779 | 0.245 |
| 35 | 5.597 | 1.699 | 1.297 | 0.402 |
| 40 | 8.613 | 2.635 | 2.015 | 0.620 |
| 45 | 12.453 | 3.863 | 2.954 | 0.909 |
| 50 | 17.025 | 5.405 | 4.127 | 1.279 |
| 60 | 28.016 | 9.446 | 7.160 | 2.286 |
| 70 | 41.086 | 14.722 | 11.051 | 3.671 |
| 80 | 55.778 | 21.152 | 15.709 | 5.443 |
| 90 | 71.60 | 28.63 | 21.03 | 7.59 |
| 100 | 88.07 | 37.02 | 26.91 | 10.11 |
| 110 | 104.78 | 46.20 | 33.23 | 12.97 |
| 120 | 121.40 | 56.03 | 39.89 | 16.14 |
| 130 | 137.71 | 66.39 | 46.79 | 19.61 |
| 140 | 153.58 | 77.18 | 53.85 | 23.33 |
| 150 | 168.92 | 88.30 | 61.01 | 27.29 |
| 160 | 183.68 | 99.68 | 68.22 | 31.46 |
| 170 | 197.85 | 111.24 | 75.43 | 35.81 |
| 180 | 211.43 | 122.94 | 82.61 | 40.33 |
| 190 | 224.42 | 134.72 | 89.74 | 44.98 |
| 200 | 236.82 | 146.55 | 96.78 | 49.77 |
| 210 | 248.67 | 158.39 | 103.74 | 54.66 |
| 220 | 259.95 | 170.22 | 110.58 | 59.64 |
| 230 | 270.71 | 182.01 | 117.31 | 64.69 |
| 240 | 280.94 | 193.76 | 123.92 | 69.84 |
| 250 | 290.67 | 205.43 | 130.40 | 75.03 |
| 260 | 299.92 | 217.01 | 136.74 | 80.27 |
| 270 | 308.71 | 228.49 | 142.95 | 85.54 |
| 280 | 317.05 | 239.87 | 149.02 | 90.85 |
| 290 | 324.97 | 251.14 | 154.95 | 96.19 |
| 298.15 | 331.12 | 260.23 | 159.68 | 100.55 |

Table 2a. (Supplementary information) Microprobe

results on synthetic grossular in terms of oxides

and cations (based on 8 cations and 12 oxygens).

| Oxides | Gr - Has* | Gr - 92 | Gr - Kiel |
| --- | --- | --- | --- |
| SiO2 | 38.46 | 38.61 | 39.81 |
| TiO2 | 0.01 | 0.01 | 0.01 |
| Al2O3 | 23.54 | 23.37 | 22.66 |
| Cr2O3 | 0.01 | 0.01 | - |
| FeO | 0.02 | 0.02 | 0.03 |
| MgO | 0.02 | 0.02 | 0.02 |
| CaO | 37.66 | 37.66 | 37.63 |
| V2O3 | 0.05 | 0.03 | 0.03 |
| Total | 99.77 | 99.73 | 100.19 |

| Cations |  |  |  |
| --- | --- | --- | --- |
| Si | 2.90 | 2.91 | 2.98 |
| Ti | - | - | - |
| Al | 2.09 | 2.07 | 3.02 |
| Cr | - | - | - |
| Fe | - | - | - |
| Mg | - | - | - |
| Ca | 3.04 | 3.04 | 3.02 |
| V | - | - | - |
| Total | 8.03 | 8.02 | 8.02 |

*On sample chip showing little to no inclusions.

- Table 2b. (Supplementary information) Microprobe results on the

- four natural grossulars in terms of oxide components.

| Oxides | Gr-82-112 | Gr-44091 | Gr-1/1 | Gr-L/K |
| --- | --- | --- | --- | --- |
| SiO2 | 39.69 | 39.29 | 39.32 | 39.49 |
| TiO2 | 0.01 | 0.06 | 0.49 | 0.42 |
| Al2O3 | 22.47 | 22.47 | 22.06 | 22.18 |
| Cr2O3 | 0.01 | - | 0.01 | 0.03 |
| FeO | 0.41 | 1.41 | 0.32 | 0.07 |
| MnO | 0.08 | 0.65 | 0.35 | 0.55 |
| MgO | 0.03 | 0.02 | 0.34 | 0.48 |
| CaO | 37.43 | 35.81 | 36.75 | 36.41 |
| V2O3 | 0.04 | 0.03 | 0.09 | 0.29 |
| H2O | 0.3* | 0.3* | 0.2* | 0.2* |
| Total | 100.47 | 100.04 | 99.93 | 100.12 |

* from Rossman and Aines (1989)

Supplementary Table 3. (supplementary information) Parameters for

calculating smoothed values of the heat capacity

of grossular from Eq. (3) between 0 and 298 K.

Parameters were derived by fitting the final

heat capacity data of synthetic grossular,

as described in the text, with Eq. (3).

|  | grossular |
| --- | --- |
|  | synthetic |
| Low temperature |  |
| n (mol) | 11.627615 |
| θD (K) | 613.0849 |
| m (mol) | 0.843008 |
| θE (K) | 230.3562 |
| ns (mol) | 0.011577 |
| θS (K) | 88.4413 |
| Tswitch (K) | 41.41 |
| High temperature |  |
| n (mol) | 13.685281 |
| θD (K) | 652.9196 |
| m (mol) | 6.492280 |
| θE (K) | 1121.9173 |
| ns (mol) | 1.069298 |
| θS (K) | 237.4916 |