Scordari et al.: FLUOROPHLOGOPITE FROM PIANO DELLE CONCAZZE (Mt. ETNA, ITALY); Deposit material (7 total items); AM-13-046; American Mineralogist May June 2013

Table 3   Crystallographic coordinates and displacement parameters of the studied micas. In square brackets are quoted  the cations used for occupancy refinement

.

| Atom | x/a | y/b | z/c | Occupancy | Uiso | U11 | U22 | U33 | U12 | U13 | U23 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| # Sample | E0 |  |  |  |  |  |  |  |  |  |  |
| K | 0 | 0 | 0 | 0.9049(9) | 0.0318 | 0.0331(10) | 0.0300(6) | 0.0325(6) | 0 | 0.0059(7) | 0 |
| T[Si] | 0.5745(1) | 0.16681(5) | 0.22369(5) | 0.9861(10) | 0.0092 | 0.0086(3) | 0.0074(2) | 0.0119(2) | 0.0001(2) | 0.0026(2) | 0.0002(2) |
| M1[Mg] | 0 | 0.5 | 0.5 | 0.7726(8) | 0.0098 | 0.0088(6) | 0.0060(3) | 0.0154(4) | 0 | 0.0042(4) | 0 |
| M1[Fe] | 0 | 0.5 | 0.5 | 0.2277(7) | 0.0098 | 0.0088(6) | 0.0060(3) | 0.0154(4) | 0 | 0.0042(4) | 0 |
| M2[Mg] | 0 | 0.83604(9) | 0.5 | 0.8113(8) | 0.0105 | 0.0074(4) | 0.0119(3) | 0.0125(3) | 0 | 0.0025(3) | 0 |
| M2[Fe] | 0 | 0.83604(9) | 0.5 | 0.1889(7) | 0.0105 | 0.0074(4) | 0.0119(3) | 0.0125(3) | 0 | 0.0025(3) | 0 |
| O1 | 0.8176(4) | 0.2381(2) | 0.1652(2) | 1.0000(8) | 0.0183 | 0.0162(10) | 0.0225(7) | 0.0165(6) | -0.0011(5) | 0.0038(7) | -0.0064(6) |
| O2 | 0.5302(6) | 0 | 0.1655(2) | 1.0000(8) | 0.0186 | 0.028(2) | 0.0119(7) | 0.0153(8) | 0 | 0.0012 (9) | 0 |
| O3 | 0.6304(3) | 0.1675(2) | 0.3898(1) | 1.0000(8) | 0.0100 | 0.0097(7) | 0.0084(4) | 0.0125(4) | -0.0001(4) | 0.0035(5) | 0.0005(5) |
| F4 | 0.1306(5) | 0 | 0.4003(2) | 1.0000(8) | 0.0129 | 0.0129(11) | 0.0118(6) | 0.0147(7) | 0 | 0.0044(8) | 0 |
| # Sample | # E1 |  |  |  |  |  |  |  |  |  |  |
| K | 0 | 0 | 0 | 0.9131(7) | 0.0314 | 0.0314(4) | 0.0313(5) | 0.0308(4) | 0 | 0.0042(3) | 0 |
| T[Si] | 0.57457(6) | 0.16688(4) | 0.22366(4) | 0.9819(9) | 0.0089 | 0.0079(1) | 0.0083(1) | 0.0103(1) | 0.0000(1) | 0.0011(1) | 0.0000(1) |
| M1[Mg] | 0 | 0.5 | 0.5 | 0.7762(8) | 0.0094 | 0.0077(2) | 0.0070(2) | 0.0136(3) | 0 | 0.0024(2) | 0 |
| M1[Fe] | 0 | 0.5 | 0.5 | 0.2236(6) | 0.0094 | 0.0077(2) | 0.0070(2) | 0.0136(3) | 0 | 0.0024(2) | 0 |
| M2[Mg] | 0 | 0.83630(6) | 0.5 | 0.8019(8) | 0.0108 | 0.0066(2) | 0.0138(2) | 0.0118(2) | 0 | 0.0007(1) | 0 |
| M2[Fe] | 0 | 0.83630(6) | 0.5 | 0.1980(7) | 0.0108 | 0.0066(2) | 0.0138(2) | 0.0118(2) | 0 | 0.0007(1) | 0 |
| O1 | 0.8170(2) | 0.2377(1) | 0.1651(1) | 1.0000(8) | 0.0177 | 0.0160(4) | 0.0231(5) | 0.0139(4) | -0.0015(3) | 0.0027(3) | -0.0060(4) |
| O2 | 0.5303(3) | 0 | 0.1657(2) | 1.0000(8) | 0.0179 | 0.0260(7) | 0.0126(5) | 0.0139(6) | 0 | 0.0003(5) | 0 |
| O3 | 0.6307(2) | 0.1676(1) | 0.38978(9) | 1.0000(8) | 0.0103 | 0.0097(3) | 0.0102(3) | 0.0107(3) | -0.0002(3) | 0.0013(2) | 0.0004(3) |
| F4 | 0.1298(2) | 0 | 0.4008(1) | 1.0000(8) | 0.0128 | 0.0108(4) | 0.0142(5) | 0.0134(5) | 0 | 0.0019(4) | 0 |

| Atom | x/a | y/b | z/c | Occupancy | Uiso | U11 | U22 | U33 | U12 | U13 | U23 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| # Sample | E2 |  |  |  |  |  |  |  |  |  |  |
| K | 0 | 0 | 0 | 0.8939(8) | 0.0316 | 0.0317(5) | 0.0311(5) | 0.0319(5) | 0 | 0.0052(4) | 0 |
| T[Si] | 0.57444(7) | 0.16685(4) | 0.22370(4) | 0.9862(9) | 0.0088 | 0.0086(1) | 0.0076(1) | 0.0104(2) | 0.0000(1) | 0.0020(1) | 0.0001(1) |
| M1[Mg] | 0 | 0.5 | 0.5 | 0.7759(8) | 0.0092 | 0.0083(3) | 0.0062(3) | 0.0138(3) | 0 | 0.0036(2) | 0 |
| M1[Fe] | 0 | 0.5 | 0.5 | 0.2237(6) | 0.0092 | 0.0083(3) | 0.0062(3) | 0.0138(3) | 0 | 0.0036(2) | 0 |
| M2[Mg] | 0 | 0.83595(7) | 0.5 | 0.8068(8) | 0.0104 | 0.0069(2) | 0.0126(2) | 0.0120(2) | 0 | 0.0020(2) | 0 |
| M2[Fe] | 0 | 0.83595(7) | 0.5 | 0.1932(7) | 0.0104 | 0.0069(2) | 0.0126(2) | 0.0120(2) | 0 | 0.0020(2) | 0 |
| O1 | 0.8166(2) | 0.2379(2) | 0.1650(1) | 1.0000(8) | 0.0181 | 0.0167(5) | 0.0227(6) | 0.0151(5) | -0.0014(4) | 0.0037(4) | -0.0059(4) |
| O2 | 0.5304(4) | 0 | 0.1655(2) | 1.0000(8) | 0.0182 | 0.0261(8) | 0.0132(6) | 0.0145(7) | 0 | 0.0014 (6) | 0 |
| O3 | 0.6308(2) | 0.1673(1) | 0.3899(1) | 1.0000(8) | 0.0095 | 0.0088(3) | 0.0085(3) | 0.0114(4) | -0.0003(3) | 0.0024(3) | 0.0004(3) |
| F4 | 0.1307(3) | 0 | 0.4004(2) | 1.0009(8) | 0.0130 | 0.0111(5) | 0.0140(6) | 0.0144(6) | 0 | 0.0034(4) | 0 |
| # Sample | # E3 |  |  |  |  |  |  |  |  |  |  |
| K | 0 | 0 | 0 | 0.8970(7) | 0.0311 | 0.0318(3) | 0.0312(4) | 0.0299(3) | 0 | 0.0048(3) | 0 |
| T[Si] | 0.57472(5) | 0.16681(3) | 0.22370(3) | 0.9808(9) | 0.0090 | 0.0088(1) | 0.0083(1) | 0.0099(1) | 0.0000(1) | 0.0017(1) | 0.0001(1) |
| M1[Mg] | 0 | 0.5 | 0.5 | 0.7672(7) | 0.0098 | 0.0087(2) | 0.0078(2) | 0.0135(2) | 0 | 0.0032(1) | 0 |
| M1[Fe] | 0 | 0.5 | 0.5 | 0.2323(6) | 0.0098 | 0.0087(2) | 0.0078(2) | 0.0135(2) | 0 | 0.0032(1) | 0 |
| M2[Mg] | 0 | 0.83616(5) | 0.5 | 0.7932(7) | 0.0111 | 0.0077(1) | 0.0140(2) | 0.0115(1) | 0 | 0.0014(1) | 0 |
| M2[Mg] | 0 | 0.83616(5) | 0.5 | 0.2065(6) | 0.0111 | 0.0077(1) | 0.0140(2) | 0.0115(1) | 0 | 0.0014(1) | 0 |
| O1 | 0.8170(2) | 0.2379(1) | 0.16507(8) | 1.0000(8) | 0.0187 | 0.0173(3) | 0.0244(4) | 0.0145(3) | -0.0016(3) | 0.0032(2) | -0.0069(3) |
| O2 | 0.5306(3) | 0 | 0.1658(1) | 1.0000(8) | 0.0183 | 0.0272(6) | 0.0128(4) | 0.0139(4) | 0 | 0.0012(4) | 0 |
| O3 | 0.6309(1) | 0.16750(8) | 0.38995(7) | 1.0000(8) | 0.0104 | 0.0105(2) | 0.0104(2) | 0.0102(4) | 0.0001(2) | 0.0016(2) | 0.0005(2) |
| F4 | 0.1302(2) | 0 | 0.4005(1) | 1.0008(7) | 0.0129 | 0.0119(3) | 0.0142(4) | 0.0127(3) | 0 | 0.0023(3) | 0 |